Direct visualization of orbital electron occupancy

Tongtong Shang1,2†, Dongdong Xiao1,3†, Fanqi Meng4†, Xiaohui Rong1, Xiaozhi Liu1,2, Xinyan Li1,2, Qinghua Zhang1, Yuren Wen5, Xuefeng Wang1,2, Dong Su1,2, Yong-sheng Hu1,2, Hong Li1,2, Qian Yu6, Ze Zhang6, Vaclav Petricek7, Lijun Wu8*, Lin Gu1,2,3*, Jian-Min Zuo9, Yimei Zhu8, Ce-Wen Nan4, Jing Zhu10

Affiliations:

1Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, P. R. China

2School of Physical Sciences, University of Chinese Academy of Sciences, Beijing 100049, China

3Songshan Lake Materials Laboratory, Dongguan, Guangdong 523808, P. R. China

4State Key Lab of New Ceramics and Fine Processing, School of Materials Science and Engineering, Tsinghua University, 100084 Beijing, P. R. China

5School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing 100083, P. R. China

6Department of Materials Science and Engineering, Center of Electron Microscopy and State Key Laboratory of Silicon Materials, Zhejiang University, 310027, Hangzhou, P. R. China

7Institute of Physics, Academy of Sciences of the Czech Republic, 2, 180 40 Praha 8, Czech Republic

8Condensed Matter Physics and Materials Science Division, Brookhaven National Laboratory, Upton, New York 11973, USA

9Department of Materials Science and Engineering, University of Illinois at Urbana Champaign, 1304 W Green St, Urbana, IL 61801, USA

10Beijing National Center for Electron Microscopy, Laboratory of Advanced Materials, Department of Materials Science and Engineering, Tsinghua University, Beijing 100084, P. R. China

*Email: ljwu@bnl.gov; l.gu@iphy.ac.cn

Supplementary Text

Mapping the electron density

The refinement and extraction of low-order structure factors were performed using the Program Wu1. The refined parameters are electron-beam incident direction, sample thickness, and structure factors. To avoid very large matrices and a reasonable accuracy for the Bloch wave theory, beams were selected according to certain criteria2. We chose 2.6 for gmax, 3.0 for 2KSgmax, 0.005 for Umax2KSg.

Using the Mott-Bethe formula we can convert electron structure factors to X-ray structure factors, and replace the corresponding structure factors to perform a multipole refinement. The refined low-order electron and x-ray structure factors are listed in Table S1-S4 of Li1-xCoO2. The high-order X-ray structure factors are mainly determined by the atomic position, atomic displacement parameters, and core electrons. It can be refined and extracted using Rietveld refinement from SPXRD.

All Rietveld refinement and multipole refinement were performed in JANA20063 with scattering factors derived from Slater-type orbitals (STO) atomic relativistic wavefunctions. The Rietveld refinements are shown in Fig. S5-S8. To accurately extract the high-order structure factors, the resolution of the data was cut off from 1.67 Å-1 to 1.2 Å-1, where the overlap between diffraction peaks was severe. Since the multipole model4 is based on spherical harmonic density functions centered around each atomic nucleus, the limit lmax = 4 was used for truncation of the multipole expansion at the hexadecapole level. The functions allowed for a particular site are symmetrically restricted. The coordinate systems used for both Co (3m) and O (3m) are that the z-axis is parallel to the 3-fold axis [001] direction, and the y axis is perpendicular to the mirror plane, i.e. alone [010] direction. Several constraints were imposed on the multipole refinement: the valence population of Li ion was fixed at Pv = 0, κ[Li] = 1 and the electron deformation density of Li was not refined. For Co, only the seven 3d electrons were considered as valence electrons. The two 4s electrons were treated as core electrons, since the 4s electrons contribute very little to the scattering factors5. The topological electron density analysis of the obtained total electron densities based on Bader’s quantum theory of atoms in molecules was also calculated using JANA2006. The results for the bond critical points are shown in Table 1.

Co 3d-orbital populations

In Li1-xCoO2, the CoO6 octahedra is within a trigonally distorted field. The 3d electron density can be expressed by5

ρ3d=[R(r)]2P1(a1)2+(1/2)P2[eg-2+eg+2]+(1/2)P3[eg-'2+(eg+')2],     (S1)

where R(r) is the radial function, (a1), (eg-) and eg+ correspond to the three t2g orbitals, eg-' and eg+' correspond to the two eg orbitals. P1, P2 and P3 are the occupancies of the (a1), (eg) and eg', respectively.

The relationship between the occupancies of 3d orbital and the populations of spherical density functions, which are refined from multipole modelling, is given by

P1=1/3P00+1/7[(196π/5)1/2/M20]P20+(3/35)[(196π)1/2/M40]P40

P2=2/3P00-5/7[(196π/5)1/2/M20]P20+(6/35)[(196π)1/2/M40]P40-2P4

P3=1/3P00+4/7[(196π/5)1/2/M20]P20-(9/35)[(196π)1/2/M40]P40+2P4    (S2)

P4=3/(62+1)-9/7[(196π/5)1/2/M20]P20+3/7[196π12/M40]P40+[(63π/5)1/2/M43]P43+,

where the P00, P20, P40, P43+ are the refined populations of spherical harmonic density functions, respectively. Mlm denotes the ratio of normalization factors for wave functions and density functions. The Co 3d-orbital occupancies can be calculated according to Eq. S2.

Fig. S1. STEM-HAADF images of Li1-xCoO2 along the [100] zone axis.

(A) pristine LiCoO2, (B) Li0.6CoO2, (C) Li0.4CoO2, (D) Li0.3CoO2. Scale bar: 2 nm

Fig. S2. Initial charge-discharge curves of LiCoO2, charge to 4.6 V and then discharge to 3.0 V versus Li/Li+.

The green circles from the left to the right correspond to x=0.4, 0.6, 0.7, respectively.

Fig. S3. 3D rendering of the static deformation density map of the CoO6 octahedra for Li0.3CoO2.

In this map, the color scheme ranges from -0.2 to 0.2 e Å-3 and can offer more information compared to Fig. 3I.

Fig. S4. Laplacian maps in the (014) plane.

(A) LiCoO2 (B) Li0.6CoO2, (C) Li0.4CoO2, (D) Li0.3CoO2. contours are drawn at ± 2×10n, ± 4×10n and ± 8×10n e Å-5 (n = ± 3, ± 2, ± 1, 0), with solid red and dotted blue lines for positive and negative values, respectively.

Fig. S5. Rietveld refinement for the SPXRD pattern of LiCoO2.

Fig. S6. Rietveld refinement for the SPXRD pattern of Li0.6CoO2.

Fig. S7. Rietveld refinement for the SPXRD pattern of Li0.4CoO2.

Fig. S8. Rietveld refinement for the SPXRD pattern of Li0.3CoO2.

Table S1. Low-order structure factors measurement using CBED of LiCoO2.

| Reflection | FECBED | χ2 | FXCon | FXObs |
| --- | --- | --- | --- | --- |
| 003 | -12.0281 | 0.128 | -75.2026 | -74.7950 |
| 011 | -7.7820 | 8.255 | -54.8774 | -54.9590 |
| 006 | 5.2031 | 0.128 | 35.0276 | 35.3030 |
| 012 | 4.6897 | 2.640 | 32.9610 | 33.7800 |
| 014 | 17.6667 | 5.131 | 88.8956 | 90.5540 |

FECBED denotes the refined electron-structure-factors from CBED. χ2 is the goodness of fit. FXCon represents the X-ray structure factors converted from electron-structure factors using the Mott-Bethe formula. FXObs stands for the X-ray structure factors obtained using the synchrotron powder XRD.

Table S2. Low-order structure factors measurement using CBED of Li0.6CoO2.

| Reflection | FECBED | χ2 | FXCon | FXObs |
| --- | --- | --- | --- | --- |
| 003 | -15.2838 | 2.447 | -80.4759 | -80.0610 |
| 011 | -8.2820 | 1.235 | -56.2763 | -57.5079 |
| 006 | 4.0447 | 2.447 | 36.9176 | 35.1539 |
| 012 | 4.8031 | 4.154 | 29.4540 | 30.1469 |
| 014 | 17.6636 | 2.345 | 84.4921 | 86.3889 |

FECBED denotes the refined electron-structure-factors from CBED. χ2 is the goodness of fit. FXCon stands for the X-ray structure factors converted from electron-structure factors using the Mott-Bethe formula. FXObs represents the X-ray structure factors obtained using synchrotron powder XRD.

Table S3. Low-order structure factors measurement using CBED of Li0.4CoO2.

| Reflection | FECBED | χ2 | FXCon | FXObs |
| --- | --- | --- | --- | --- |
| 003 | -19.0487 | 0.439 | -82.2019 | -81.8140 |
| 011 | -7.8576 | 0.483 | -58.3635 | -57.0550 |
| 006 | 4.8761 | 0.439 | 36.2501 | 37.2120 |
| 012 | 3.2848 | 2.107 | 30.9666 | 31.0820 |
| 014 | 16.6159 | 0.976 | 84.6782 | 87.9260 |

FECBED denotes the refined electron-structure-factors from CBED. χ2 is the goodness of fit. FXCon represents the X-ray structure factors converted from electron-structure factors using the Mott-Bethe formula. FXObs stands for the X-ray structure factors obtained using synchrotron powder XRD.

Table S4. Low-order structure factors measurement using CBED of Li0.3CoO2.

| Reflection | FECBED | χ2 | FXCon | FXObs |
| --- | --- | --- | --- | --- |
| 003 | -17.0316 | 0.463 | -83.3051 | -82.5350 |
| 011 | -8.5585 | 1.364 | -58.1658 | -57.2490 |
| 006 | 3.6727 | 0.463 | 36.4529 | 35.9679 |
| 012 | 3.3336 | 0.414 | 29.9553 | 31.4750 |
| 014 | 15.7307 | 1.372 | 86.4530 | 86.9929 |

FECBED denotes the refined electron-structure-factors from CBED. χ2 is the goodness of fit. FXCon stands for the X-ray structure factors converted from electron-structure factors using the Mott-Bethe formula. FXObs represents the X-ray structure factors obtained using synchrotron powder XRD.

Table S5. Lattice parameters, atomic coordinates, bond length, and bond angle of Li1-xCoO2.

| Parameters | LiCoO2 | Li0.6CoO2 | Li0.4CoO2 | Li0.3CoO2 |
| --- | --- | --- | --- | --- |
| a (Å) | 2.812792(4) | 2.812155(14) | 2.80962(4) | 2.808697(16) |
| c (Å) | 14.02096(3) | 14.17254(18) | 14.2662(6) | 14.2924(2) |
| z(O) | 0.23989(5) | 0.23646(8) | 0.23501(15) | 0.23541(13) |
| Co-O bond length (Å) | 1.9213(4) | 1.9012(6) | 1.8927(12) | 1.8960(10) |
| O-O spacing (Å) | 2.6179(12) | 2.5592(18) | 2.537(4) | 2.548(3) |
| CoO6 angle (°) | 85.89(3) | 84.61(4) | 84.16(8) | 84.42(7) |

Table S6. Results from multipole refinement of the experimental data.

| Parameters | LiCoO2 | Li0.6CoO2 | Li0.4CoO2 | Li0.3CoO2 |
| --- | --- | --- | --- | --- |
| (sinθ/λ)max (Å-1) | 1.2 | 1.2 | 1.2 | 1.2 |
| R(F2) (%) | 1.39 | 1.86 | 1.49 | 1.04 |
| wR(F2) (%) | 2.10 | 2.12 | 2.20 | 1.58 |
| Nrefl | 222 | 217 | 219 | 220 |
| U11, U33(Li) (Å2) | 0.006246 (1125) 0.010248 (1818) | 0.012628 (2809) 0.005017 (2961) | 0.00933 (3309) 0.004931 (3561) | 0.007591 (2780) 0.004703 (3253) |
| U11, U33(Co) (Å2) | 0.001333 (172) 0.002367 (186) | 0.001842 (204) 0.001596 (231) | 0.000883 (191) 0.002034 (192) | 0.001166 (156) 0.001885 (156) |
| U11, U33(O) (Å2) | 0.003567 (612) 0.000403 (1269) | 0.002885 (275) 0.003163 (374) | 0.000839 274) 0.008891 (385) | 0.001729 (212) 0.006926 (248) |
| Pv(Co) | 6.50(22) | 6.44(27) | 6.66 (33) | 7.24 (29) |
| Pv(O) | 6.75(11) | 6.58 (13) | 6.37(16) | 6.03(14) |
| P20, P40, P43+(Co) | 0.291(57) 0.367(46) -0.296(42) | 0.103 (69) 0.228 (39) -0.040 (32) | 0.763 (216) 1.698 (371) 0.790 (364) | 0.449 (273) 0.893 (502) 1.256 (423) |
| P10, P20, P30, P33+, P40, P43+(O) | -0.003(40) 0.295(97) -0.032(24) -0.003(25) 0.075(30) -0.063(31) | -0.056 (83) 0.228 (103) 0.031 (95) 0.153 (98) 0.220 (104) -0.139 (87) | 0.016 (85) 0.117 (101) 0.064 (101) 0.001 (89) 0.173 (156) 0.120 (134) | -0.225 (123) 0.115 (132) -0.094 (131) 0.267 (200) 0.514 (182) 0.014 (187) |
| κ, κ'(Co) | 1.03(4), 1.95(9) | 1.06(5), 2.20(25) | 1.05(5), 0.62(4) | 1.04(3), 0.55(5) |
| κ, κ'(O) | 1.00(2), 2.12(4) | 1.00 (2), 0.79 (14) | 1.00(2), 0.82(24) | 1.02(2), 0.56(10) |

Reference

1.	Ma C, Wu L, Yin W-G, Yang H, Shi H, Wang Z, et al. Strong Coupling of the Iron-Quadrupole and Anion-Dipole Polarizations in Ba(Fe1-xCox)(2)As-2. Physical Review Letters 2014, 112(7).

2.	Zuo JM, Weickenmeier AL. ON THE BEAM SELECTION AND CONVERGENCE IN THE BLOCH-WAVE METHOD. Ultramicroscopy 1995, 57(4): 375-383.

3.	Václav P, Michal D, Lukáš P. Crystallographic Computing System JANA2006: General features. Zeitschrift für Kristallographie - Crystalline Materials 2014, 229(5): 345-352.

4.	Hansen NK, Coppens P. Testing aspherical atom refinements on small-molecule data sets. Acta Crystallographica Section A 1978, 34(6): 909-921.

5.	Stevens ED, Coppens P. Refinement of metal d-orbital occupancies from X-ray diffraction data. Acta Crystallographica Section A 1979, 35(4): 536-539.