Figure 1S: Guaiacol conversion under different rpm over Pt-AC Commercial and Pt-ACS-11. Operation conditions: 200 °C, 12 atm of H2, 200 min and mass ratio guaiacol/cat=5.6 and catalyst particle diameter 0.4 mm.

Figure 2S: Guaiacol conversion vs different particle diameter over Pt-AC Commercial and Pt-ACS-11. Operation conditions: 200 °C, 12 atm of H2, 200 min and mass ratio guaiacol/cat=5.6 and 360 rpm.