Extended abstract

In this work, it was shown that, although the ZnO amount in F1 sample was higher than F3 but the K2O role as modifier is responsible for the decreasing of the melting temperature. This means that K2O can breaks up the network more effectively than ZnO and CaO, respectively. K2O has a lower IFS than ZnO, and CaO, thus the decreased the Tm in F1. In addition, the potassium ions lead to an increase in the size of the interstices of the glass network and increase the free volume of the network. Therefore, F1 frites has larger molar volumes than the other frites. This offsets the increase in the atomic weight and causes a decrease in the density of the frit.

In addition, the low temperature melting points (also crystallization temperatures) of fine-ZnO bearing system (N type) could be related to the pronounced physical interactions of ZnO with the silicate chains. The fine-ZnO particles pass lower elastic modulus in comparison with the silicate neat, which caused to arresting of the degradation of silicate chains at lower temperatures through the decreasing of ZnO powder size in frit batch .

On the other hand, by increasing the S ratio the Tg values were increased (ΔTg=154ºC) but the crystallization temperatures were almost unchanged or few increased (ΔTp=17ºC). The increased of Tg values corresponded to the decreased NBO (None Bridging Oxygen) amounts and rigid glass network.

The fine grade frites show 30% higher GFA(glass forming ability), the stability increases up to 4.7% in the fine grade bearing sample (N1) as well, thus it can be said that the fine grade melt has a high viscosity between Tg and Tm typically exhibits a high GFA with a low required cooling rate. The slope and trend of GFA values (Tp- Tg/Tm) in fine ZnO grade bearing frites are sharper than coarse grade ones.The increased stability factor from 0.60(F3) to 0.64(F1) expected from the decrease of elastic moduli. . However, due to the little differences between the glass stability of F and N samples their firing temperatures were not different sufficiently. F3 sample has higher sintering and crystallization temperature compared to the F1 and F2 glazes but because of the K2O the CTE of the glazes were high. the CTE of the glazes (6.9×10-6/K -6.2×10-6/K) are lower than the CTE of the body (7.4×10-6/K to 9.9×10-6/K) when the compressive stress (due to the unsuitable heating time and temperature) exceeds the strength of glaze, the tile-glaze system will be warped. It was seen in some of the sintered samples.

The Si-O bending vibration (around 800 cm-1) decreases in F1 and F2 frites. The observed low frequency band at 466 cm-1 in all the frites samples (F1, F2, N1, N2) was due to vibration of Zn2+ metal cations [24]. The zinc ions have the mixed oxygen coordination numbers of four and five; the interconnections between SiO4 and ZnO are diverse. Either zinc can exist as a network former (tetrahedral coordination) which forms discrete ZnO tetrahedral or as a network modifier (octahedral co-ordination) which breaks up the amorphous silica structure [27-25]. The shift of IR reflection that is related to ZnO in the case of N3 and F3 sample toward the higher wave number could be related to the tetrahedral coordination of ZnO in these systems [26]. The weak band located at 566.82 cm-1 ascribed to the symmetric stretching vibrations of the ZnO4 groups in F2 ,F1 samples as well.

By comparing the N1,N2 samples with the F1,F2 sample's transmittance bands at 780-800 cm-1 the shift of the peaks to lower transmittance band in the case of N samples occurred, it can be deduced that the ZnO3 units were formed instead of ZnO4 units in N samples [17]. By using nano size ZnO perhaps (in N1,N2) the melt layer at low temperature forms and the Si-O-Zn bonds could not be arranged well which confirmed by FT-IR results

At the temperature above 1000◦C several processes occurred simultaneously including disintegration of wollastonite phase as well as the crystallization of the Willemite and Calcium Aluminum Silicate phases in the F2, N2 and F1,N3 samples respectively. The formation of Willemite phase requires both Zn and Si cations to interact with each other. The probability and feasibility of such mobility and the interaction would be higher and the diffusion might occurred in a liquid phase of F2 phase.

The F3 glaze has the highest hardness value that can be related to the Anorthite phase with 6 Mohs hardness [27]. The higher relative mole fraction of divalent cations in the residual glass phase of F3 and N3 samples compared to the F2 and N2 ones could be caused to the higher hardness as well. In the F1 and N1 glazes, high percentage of amorphous phase (XRD result) and Wollastonite (with 4.4 Mohs hardness) phase led to the low hardness value.

Both F3 and N3 glazes have the lower gloss values in comparison to the F1 sample. In fact, the effective formation of crystalline phases in these glazes (Anorthite and Wollastonite) declines their surface smoothness and conducts their appearance to the white matte status. The F2 sample has the Willemite phase but perhaps the Anorthite phase formation degraded the gloss value of this system.

The K2O evaporation from the surface of glazes results in Wollastonite transformation to Parawollastonite. In F3 and N3 samples the K2O wt.% is lower and could cause to the phases differences.