Supporting information

Acid Deashing Kinetics and Alkali Activation of Carbon Rich Particles in Coal Gasification Fine Slag to Prepare Capacitor Carbon

Nana Yang1, Shanxin Xiong1,2*, Shuai Zhang1, Fengyan Lv1, Yukun Zhang1, Xiaoqin Wang1, Jia Chu1, Zhen Li1, Jianwei Xu3

1 College of Chemistry and Chemical Engineering, Xi’an University of Science and Technology, Xi’an 710054, PR China

2 Key Laboratory of Coal Resources Exploration and Comprehensive Utilization, Ministry of Land and Resources, Xi’an 710021, PR China

3Institute of sustainability for chemicals, energy and environment, 138634, Singapore

* To whom correspondence should be addressed, e-mail: xiongsx@xust.edu.cn

Table S1. Proximate analysis, ultimate analysis and loss on ignition of CGFS

| Proximate analysis (%) |  |  |  |  | Ultimate analysis (%) |  |  |  |  |  | Loss on ignition (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mad | Ad | Vd | FCd* |  | Cdaf | Odaf* | Hdaf | Ndaf | Sdaf |  | 24.25% |
| 12.31 | 69.28 | 4.36 | 26.35 |  | 85.81 | 11.51 | 1.81 | 0.65 | 0.22 |  |  |

ad: air dry basis, d: dry basis, daf: dry ash free basis, M: moisture, A: ash, V: volatiles, FC: fixed carbon, *: by difference

1-kyanite Al2SiO5  2-albite Na(AlSi3O8)  3-quartz SiO2  4-anorthite CaAl2Si2O8  5-diopside Ca(Mg0.7Al0.3)(Si1.7Al0.3)O6  6-hematite Fe2O3  7-mullite Al6Si2O13  8-pyrope (Mg0.804Ca0.196)3Al2(SiO4)3  9-corundum Al2O3

Figure S1. XRD spectra of CRP

Figure S2. SEM images of CRP (a), D-CRP (b), and CRP-AC (90 min) (c).

Table S2. Parameters of equivalent circuit for CRP-AC

| Samples | Rs (Ω) | Rct (Ω) | Zw (Ω) |
| --- | --- | --- | --- |
| CRP-AC (60 min) | 1.212 | 0.751 | 1.052 |
| CRP-AC (70 min) | 1.111 | 0.811 | 1.024 |
| CRP-AC (80 min) | 1.012 | 0.879 | 1.012 |
| CRP-AC (90 min) | 0.942 | 1.399 | 0.873 |
| CRP-AC (100 min) | 1.321 | 1.552 | 1.121 |