Supporting information for “Unraveling the proton transfer of cellulose dissolution in aqueous NaOH/Urea solution: insights from thermodynamics by molecular dynamics simulation”

Wenze Cao1,∔, Jinghua Wu1,∔, Yu Chen1,*, Jierui Ye1, Lingfeng Zhou1, Xiaojing Fan1, Yiwei Li1, Jingyu Li1,*

1School of Materials Science and Engineering, Beijing Institute of Technology, 100081, Beijing, China

∔Contributed equally.

*Corresponding authors: cy.md.simulation@gmail.com; lijingyu@bit.edu.cn

According to the French method (French & Johnson, 2004), phi (φ) refers to the dihedral angle ∠O5'-C1'-O4-C4, psi (ψ) refers to the dihedral angle ∠C1'-O4-C4-C5, n refers to the number of turns per revolution, and h refers to the feed amount per residue along the helical axis. P represents the pitch, which is the product of n and h, and rho represents the helical radius. r represents the distance of the β-glucose ring (O1-O1'), Phi refers to the angle (O1-O1'-O1''), and Tau refers to the torsion angle formed by three r bonds (O1-O1'-O1''-O'''). The structural parameters of the cellulose chain in the crystal calculated in this paper are n=2, h=5.19 Å, and P=n×h=10.38 Å. Χ=360°/n, the second anhydroglucose unit (AGU) is rotated 180°, and the first AGU plus P has the same coordinates as the third AGU. The two adjacent AGUs undergo a 180° rotation transformation, so the structure of the cellulose chain in the crystal is 21-symmetric structure, as shown in Table S1. Whether it is a left-handed or right-handed helix, the absolute value of X is 180°. In addition, when the cellulose chain is a 31 helix structure, the absolute value of X is 120°. When the cellulose chain is placed in W, U/W, B/W and B/U/W systems, the structural parameter X is close to 120°, providing certain data support for the structural changes of cellulose chain in aqueous solution. As shown in Table S2, when the cellulose chain structure is a 21-symmetric structure, phi=-98°, psi=-142°; phi+psi=-240°, 360+(-142-98)=120°. Therefore, 120° is within the range of 21 helix.

Table S1. Puckering parameters of cellulose in different solvents

| Models | r (Å) | Phi (º) | Tau (º) | rho | Residues/turn Theta=n | Rise/residue d=h | P=n*h | Χ=360°/n |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| right-hand21 | 5.48 | 142.30 | 180 | 0.89 | 2 | 5.19 | 10.38 | 180 |
| left-hand21 | 5.48 | 142.30 | -180 | 0.89 | -2 | 5.19 | -10.38 | -180 |
| Crystal-31 | 5.45 | 139.52 | -115.6 | 1.26 | -3 | 5 | -15 | -120 |
| DP=7 (Box：4 × 4 × 4 nm3) |  |  |  |  |  |  |  |  |
| C/U/B/W | 5.53 | 134.13 | -54.22 | 3.28 | -5.15 | 4.05 | -20.86 | -69.88 |
| C/U/W | 5.47 | 135.05 | -108.59 | 1.48 | -3.14 | 4.88 | -15.30 | -114.73 |
| C/B/W | 5.41 | 138.08 | -80.58 | 1.96 | -4.04 | 4.66 | -18.80 | -89.15 |
| C/W | 5.44 | 137.69 | -83.28 | 1.91 | -3.93 | 4.70 | -18.46 | -91.63 |
| DP=20 (Box：6 × 6 × 11 nm3) |  |  |  |  |  |  |  |  |
| C/U/B/W | 5.44 | 133.46 | -109.11 | 1.50 | -3.11 | 4.81 | -14.97 | -115.62 |
| C/U/W | 5.53 | 133.55 | 112.07 | 1.48 | -3.05 | 4.91 | -14.95 | -118.22 |
| C/B/W | 5.54 | 131.98 | -92.39 | 1.88 | -3.54 | 4.71 | -16.70 | -101.56 |
| C/W | 5.48 | 133.78 | -105.80 | 1.55 | -3.20 | 4.83 | -15.45 | -112.61 |
| DP=20 (Box：11 × 11 × 11 nm3) |  |  |  |  |  |  |  |  |
| C/U/B/W | 5.5 | 132.47 | -112.4 | 1.5 | -3.03 | 4.86 | -14.73 | -118.8 |
| C/U/W | 5.48 | 133.57 | -114.9 | 1.43 | -2.98 | 4.88 | -14.54 | -120.7 |
| C/B/W | 5.49 | 133.56 | -81.5 | 2.1 | -3.92 | 4.59 | -17.99 | -91.8 |
| C/W | 5.49 | 133.06 | -123.4 | 1.35 | -2.8 | 4.92 | -13.78 | -128.4 |

Table S2. φ and ψ values of cellulose in different literature and at different DP

| Models |  | ψ(C1-O1-C4'- C5') | φ(O5-C1-O1-C4') | φ+ψ |
| --- | --- | --- | --- | --- |
| Nishiyama’s Iβ(center)(Nishiyama, Langan, & Chanzy, 2002)-21 |  | -146.06 | -88.72 | -234.78 |
| Nishiyama’s Iβ(corner)(Nishiyama et al., 2002)-21 |  | -142.3 | -98.45 | -240.75 |
| This work-21 |  | -142.3 | -98.0 | -240.3 |
| Nishimura(Nishimura & Sarko, 1991)-21 |  | -150.92 | -92.42 | -243.34 |
| Nishimura(Nishimura, Okano, & Sarko, 1991)-21 |  | -148.77 | -92.82 | -241.59 |
| French(French & Johnson, 2004)-31 |  | -102.18 | -67.71 | -169.9 |
| Whitaker(Whitaker, Nieduszynski, & Atkins, 1974)-Na-II-31 |  | 76.07/-76.01 | 89.77/-89.82 | 165.83 |
| Xylan-crystal-31 |  | -104.91 | -66.7 | -171.61 |
| DP=20 （Box：11 × 11 × 11 nm3） | C/U/B/W | -121.739 | -65.789 | -187.528 |
|  | C/U/W | -128.619 | -67.043 | -195.662 |
|  | C/B/W | 79.0747 | -68.296 | 10.779 |
|  | C/W | -128.15 | -67.819 | -195.969 |
| DP=7 （Box：4 × 4 × 4 nm3） | C/U/B/W | -121.511 | -70.997 | -192.508 |
|  | C/U/W | -125.422 | -68.173 | -193.595 |
|  | C/B/W | -115.195 | -69.06 | -184.255 |
|  | C/W | -123.87 | -70.031 | -193.901 |

References:

French, A. D., & Johnson, G. P. (2004). What crystals of small analogs are trying to tell us about cellulose structure. Cellulose, 11, 5-22. https://doi.org/10.1023/B:CELL.0000014765.94239.fe

Nishimura, H., Okano, T., & Sarko, A. (1991). Mercerization of cellulose. 5. Crystal and molecular structure of Na-cellulose I. Macromolecules, 24(3), 759-770. https://doi.org/10.1021/ma00003a020

Nishimura, H., & Sarko, A. (1991). Mercerization of cellulose. 6. Crystal and molecular structure of Na-cellulose IV. Macromolecules, 24(3), 771-778. https://doi.org/10.1021/ma00003a021

Nishiyama, Y., Langan, P., & Chanzy, H. (2002). Crystal structure and hydrogen-bonding system in cellulose Iβ from synchrotron X-ray and neutron fiber diffraction. Journal of the American Chemical Society, 124(31), 9074-9082. https://doi.org/10.1021/ja0257319

Whitaker, P., Nieduszynski, I., & Atkins, E. (1974). Structural aspects of sodacellulose II. Polymer, 15(2), 125-127. https://doi.org/10.1016/0032-3861(74)90015-9