Supplementary Information

Enabling the Multiscale Interfacial Stabilization for Ah-level Anode-free Lithium Metal Battery via a Prelithiation Separator strategy

Ahu Shao a, Helin Wang a, Min Zhang a, Jiacheng Lin a, Lu Chen a, Yongsong Li a, Yuxiang Guo a, Zhiqiao Wang a, Qiurong Jia a, b, Xin Wang c, Xiaoyu Tang a, Xiaodong Zhao d, and Yue Ma a*

a State Key Laboratory of Solidification Processing, Center for Nano Energy Materials, School of Materials Science and Engineering, Northwestern Polytechnical University, Xi’an 710072, P. R. China.

b Zhengzhou BAK Battery Co., Ltd., Zhengzhou 451450, China

c Shaanxi Raisight Energy Tech Co., Ltd., Xi’an 710086, China

d Fujian Blue Ocean&Black Stone Technology Co., Ltd., Zhangzhou 363000, China

Corresponding author: mayue04@nwpu.edu.cn (Y. Ma)

Supplementary Fig. 1 XRD patterns of mixed precursor.

Supplementary Fig. 2 (a-b) The SEM image of Li2S@C materials. Content.

Supplementary Fig. 3 Galvanostatic charge-discharge profiles of Li2S@C|PE at 0.1 C

Supplementary Fig. 4 DC polarization curves of (a) the Li|PE|Li symmetric cell, and (b) the Li|Li2S@C|PE|Li symmetric cell. The insets show the EIS curves before and after polarization.

Supplementary Fig. 5 The voltage curve of NCN811||Li with the PE separator cells at 0.5 C in the potential range of 3.0-4.3 V (vs. Li+/Li).

Supplementary Fig. 6 The voltage curve of LCO||Li with the PE separator cells at 0.5 C in the potential range of 3.0-4.5 V (vs. Li+/Li).

Supplementary Fig. 7 (a-b) The high-angle annular dark-field image and Ni, S elemental mappings of the cycled NCM811 cathode particle in the NCM811||Li paired with Li2S@C|PE.

Supplementary Fig. 8 Schematic illustration of cell prototypes under high-voltage conditions.

Supplementary Fig. 9 (a-b) The top-view SEM image of cycled Li metal anode with PE separator.

Supplementary Fig. 10 (a-b) The top-view SEM image of cycled Li metal anode with Li2S@C|PE separator.

Supplementary Fig. 11 Li+ diffusion coefficients were calculated from the GITT profiles of NCM811||Li cell with PE and Li2S@C|PE, respectively.

Supplementary Fig. 12 (a) The equivalent circuits for EIS fitting. (b) The fitted resistance for NCM811| |Li with PE and Li2S@C|PE.

Supplementary Fig. 13 DRT curves calculated form EIS measurements in the NCM811||Li with PE separator cell, (a) before and (b) after cycled.

Supplementary Fig. 14 DRT curves calculated form EIS measurements in the NCM811||Li with Li2S@|PE separator cell, (a) before and (b) after cycled.

Supplementary Fig. 15 The XRD curve of the Ag-Cu anode. The inset graph shows the characteristic peak of cubic phase Ag.

Supplementary Fig. 16 (a) The cross-sectional SEM image of the Ag-Cu anode. (b) The corresponding EDS mapping of Ag and Cu signals.

Supplementary Fig. 17 Nyquist plot of (a) Li||Cu half-cell and (b) Li||Ag-Cu half-cell before cycling, the inset graph shows equivalent circuits.

Supplementary Fig. 18 The Ag-Li binary phase diagram.

Supplementary Fig. 19 The ICE of half-cell cycling with capacities of 1 mAh cm-2 under 0.5 mA cm-2 (a) Li||Cu half-cell, (b) Li||Ag-Cu half-cell.

Supplementary Fig. 20 The top-view of SEM image of cycled Li metal anode with Li||Cu half-cell.

Supplementary Fig. 21 The top-view of SEM image of cycled Li metal anode with Li||Ag-Cu half-cell.

Supplementary Fig. 22 Voltage profiles of NCM811||Ag-Cu model paired with Li2S@C|PE separator for the initial 6 cycles.

Table S1. The comparisons of typical physical properties for different separators.

Table S2. The detailed parameters of a high-energy NCM811||Ag-Cu cell with Li2S@C|PE AFLMBs pouch cell.