Environmentally Friendly Shape Memory Smart Composite Materials with Multiple Response Modes

Supplementary Information

Fang Suoa, Zhongyang Baib, Xiangwei Mac, Yongtao Yaoa,*, Yanju Liud

a National Key Laboratory of Science and Technology for Advanced Composites in Special Environments, Harbin Institute of Technology, Harbin 150080, China

b Key Laboratory of Bio-Based Material Science and Technology (Ministry of Education), Material Science and Engineering College, Northeast Forestry University, Harbin 150040, China

c Daqing Inspection and Testing Center, Daqing 163311, China

d Department of Astronautic Science and Mechanics, Harbin Institute of Technology, Harbin 150000, People’s Republic of China

Experiment

Table S1 3D printing parameters

| Parameter | Value |
| --- | --- |
| Nozzle temperature (℃) | 210 |
| Layer height (mm) | 0.2 |
| Infill density (%) | 100 |
| Printing speed (mm/s) | 40 |
| Nozzle flow rate (%) | 200 |
| Support density (%) | 15 |
| Printing plate temperature (℃) | 25 |

Results and Discussion

Fig. S1 FTIR of citric acid

Fig. S2 The reaction mechanism between CMC, Fe³⁺, and CA.

Fig. S3 Water responsive controlled programming.

*Corresponding author. E-mail:

yaoyt@hit.edu.cn (Yongtao Yao)