EXPERIMENTAL SECTION

Reagents and materials

Imidazolate-2-carboxaldehyde (ICA), cerium (III) Acetate, dimethylbenzene, oleylamine were purchased from Sigma-Aldrich Chemical Co. (USA), various fluorescent dyes, including 4′,6-diamidino-2-phenylindole (DAPI) and 1,10-dioctadecyl-3,3,30,30-tetramethylindotricarbocyanine iodide (Dir), were all obtained from Sigma-Aldrich Chemical Co. (USA). DCFH­DA (2′,7′­dichlorofluorescin diacetate) was purchased from Beyotime Chemical Reagent Co. Ltd. (China). siRNA targeting CTGF mRNA (siCTGF, the antisense strand, 5′-UCAAAGAUGUCAUUGU CCCTT-3′) were synthesized by HANBI (Shanghai, China). All primers were from sangon (Shanghai, China). Unless otherwise stated, all other reagents were obtained from Beijing Chemical Reagent Co. (Beijing, China) and used as received without further purification.

Synthesis of ceria NPs

Ceria nanoparticles (NPs) were synthesized using a previously established protocol with minor modifications.[1] Specifically, 0.43g cerium (III) acetate and 3.25g oleylamine were added dropwise to a 15 ml dimethylbenzene solution under continuous stirring for 4-6 h. The mixture was then heated to 90°C for 10 min, after which 1 ml H2O was introduced, resulting in a color change from deep brown to pale yellow. To enhance biocompatibility for in vivo applications, the surface of the hydrophobic ceria nanoparticles was modified using commercially available DSPE-PEG (5K), as previously described.[1] 5 ml DSPE-PEG solution in chloroform (20 mg/ml) and ceria nanoparticles solution were mixed and agitated for 10 min. Subsequently, the resulting mixture was incubated in a rotary evaporator at 60°C under vacuum conditions for 2 h. Post-incubation, the mixture was cooled and underwent a washing step before being resuspended in distilled water for future applications.

Synthesis of zif-90/Ce NPs

Zif-90/Ce NPs were synthesized using a previously established method for pure zif-90 with slight modifications. Specifically, a solution of imidazolate-2-carboxaldehyde (ICA) (2 ml, 0.8 M) containing 20 mg CeO2 was introduced into a solution of zinc acetate dihydrate (2 ml, 0.4 M) in dimethylformamide (DMF) under vigorous stirring. To enhance the stability of the nanoparticles, an additional 10 ml of DMF was incorporated into the reaction mixture following a 5-min interval. The resultant mixture was subsequently subjected to centrifugation and repeatedly washed with DMF and ethanol. Finally, the synthesized zif-90/Ce NPs were dried. Afterwards, the pure zif-90 NPs were prepared with the same procedure but without CeO2.

Synthesis of zif-90/Ce/siR NPs

The siRNA was dissolved in DEPC-treated water to achieve a concentration of 0.1 μg/μl prior to each use. A mixture was prepared by combining zif-90/Ce NPs dispersed in MLQ with siCTGF solution at weight ratios of 200:1, 100:1, 80:1 and 50:1. The resulting mixture was then agitated at room temperature for 20 min to produce zif-90/Ce/siR NPs. Following siRNA loading, the prepared NPs were centrifuged, and the supernatant was discarded to remove free siRNA. The resulting precipitate was collected and subsequently suspended in an aqueous solution for further use.

cell production and cell membrane separation

Human embryonic kidney cells (HEK 293T) were purchased from and authenticated from the ATCC company (Shanghai, China) and then cultured in a DMEM medium supplemented 10% FBS and 1% streptomycin-penicillin. Moreover, HEK 293T cells were genetically modified to express anti FAP Car lentivirus specifically targeting FAP. This Car lentivirus was constructed using the scFv fragment from the mouse FAP antibody (clone 73.3) fused to the cytoplasmic domains of human CD3ζ (Figure S2A-C). Additionally, the lentivirus contained a transgene encoding the green fluorescent protein (GFP) to facilitate the assessment of transduction efficiency,[2] which was transfected for 48 h with an infection (MOI) of 10 (Figure. S2D-E).

The membranes from HEK 293T and anti FAP-car HEK 293T were created using a slight modification of a previous procedure.[3] Anti-FAP-car HEK 293T cells were suspended in hypotonic lysing buffer, sonicated for 2 min and then extruded through polycarbonate membranes with 400-, 200-, and 100-nm pores using an Avanti Polar Lipids micro extruder (USA). Following centrifugation at 14,000×g for 20 min at 4 °C, the supernatant was collected and subjected to freeze-drying. Subsequently, the cell membrane was obtained.

Preparation of Membrane Camouflaged Nanoparticles (FM@zif-90/Ce/siR NPs)

In order to cover the polymeric cores in cell membranes, the generated cell membrane fragments were mixed with zif-90/Ce/siR NPs at a nanoparticle-to-membrane weight ratio of 1.5:1. After sonication for 30 min in a bath sonicator, the mixture was centrifuged to separate the product.

Characterization of FM@zif-90/Ce/siR NPs

Firstly, the morphology and element composition of FM@zif-90/Ce/siR NPs were investigated by transmission electron microscopy (TEM, FEI Talos F200X, Super-X, Thermo Fisher, USA) and scanning electron microscope (SEM, Hitachi S4800, Japan), The atomic force microscopy (AFM, Agilent 5500 Scanning Probe Microscope, USA) was used for examining the thicknesses of zif-90 NPs. Hydrodynamic diameter and zeta potential were determined by dynamic laser particle size analyze (NanoBook 90Plus PALS, Brookhaven, USA). Powder X-ray diffraction (XRD, Bruker D8 Advance, Geman) was tested on a Bruker D8 Focus with Cu Kα radiation. X-ray photoelectron spectroscopy (XPS) was performed on a Thermo Fisher ESCALAB Xi (USA). N2 adsorption-desorption isotherms were used to measure the surface area and porosity of zif-9 NPs and FM@zif-90/Ce/siR NPs by a Micromeritics ASAP 2460 automated sorption analyzer (UAS). Thermogravimetric analysis (TGA) of zif-90 and FM@zif-90/Ce/siR NPs was performed by thermogravimetric analyzers (TA Instruments TGA 550, USA).

To assess the siRNA loading efficiency of FM@zif-90/Ce/siR NPs following the cell membrane coating, the amount of unloaded siRNA in the supernatant was quantified. Sodium dodecyl sulfate-polyacrylamide gel electrophoresis (SDS-PAGE) and coomassie blue staining were employed to analyze the protein compositions of FM@zif-90/Ce/siR NPs. The cy3-labeled siRNA was employed to monitor the ATP-responsive release process. 1 ml FM@zif-90/Ce/siR NPs (10 mg/ml in PBS) was placed into a dialysis bag with a molecular weight cut-off of 2 kDa. The sample was subsequently dialyzed in 30 ml PBS containing specified ATP concentrations (0.5mM or 1mM) within an oscillation incubator set to 100rpm and 37°C. The amount of released siRNA was quantified by measuring red fluorescence at predetermined time intervals.

Detection of the SOD-like and CAT-like activity

The ROS scavenging capability of FM@zif-90/Ce/siR NPs was evaluated using the primary ROS, O2•− and H2O2. The superoxide anion scavenging activity was quantified employing the Total Superoxide Dismutase Assay Kit (S0038, Beyotime Biotechnology, China). The hydrogen peroxide quenching activity was measured using the Hydrogen Peroxide Assay Kit (S0101, Beyotime Biotechnology, China).

Cell viability assay

The impact of FM@zif-90/Ce/siR NPs on the viability of CFs was evaluated using the cell counting kit-8 (CCK-8) kit (Beyotime Biotechnology, China). 1.0 × 105 cells were seeded into each well of a 96-well plate and then were incubated with various concentrations of FM@zif-90/Ce/siR NPs (0, 10, 20, 40, 80 and 100 µg/ml) for 24 h. Next, 10 µl CCK-8 solution was added to 100 µL of culture medium. The cells were subsequently incubated for 4 h at 37°C and the absorbance was measured at 450 nm.

Cellular Binding and/or Internalization

To evaluate the cellular uptake of FM@zif-90/Ce/siR NPs, TGF-β1-induced CFs were treated with cy3-labeled siCTGF-loaded simple nanoparticles (zif-90/Ce/siR NPs), non-targeted mimetic nanoparticles (M@zif-90/Ce/siR NPs) and targeted mimetic nanoparticles (FM@zif-90/Ce/siR NPs). After a 4-hour incubation, cells were washed with PBS, fixed with 4% paraformaldehyde, washed again and stained with DAPI for 10 min to assess the targeting efficacy on TGF-β1-induced cardiac fibroblasts. The targeting efficacy was then assessed using confocal laser scanning microscopy (CLSM, Nikon, Japan).

Intracellular ROS scavenging ability and antifibrosis treatment in vitro

The ROS scavenging ability of FM@zif-90/Ce/siR NPs was evaluated using DCFH-DA. Initially, CFs were cultured in 6-well cell culture plates and incubated with TGF-β1 (10 ng/ml) for 24 h, excluding the negative control group. Subsequently, the cells were treated with zif-90/Ce/siR NPs, M@zif-90/Ce/siR NPs and FM@zif-90/Ce/siR NPs for 48 h. Following washing with PBS, DCFH-DA (10 μM) was added and co-incubated with the cells at 37°C for 30 min. The intracellular fluorescence was then observed using fluorescence microscopy. Alternatively, the cells were washed with PBS, collected and analyzed via flow cytometry analysis. Subsequently, employing the identical treatment, the indices of inflammation and fibrosis were evaluated in vitro.

Targeting affinity study in cardiac fibrosis model

In order to assess the biodistribution of the administered micelles in vivo, a group of balb/c mice (male, 6 weeks old, n=5) were intraperitoneally injected with isoproterenol (ISO) (30 mg/kg/d, daily for 2 weeks) to induce cardiac fibrosis. On the 14th day, the mice were subcutaneously administered 100 μl of Dir-loaded nanoparticles. At 24 h after the treatment, various tissues from mice were collected to observe the distribution of different groups of nanoparticles in the heart, liver, spleen, lungs, and kidneys using an in vivo imaging system (PerkinElmer, USA). The fluorescence signal was analyzed and quantified using the Living Image Software (PerkinElmer, USA).

Antifibrosis treatment of FM@zif 90/Ce/siR NPs in vivo

All animal experiments conducted in this study were ethically approved by the Institutional Animal Care and Use Committee of Air Force Military Medical University. Cardiac fibrosis was induced using isoproterenol (ISO), as previously described.[4] On day 3, the mice were randomly assigned to five groups (n=6) for the following treatments: 1) control group (control); 2) cardiac fibrosis model (model); 3) cardiac fibrosis model treated with zif-90/Ce/siR NPs (zif-90/Ce/siR NPs); 4) cardiac fibrosis model treated with M@zif-90/Ce/siR NPs (M@zif-90/Ce/siR NPs); 5) cardiac fibrosis model treated with FM@zif-90/Ce/siR NPs(FM@zif-90/Ce/siR NPs)(15μg siRNA/mouse). The therapeutic interventions were administered at three-day intervals for a total of five sessions. Subsequently, the functionality and morphology of the cardiac tissue were evaluated using a Vevo 2100 imaging system (Visual Sonics, Toronto, Canada) equipped with an M-mode and high-frequency transducer (MS400). Following these assessments, cardiac tissues were collected for histological and biomedical analyses.

In Vivo Biocompatibility Evaluation

Normal balb/c mice were divided into two groups with three mice in each group, and then they were intravenously injected with saline and FM@zif-90/Ce/siR NPs every three days five times. After treatment, the mice were sacrificed, and the major organs, including brain, liver, spleen, lung and kidney were eviscerated for further histological analyses. Meanwhile, the blood of mice was collected for biochemical analysis.

Statistical Analysis

The statistical analysis was conducted utilizing GraphPad Prism 9.5.0 (GraphPad, Boston, MA, USA). A one-way ANOVA test, accompanied by Tukey’s multiple comparison test, was employed to scrutinize the differences among various groups. The Student’s t-test was utilized to examine the statistical significance between two distinct groups, with differences deemed significant. The average values were represented as mean ± SEM. In all instances, p values < 0.05 were consistently considered statistically significant. (ns denotes no significance, *p < 0.05, **p < 0.01, ***p < 0.001, ****p < 0.0001).

Fig. S1 (A) STEM of CeO2 NPs. (B) TEM and element mapping of pure zif-90. (C) Pore diameter of zif-90. (D)TGA of pure zif-90 and FM@zif-90/Ce/siR NPs.

Fig. S2 (A) Car structure. (B) CMV vector structure. (C) Gel electrophoresis of CMV vector. (1: marker, from top to bottom: 10 kb, 8 kb, 6 kb, 5 kb, 4 kb, 3.5 kb, 3 kb, 2.5 kb, 2 kb, 1.5 kb, 1 kb, 750 bp, 500 bp, 250 bp. 2: Carrier digest product. 3: Undigested vector). (D) Representive fluorescence image of anti FAP-Car positive cells. (E) The rate of positive cells after anti FAP-Car transfection using the flow cytometry.

Fig. S3 Masson’s trichrome staining and FAP expression in myocardial tissue of control and ISO-induced model mice (scale bar=20 μm).

References

1. Ni D, Wei H, Chen W, Bao Q, Rosenkrans Z. T, Barnhart T E, Ferreira C A, Wang Y, Yao H, Sun T, Jiang D, Li S, Cao T, Liu Z, Engle J W, Hu P, Lan X, Cai W. Ceria Nanoparticles Meet Hepatic Ischemia-Reperfusion Injury: The Perfect Imperfection. Adv Mater. 2019; 31 (40), e1902956.

2. Wang L, Lo A, Scholler J, Sun J, Majumdar R S, Kapoor V, Antzis M, Cotner Ce, Johnson L A, Johnson La, Durham A C, Durham Ac, Solomides C C, June C H, Puré E, Albelda S M. Targeting fibroblast activation protein in tumor stroma with chimeric antigen receptor T cells can inhibit tumor growth and augment host immunity without severe toxicity. Cancer Immunol Res. 2014; 2 (2): 154–166.

3. Park J H, Jiang Y, Zhou J, Gong H, Mohapatra A, Heo J Y, Gao W, Fang R, Zhang L. Genetically engineered cell membrane–coated nanoparticles for targeted delivery of dexamethasone to inflamed lungs. Science Advances. 2021;7(25)

4. Park S, Ranjbarvaziri S, Lay F D, Zhao P, Miller M J, Dhaliwal J S, Huertas-Vazquez A, Wu X, Qiao R, Soffer J M, Rau C, Wang Y, Mikkola H K A, Lusis A J, Ardehali R. Genetic Regulation of Fibroblast Activation and Proliferation in Cardiac Fibrosis. Circulation. 2018; 118. 035420.