APPENDIX

Management of orange peels and chokeberry/red currant seeds via pyrolysis and CO2-consuming activation using microwave-assisted heating: Changes in textural, surface-chemistry features and detoxifying potential from biomass to activated carbon

Table A.1 Formulas and structures of organic adsorbates

| Name | Structure |
| --- | --- |
| Rhizobium leguminosarum bv. trifolii exopolysaccharide (EPS) monomer | (Skorupska et al., 2006) |
| Cationic polyacrylamide (CtPAM) monomer | (Estrada et al. 2020) |
| Anionic polyacrylamide (AnPAM) monomer | (Estrada et al. 2020) |
| Diuron, DCMU, N-(3,4-dichlorophenyl)-N,N-dimethyl-urea | (Giacomazzi and Cochet 2004) |
| Glyphosate, GLY, N-(phosphonomethyl) glycine | (Peillex and Pelletier 2020) |

Table A.2 The equations applied for experimental data modelling

| Equation | Formula | References |
| --- | --- | --- |
| Pseudo I-order | qt=k2∙qe2∙t1+k2∙qe∙t (3) | (Lagergren, 1988) |
| Pseudo II-order | qt=qe∙(1-e-k1∙t)t12 (4) | (Ho and McKay, 1999) |
| IPD | qt=kDt12+C (5) | (Ouyang et al., 2020) |
| Elovich | qt=1βln⁡(1+αβt) (6) | (Ouyang et al., 2020) |
| Langmuir | qe=QmKL Ce1+KLCe (7) | (Foo and Hameed 2010) |
| Freundlich | qe=KF∙Ce1/n (8) | (Foo and Hameed 2010) |
| Langmuir-Freundlich | qe=Am∙KLF∙Cem1+KLF∙Cem (9) | (Szewczuk-Karpisz et al., 2021) |
| Redlich-Peterson | qe=KR∙Ce1+aR∙CeβR (10) | (Tomczyk et al. 2023) |
| Temkin | qe=RTb lnACe (11) | (Kończyk et al. 2022) |
| Dubinin-Radushkevich | qe=qD∙e(-βD[RTln(1+1Ce]2) (12) | (Tomczyk et al., 2023) |

qt (mg/g) – the amount adsorbed at time t (min); qe (mg/g) – the amount adsorbed at equilibrium; k1 (1/min) and k2 (g/mg·min) – the reaction rate constants; Ce (mg/L) – the equilibrium concentration of adsorbate in the solution; C (mg/g) – the constant; kD (g/mg·min1/2) – the IPD rate constant; α (mg/g·min) – the primary rate of adsorption; β – the desorption parameter; Qm (mg/g) – the maximum adsorbed amount in the monomolecular layer; KL (L/mg) – the Langmuir constant; KF (mg/g (mg/L)1/n) – the Freundlich parameter; KLF, (L/mg) – related to the affinity of the adsorbate for active sites; Am (mg/g) – the amount of the available surface sites; m – the parameter determining the shape of the energy distribution function; KR (L/mg) – the Redlich–Peterson adsorption capacity constant; aR [(L/mg)β] – the Redlich–Peterson isotherm constant; βR – the exponent between 0 and 1; A – the Temkin model constant; b (kcal/mol) – the adsorption heat; R (8.314 J/K·mol) – the universal gas constant; T (K) – the absolute temperature; qD (mg/g) – the theoretical isotherm saturation capacity; βD – the Dubinin-Raduskevich isotherm constant.

Tab. A.3 Equilibrium parameters for Cd, Cu, As, and Se adsorption on OB and the OB-derived materials

|  |  | As(V) |  |  |  |  | Se(IV) |  |  |  |  | Cd(II) |  |  |  |  | Cu(II) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Model | parameter | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 |
| Langmuir (linear) | Qm [mg/g] | 2.892 | 2.950 | 4.210 | 7.220 | 5.033 | - | 25.875 | 3.880 | 1.872 | 2.720 | 15.270 | 26.243 | 33.543 | 91.519 | 42.071 | 10.756 | 16.187 | 14.076 | 17.685 | 35.245 |
|  | KL [L/mg] | 0.005 | 0.006 | 0.006 | 0.006 | 0.022 | - | 0.001 | 0.017 | 0.013 | 0.074 | 0.045 | 0.016 | 0.028 | 0.004 | 0.022 | 0.226 | 0.036 | 0.183 | 0.132 | 0.165 |
|  | R2 | 0.802 | 0.378 | 0.320 | 0.538 | 0.956 | - | 0.184 | 0.954 | 0.702 | 0.985 | 0.984 | 0.956 | 0.969 | 0.135 | 0.999 | 0.998 | 0.971 | 0.999 | 0.999 | 0.999 |
| Freundlich (linear) | n | 1.187 | 1.154 | 1.133 | 1.161 | 1.649 | - | 1.042 | 1.550 | 1.367 | 2.422 | 2.039 | 1.968 | 2.345 | 1.051 | 1.631 | 3.764 | 1.891 | 4.026 | 3.604 | 3.260 |
|  | KF [mg/g (mg/L)1/n] | 1.023 | 0.823 | 0.564 | 0.346 | 0.286 | - | 0.306 | 0.419 | 0.910 | 0.410 | 0.078 | 0.067 | 0.044 | 0.035 | 0.034 | 0.094 | 0.076 | 0.074 | 0.060 | 0.028 |
|  | R2 | 0.939 | 0.767 | 0.748 | 0.853 | 0.818 | - | 0.928 | 0.890 | 0.708 | 0.678 | 0.777 | 0.985 | 0.987 | 0.829 | 0.948 | 0.685 | 0.743 | 0.800 | 0.930 | 0.770 |
| Langmuir-Freundlich | Am [mg/g] | 1.798 | 1.588 | 2.171 | 4.104 | 4.177 | - | 6.219 | 3.154 | 1.276 | 2.579 | 13.923 | 46.504 | 58.393 | 34.614 | 39.431 | 10.430 | 13.666 | 13.698 | 19.670 | 36.857 |
|  | KLF [L/mg] | 0.003 | 0.002 | 0.000 | 0.002 | 0.004 | - | 0.000 | 0.002 | 0.001 | 0.002 | 0.012 | 0.019 | 0.035 | 0.003 | 0.018 | 0.032 | 0.002 | 0.183 | 0.199 | 0.318 |
|  | m | 1.353 | 1.775 | 2.222 | 1.627 | 1.680 | - | 2.096 | 1.779 | 2.107 | 2.255 | 1.558 | 0.705 | 0.643 | 1.533 | 1.102 | 1.912 | 2.130 | 1.098 | 0.684 | 0.699 |
|  | R2 | 0.999 | 0.998 | 0.996 | 0.997 | 0.999 | - | 0.923 | 0.998 | 0.998 | 0.999 | 0.999 | 0.999 | 0.999 | 0.997 | 0.999 | 0.999 | 0.999 | 0.999 | 0.994 | 0.998 |
| Redlich-Peterson | KR [L/mg] | 0.021 | 0.120 | 0.721 | 0.074 | 0.140 | - | 0.049 | 0.074 | 0.047 | 0.181 | 0.785 | 0.855 | 5.220 | 0.622 | 0.960 | 46.910 | 0.756 | 2.907 | 3.849 | 14.590 |
|  | n | 0.899 | 0.678 | 0.612 | 1.000 | 1.000 | - | 1.000 | 1.000 | 1.000 | 1.000 | 1.000 | 0.645 | 0.616 | 1.000 | 1.000 | 0.843 | 1.000 | 1.000 | 0.908 | 0.909 |
|  | aR [(L/mg)β] | 0.016 | 0.385 | 2.283 | 0.014 | 0.028 | - | 0.004 | 0.019 | 0.030 | 0.062 | 0.051 | 0.236 | 1.250 | 0.014 | 0.023 | 9.780 | 0.047 | 0.209 | 0.348 | 0.668 |
|  | R2 | 0.996 | 0.998 | 0.989 | 0.993 | 0.996 | - | 0.989 | 0.998 | 0.997 | 0.999 | 0.997 | 0.999 | 0.998 | 0.991 | 0.995 | 0.996 | 0.998 | 0.999 | 0.999 | 0.998 |
| Temkin | A | 0.101 | 0.154 | 0.163 | 0.128 | 0.243 | - | 0.068 | 0.175 | 0.231 | 0.801 | 0.483 | 0.278 | 0.669 | 0.135 | 0.294 | 5.047 | 0.435 | 7.104 | 4.132 | 6.104 |
|  | b [kcal/mol] | 1.247 | 1.240 | 0.875 | 0.488 | 0.523 | - | 0.295 | 0.669 | 1.602 | 1.042 | 0.178 | 0.125 | 0.108 | 0.058 | 0.070 | 0.347 | 0.170 | 0.287 | 0.217 | 0.114 |
|  | R2 | 0.995 | 0.995 | 0.998 | 0.989 | 0.996 | - | 0.999 | 0.997 | 0.997 | 0.999 | 0.997 | 0.999 | 0.998 | 0.985 | 0.994 | 0.997 | 0.998 | 0.996 | 0.993 | 0.996 |
| Dubinin-Radushkevich | KDR | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | - | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
|  | qD | 0.974 | 1.315 | 1.904 | 2.856 | 3.418 | - | 4.568 | 2.312 | 1.202 | 2.497 | 11.971 | 11.967 | 17.139 | 21.835 | 20.740 | 10.232 | 12.294 | 12.520 | 14.247 | 29.005 |
|  | R2 | 0.834 | 0.981 | 0.982 | 0.930 | 0.944 | - | 0.919 | 0.857 | 0.995 | 0.986 | 0.960 | 0.597 | 0.620 | 0.939 | 0.774 | 0.993 | 0.957 | 0.963 | 0.811 | 0.947 |

Tab. A.4 Kinetic parameters for Cd, Cu, As, and Se adsorption on OB and the OB-derived materials

|  |  | As(V) |  |  |  |  | Se(IV) |  |  |  |  | Cd(II) |  |  |  |  | Cu(II) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Model | parameter | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 | OB | OBCC | OBCM | OFC800 | OFM800 |
| PFO (linear) | qe [mg/g] | 0.860 | 1.474 | 1.759 | 2.394 | 1.782 | - | 3.384 | 2.424 | 0.595 | 0.952 | 10.355 | 18.812 | 33.334 | 23.388 | 21.877 | 3.367 | 5.174 | 6.167 | 7.600 | 11.176 |
|  | k1 [1/min] | 0.013 | 0.026 | 0.047 | 0.033 | 0.017 | - | 0.045 | 0.052 | 0.043 | 0.044 | 0.043 | 0.037 | 0.052 | 0.041 | 0.039 | 0.033 | 0.035 | 0.040 | 0.027 | 0.066 |
|  | R2 | 0.951 | 0.997 | 0.948 | 0.906 | 0.901 | - | 0.979 | 0.964 | 0.922 | 0.949 | 0.951 | 0.965 | 0.907 | 0.995 | 0.997 | 0.818 | 0.858 | 0.987 | 0.936 | 0.838 |
| PSO (linear) | qe [mg/g] | 7.573 | 5.170 | 2.945 | 5.046 | 4.073 | - | 3.774 | 3.220 | 1.257 | 2.629 | 20.207 | 20.207 | 20.207 | 24.581 | 26.110 | 10.553 | 12.866 | 13.264 | 16.872 | 29.172 |
|  | k2 [g/mg·min] | 0.000 | 0.000 | 0.002 | 0.001 | 0.016 | - | 0.009 | 0.007 | 0.065 | 0.058 | 0.000 | 0.000 | 0.000 | 0.001 | 0.001 | 0.014 | 0.006 | 0.008 | 0.005 | 0.005 |
|  | R2 | 0.005 | 0.068 | 0.507 | 0.459 | 0.998 | - | 0.999 | 0.973 | 0.999 | 0.999 | 0.176 | 0.176 | 0.176 | 0.991 | 0.993 | 0.999 | 0.998 | 0.999 | 0.999 | 0.999 |
| IPD | kD [g/mg·min1/2] | 0.045 | 0.072 | 0.106 | 0.150 | 0.134 | - | 0.145 | 0.135 | 0.050 | 0.125 | 0.379 | 0.746 | 1.027 | 1.102 | 1.174 | 0.365 | 0.522 | 0.452 | 0.610 | 1.071 |
|  | C [mg/g] | 0.000 | 0.000 | 0.094 | 0.210 | 1.250 | - | 0.520 | 0.320 | 0.354 | 1.140 | 0.000 | 0.000 | 0.000 | 1.356 | 2.460 | 4.130 | 4.039 | 5.503 | 5.530 | 11.125 |
|  | R2 | 0.998 | 0.999 | 0.996 | 0.987 | 0.987 | - | 0.978 | 0.990 | 0.996 | 0.976 | 0.997 | 0.997 | 0.997 | 0.999 | 0.999 | 0.998 | 0.999 | 0.999 | 0.998 | 0.999 |
| Elovich | α [mg/g· min] | 0.013 | 0.021 | 0.077 | 0.137 | 3.736 | - | 0.250 | 0.162 | 0.490 | 5.738 | 0.095 | 0.180 | 0.241 | 0.641 | 1.113 | 14.640 | 4.257 | 100.686 | 10.069 | 49.614 |
|  | β | 3.266 | 2.074 | 1.861 | 1.222 | 2.000 | - | 1.315 | 1.440 | 5.150 | 3.153 | 0.353 | 0.175 | 0.125 | 0.166 | 0.176 | 0.760 | 0.483 | 0.790 | 0.421 | 0.286 |
|  | R2 | 0.995 | 0.994 | 0.999 | 0.998 | 0.998 | - | 0.999 | 0.999 | 0.999 | 0.999 | 0.996 | 0.996 | 0.997 | 0.999 | 0.999 | 0.999 | 0.999 | 0.999 | 0.994 | 0.997 |

a)

b)

c)

d)

Fig. A.1 N2 adsorption/desorption isotherms (a, b) and pore size distribution (c, d) for chokeberry seeds and black currant seeds, respectively, as well as BCs and ACs produced from them

a)   b)

Fig. A.2 SEM images at 3000x magnification of the OBCC (a) and OFC800 (b) samples

a)

b)

c)

d)

Fig. A.3. Surface charge density as a function of pH value for Bs, BCs, and ACs (a-c) as well as for the OFM800 sample with and without macromolecular compounds (d)

a)

b)

Fig. A.4. FTIR spectra of chokeberry as well as BCs and ACs produced from them (a) and black currant as well as BCs and ACs produced from them (b)

Fig. A.5. Adsorbed amounts of metals, metalloids, and herbicides on Bs and obtained BCs/ACs (initial Cd/Cu/As/Se concentration = 100 mg/L, DCMU/GLY = 10 mg/L)

Fig. A.6. Adsorbed amounts of metals and metalloids on the OFM800 sample at various pH values

Ca

O

C

a)

Cd

Ca

O

C

b)

Cu

Ca

O

C

c)

As

C

O

Ca

d)

Se

Ca

O

C

e)

Fig. A.7 SEM-EDS maps for the OFM800 (a) sample after adsorption of Cd (b), Cu (c), As (d), Se (e) ions