Table 1. Physico-chemical Characterization of Bevacizumab-Loaded Albumin Nanoparticles. B-NP: bare nanoparticles; B-NP-DEX10: DEX-coated nanoparticles with a DEX-to-albumin ratio of 0.1; B-NP-DEX25: DEX-coated nanoparticles with a DEX-to-albumin ratio of 0.25; B-NP-DEX50: DEX-coated nanoparticles with a DEX-to-albumin ratio of 0.5. Data are presented as mean ± SD (n > 6). BEVA: bevacizumab.

|  | Particle size (nm) | PDI | Zeta potential (mV) | EE (%) | BEVA loading (μg/mg) |
| --- | --- | --- | --- | --- | --- |
| B-NP | 225 ± 5 | 0.06 ± 0.02 | -36 ± 2 | 82 ± 2 | 107 ± 3 |
| B-NP-DEX10 | 233 ± 9 | 0.13 ± 0.02 | -27 ± 7 | 78 ± 3 | 103 ± 4 |
| B-NP-DEX25 | 244 ± 5 | 0.09 ± 0.06 | -40 ± 6 | 87 ± 4 | 112 ± 3 |
| B-NP-DEX50 | 255 ± 3 | 0.11 ± 0.01 | -36 ± 5 | 88 ± 2 | 111 ± 2 |

Table 2. Pharmacokinetic parameters of bevacizumab following intravenous administration of a single dose of 5 mg/kg. Bevacizumab: aqueous solution of the monoclonal antibody; B-NP-DEX50: bevacizumab-loaded dextran-coated albumin nanoparticles. Data are expressed as mean ± SD (n = 6). Tmax: time to reach maximum plasma concentration; Cmax: maximum plasma concentration; t1/2: plasma half-life.

|  | tmax (days) | Cmax (μg/mL) | t1/2 (days) | AUC0-30d (μg/mL·d) |
| --- | --- | --- | --- | --- |
| Bevacizumab | 0 | 129 ± 1 | 10 ± 2 | 711 ± 48 |
| B-NP-DEX50 | 0.22 ± 0.08 | 69 ± 2 | 10 ± 3 | 319 ± 29 |