Table 1  Specifications of the Ion Exchange Resin Amberlite IRA-400.

| Parameters | - Specification |
| --- | --- |
| Polymer matrix | Polystyrene DVB |
| Functional group | –N+ R3 |
| Ionic form | Cl− |
| Exchange capacity | 2.6 – 3 eq kg−1 (dry mass) |
| Effective size | 0.3–0.9 mm |
| Operating temperature | 80°C (maximum) |
| pH range | 0–14 |
| Structure |  |

Table 2 Models and equilibrium isotherms for the sorption of selenium ions onto Amberlite IR 400 resin [25-27].

| Isotherm | Linear form | Plot | Slope and intercept |
| --- | --- | --- | --- |
| Langmuir | Ceqe=1Qob+1QoCe RL = 1/ 1+bCo | Ce/qe versus Ce | Slope= 1/ Qo Intercept =1/ Qo b |
| Freundlich | logqe=logKf+1nlogCe | log qe versus log Ce | Slope= 1/n Intercept = logKf |
| Thermodynamic | lnKd=ΔS°/R+-ΔH° /R 1 /T ΔG°=−RTlnKd | lnKd versus 1/T | Slope= - ΔH°/R Intercept = ΔS°/R |
| Kinetic model |  |  |  |
| Pseudo-First-order | logqe− qt=logqe−K1 2.303 t | Log(qe-qt) versus t | Slope= - k1/2.303 Intercept = log qe |
| Pseudo-Second-order | tqt=1K2 qe2+tqe | t/qt versus t | Slope= 1/qe Intercept = 1/ K2qe2 |

Table 3.  Kinetic model parameters for the adsorption of Se(IV) ([Se(IV)] = 100 mg/L, pH = 3, V = 5 ml,  adsorbent dosage = 0.10 g, T = 25 °C) from aqueous solutions.

| kinetic | parameters | Metal ion |
| --- | --- | --- |
|  |  | Se(IV) |
| Pseudo-First order | qe (mg/g) | 1.79 |
|  | K1 (g/mg.min) | 0.767 |
|  | R2 | 0.809 |
| Pseudo-Second order | qe (mg/g) | 4.12 |
|  | K2 (g/mg.min) | 1.76 |
|  | R2 | 0.999 |
| qexp, mg/ g |  | 4.11 |

Table 4. Linearized sorption isotherm parameters for Se(IV) sorption onto the Amberlite IRA 400 resin.

| isotherm | parameters | Metal ion |
| --- | --- | --- |
|  |  | Se(IV) |
| Langmuir | Qo (mg/g) | 18.52 |
|  | b (ml/mg) | -0.066 |
|  | RL | -0.18 |
|  | R2 | 0.999 |
| Freundlich | Kf (mg/g) | 1.32 |
|  | n | 4.925 |
|  | R2 | 0.978 |
| qexp, mg/ g |  | 18.25 |

Table 5: Parameters of thermodynamics for the sorption of selenium ions.

| Metal ions | T, K | ΔGo, k J mole-1 | ΔHo, k J mole-1 | ΔSo, J mole-1K -1 |
| --- | --- | --- | --- | --- |
| Se (IV) | 298 | -17.024 | -8.15 | 29.78 |
|  | 308 | -17.32 |  |  |
|  | 318 | -17.62 |  |  |
|  | 328 | -17.92 |  |  |
|  | 338 | -18.22 |  |  |

Table 6: Desorption of Se(IV) from loaded Amberlite IRA 400  resin using several desorbing agents of different concentration ranges*.

| Desorbing agent | Concentration (mol/L) | Desorption percent (%) |
| --- | --- | --- |
| HNO3 | 0.10 | 88.90 |
|  | 0.5 | 89.12 |
|  | 1.0 | 96.40 |
| HCl | 0.10 | 91.42 |
|  | 0.5 | 92.92 |
|  | 1.0 | 93.66 |
| Sodium Acetate | 0.5 | 89.45 |
|  | 1.0 | 93.26 |

*V/m = 0.05 L/g, shaken time= 30.0 min, T = 25±1°C