Supplementary Information

NaYS2:Er3+ - a highly efficient NIR II response multi-photon up-conversion phosphor

Xiumei Yin1†, Wen Xu1,2†, Ge Zhu1, Yanan Ji1, Qi Xiao1, Xinyao Dong1, Ming He1, Baosheng Cao1, Na Zhou1, Xixian Luo1*, Lin Guo 2*, Bin Dong 1*

1Key Laboratory of New Energy and Rare Earth Resource Utilization of State Ethnic Affairs Commission, Key Laboratory of Photosensitive Materials & Devices of Liaoning Province, School of Physics and Materials Engineering, Dalian Minzu University, 18 Liaohe West Road, Dalian 116600, P. R. China.

2School of Chemistry and Environment, Beijing University of Aeronautics & Astronautics, 37 Xueyuan Road, Beijing 100191, PR China.

†These authors contributed equally to this work.

Corresponding authors: Prof. Xixian Luo (luoxx@dlmu.edu.cn); Prof. Lin Guo (guolin@buaa.edu.cn); Prof. Bin Dong (dong@dlnu.edu.cn).

I. Supplementary Methods

1. Materials and Synthesis route

Lanthanide oxide (Y2O3, Lu2O3, La2O3, Gd2O3, or Er2O3; 99.99%), and alkaline metal carbonate (Na2CO3, K2CO3, or Li2CO3; A.R.) were used as the primary materials. Carbon disulfide (CS2, aladdin, ≥99%) was employed as the sulfur source.

MLnS2:Er3+ (M=Li, Na, or K; Ln=Y, Lu, La, or Gd) phosphors were fabricated by the high temperature solid reaction method [S1]. In the typical synthesis process, the Ln2O3 and M2CO3 were mixed and thoroughly ground in an agate mortar for 30 min according to the 1:1.1 ratio, and the doping concentrations of Er3+ ions were 2, 5, 10, and 15 mol%, respectively. The mixture was transferred to the quartz boat and placed into the tube furnace. The samples were heated to 773 K under argon (Ar) atmosphere, and then saturated vapor of CS2 (40 kPa) was flowed in Ar at a flow rate of 50 mL/min. The final products were obtained after calcining the mixture at 1073, 1173, 1273, or 1373 K for two hours and washing by water and ethanol for several times.

2. Characterization

The X-ray diffraction (XRD) patterns were characterized by the Shimadzu XRD-6000 X-ray diffractometer with a Cu Kα (λ=0.1541 nm). Scanning electron microscopic (SEM) images were performed by the Hitachi S-4800 scanning electron microscope. Transmission electron microscopic (TEM) and high resolution transmission electron microscopic (HRTEM) images were measured by using a JEM-2100F transmission electron microscope. The UC luminescence spectra were measured by a Jobin Yvon iHR550 monochromator equipped with 808, 980 and 1532 nm laser diode (LD) (maximum power: 2.0 W). The absorption spectra of the samples were recorded on a Lambda 750 UV–Vis-NIR spectrophotometer (Perkin-Elmer, USA). The photo-luminescent decay curves were obtained by an Andor SR500 monochromator equipped with an R928 photomultiplier tube from Hamamatsu with 980 and 1532 nm excitation wavelength from a pulsed work Horizon OPO laser. The decay profiles were collected using a Tektronix DPO 5104 digital oscilloscope. The Up-conversion quantum yield (UCQY) was measured by the Edinburgh FLS1000 Steady/Transient State Fluorescence Spectrometer, equipped with the detector of electric cooling ultraviolet visible PMT R298 and liquid nitrogen cooling near infrared PMT R5509. The underwater optical communication test was performed by a self-designed system, the signal transmitter was composed of a signal generator and 1532 nm laser diode (LD), Jobin Yvon iHR550 monochromator and oscilloscope constitute the signal receiver.

Note 1 Transition rate equation for green emission in MnLnS2:Er3+

In order to understand qualitatively the UC luminescence mechanism in Er3+, a set of rate equations were established based on the well-known UC process:

dN1dt=R'21N2+W1N12+σ01ρN0-σ13ρN1-R1N1          (S1)

dN2dt=R'32N3-σ24ρN2-R'21N2-R2N2                  (S2)

dN3dt=R'43N3+σ13ρN1-σ35ρN3-R'32N3-R3N3         (S3)

dN4dt=R'54N5+σ24ρN2-R'43N4-R4N4                  (S4)

dN5dt=σ35ρN3-R'54N5-R5N5                          (S5)

NEr=N0+N1+N2+N3+N4+N5                       (S6)

where N0, N1, N2, N3, N4, and N5 denote the population densities of 4I15/2, 4I13/2, 4I11/2, 4I9/2, 4F9/2, and (2H11/2+4S3/2) levels of Er3+, respectively. NEr is the nominal ion density corresponding to Er3+ doping concentration. R1, R2, R3, R4, and R5 are the radiative rates of 4I13/2, 4I11/2, 4I9/2, 4F9/2 and (2H11/2+4S3/2) levels of Er3+, respectively. R'ij is non-radiative rate from level i to level j. W is the rate of the energy transfer process between Er3+ ions. ρ is the laser photon number density. σij denotes the absorption cross-section between level i and j of Er3+. Taking into account that the excited state populations (<1016 ions/cm3) are a small fraction of all the Er3+ ions (NEr>1020 ions/cm3), it can be assumed that N0≈NEr. At steady state (dNi/dt=0), the rate equations can be simplified as:

W1N12+σ01ρN0-σ13ρN1=0                           (S7)

R'32N3-σ24ρN2-R2N2=0                            (S8)

σ24ρN2-R4N4=0                                    (S9)

NEr=N0                                              (S10)

The intensities of green emissions (Igreen) can be given according to the population densities of N5:

Igreen=N5R5=σ132σ35ρ3W1(R3+R'32+σ35ρ)           (11)

Note 2.  Principle of UCQY determination

The upconversion quantum yield (UCQY) is defined as the ratio of the number of emitted upconverted photons to the number of absorbed NIR photons, which can be described as the following formula [Ref. S2, ACS Nano, 5, 4981-4986],

(S11)

The UCQY of NaYS2:Er3+ excited by 980 nm are measured and used as a reference. The UCQY of the samples to be measured and referenced can be describe as the following equations (S12) and (S13):

(S12)

(S13)

where the UCQYS and UCQYR are the UCQY of the sample to be determined and reference sample, respectively. ES and ER are the numbers of the emitted photons for measured sample and reference sample; and AS and AR are the numbers of the photons absorbed by measured sample and referenced sample, respectively. According to equations (S12) and (S13), the UCQYS of the sample can be determined:

(S14)

The UCQY of the measured sample can be calculated by the luminescence intensities and the absorption values of the measured sample and the reference sample.

Note 3.  Measurement of UCQY

The UCQY of NaYS2:Er3+ phosphor under 980 nm excitation is measured by the Edinburgh FLS1000 Steady/Transient State Fluorescence Spectrometer, equipped with detector of electric cooling ultraviolet visible PMT R298 and liquid nitrogen cooling near infrared PMT R5509. The measured UCQY of NaYS2:Er3+ phosphor excited by 980 nm excitation is 0.45%.

Note 4. Determination of PDs’s performance

Three representative parameters to characterize the performance of the PDs including photo-responsivity (R), detectivity (D*) and external quantum efficiency (EQE). R represents the photocurrent (Iph) generated per unit of incident power, D* is the ability of detecting weak signal from a noisy environment, and EQE presents the number of carriers produced in the external circuit for each absorbed incident photon, respectively. They are defined by the following equations:

R=Ilight-IdarkPS ,                                    (S15)

D*=R2eIdark/S12 ,                                  (S16)

EQE=Rhcλe ,                                     (S17)

where Ilight and Idark are the photocurrents of PDs separately under the light illumination and in the dark; P is the input light power intensity, S is the effective illuminated area; h, c, λ, and e represents the Planck’s constant, the velocity of light, the wavelength of incident light, and the elementary charge, respectively.

II. Supplementary Figures

Figure S1 XRD patterns of NaYS2:Er3+ prepared at 1073, 1173, 1273, and 1373 K. The samples prepared at 1073 and 1173 K are hexagonal phase NaYS2, while there are two phases of Y2O2S and NaYS2 while the synthesis temperature of 1273, and 1373 K.

Figure S2 UC luminescence spectra of NaYS2:Er3+ phosphor prepared at 1073, 1173, 1273, and 1373 K under the excitation source is 1532 nm (inset: integral intensity of NaYS2:Er3+ varies with synthesis temperature). The luminescence intensity of the samples present a tendency to increase first and then decrease with the temperature rises.

Figure S3 SEM images of LiYS2, NaYS2, KYS2, NaLaS2, NaGdS2, and NaLuS2 phosphors.

Figure S4 Dependence of the green, red and NIR integral UC emission intensities of NaYS2:Er3+ on the excitation power of 1532 nm.

Figure S5 Decay profiles of 564 nm (corresponding to the 4S3/2→4I15/2 transition) under the excitation with 1532 nm for NaYS2 doping with 2, 5, 10, 15 mol% Er3+. The lifetime values increase rapidly from 0.87 ms to 3.37 ms when Er3+ concentration increases from 2 to 5 mol%, and then decrease as the concentration continues increasing to 15 mol%, which might illustrates that a concentration quenching effect occurs while the Er3+ concentration higher than 5 mol%.

Figure S6 Decay profiles of 660 nm (corresponding to the 4F9/2→4I15/2 transition) under the excitation with 1532 nm for NaYS2 doping with 2, 5, 10, 15 mol% Er3+, the lifetimes of the 4F9/2 state are evaluated to be 0.28-0.56 ms.

Figure S7 Decay profiles of 800 nm (corresponding to the 4I9/2→4I15/2 transition) under the excitation with 1532 nm for NaYS2 doping with 2, 5, 10, 15 mol% Er3+. And the lifetimes of the 4I9/2 state are evaluated to be 4.8-10.28 ms.

Figure S8 Decay profiles of 1000 nm (corresponding to the 4I11/2→4I15/2 transition) under the excitation with 1532 nm for NaYS2 doping with 2, 5, 10, 15 mol% Er3+.

Figure S9 Decay profiles of 1500 nm (corresponding to the 4I13/2→4I15/2 transition) under the excitation with 980 nm for NaYS2 doping with 2, 5, 10, 15 mol% Er3+. NaYS2:Er3+ phosphors have ultra-long lifetimes of 9.44 to 33.04 ms, respectively.

Figure S10 Decays curves of 4I9/2 level to 4I13/2 level transition of Er3+ in MLnS2 (M=Li, K; Ln=La, Y, Lu, Gd).

Figure S11 Decays curves of 4I11/2 level to 4I13/2 level transition of Er3+ in MLnS2 (M=Li, K; Ln=La, Y, Lu, Gd).

Figure S12 Integral intensity of NaYS2:Er3+ excited by 1532 nm and NaYF4:Er3+ excited by 980 nm with various excitation power density (W/cm2).

Figure S13 Absorption spectrum of NaYS2:Er3+. The peaks value at 980 nm and 1532 nm are used to determine the parameter of AR/AS in the equation (S4), which is calculated to be about 0.47.

Figure S14 UC luminescence spectra of NaYS2:5%Er3+ excited by 980 and 1532 nm under the same power density (4.8 W/cm2). The excitation at 980 nm and 1532 nm are from the same tunable optical parametric oscillator. The emission intensity of NaYS2:5%Er3+ excited by 1532 nm are found to be about 28.9 times of 980 nm. According to equation (S4), the UCQY of NaYS2:5%Er3+ under 1532 nm excitation is 6.13%

Figure S15 Top view SEM image of the NaYS2:Er3+/MAPbI3 hybrid.

Figure S16 Absorption spectrum of MAPbI3 films as well as emission spectra of NaYS2:Er3+ phosphor from 2H9/2, 2H11/2, 4S3/2, 4F9/2→4I15/2 transitions under 808 nm, 980 nm, and 1532 nm excitation, respectively.

Figure S17 EQE of the NaYS2: Er3+/MAPbI3 PD.

Figure S18 On-off switching currents at the lowest detectable excitation power density of NaYS2:Er3+/MAPbI3 device under 808, 980, and 1532 nm, respectively.

III. Supplementary Tables

Table S1 Decay time constants τ (ms) of 4S3/2 (564 nm), 4F9/2 (650 nm), 4I9/2 (800 nm), 4I11/2 (1000 nm), and 4I13/2 (1500 nm) levels in NaYS2:xEr3+ (x=2, 5, 10, 15 mol%).

| Samples | 4S3/2 | 4F9/2 | 4I9/2 | 4I11/2 | 4I13/2 |
| --- | --- | --- | --- | --- | --- |
| NaYS2:2%Er3+ | 0.87 | 0.28 | 10.28 | 2.33 | 33.04 |
| NaYS2:5%Er3+ | 3.37 | 0.56 | 9.24 | 2.18 | 30.27 |
| NaYS2:10%Er3+ | 3.25 | 0.50 | 6.18 | 1.94 | 19.18 |
| NaYS2:15%Er3+ | 2.24 | 0.42 | 4.80 | 1.67 | 9.44 |

\

Table S2 Calculated decay time constants (τ; ms) of different transitions for Er3+ ions in MLnS2:5%Er3+ under 1532 nm excitation and NaYF4:Yb3+,Er3+ under 980 nm excitation.

| Samples | 4S3/2 | 4F9/2 | 4I9/2 | 4I11/2 | 4I13/2 |
| --- | --- | --- | --- | --- | --- |
| α-LiYS2 | 1.26 | 0.83 | 2.40 | 2.83 | 4.69 |
| β-KYS2 | 2.37 | 0.98 | 7.45 | 2.54 | 13.12 |
| α-NaLaS2 | 1.77 | 0.79 | 2.84 | 2.52 | 7.08 |
| β-NaYS2 | 3.37 | 0.56 | 9.24 | 2.18 | 30.27 |
| β-NaLuS2 | 2.47 | 0.82 | 9.03 | 1.97 | 29.28 |
| β-NaGdS2 | 1.64 | 0.57 | 7.78 | 1.41 | 18.77 |
| β-NaYF4 | 4.83 | 0.82 | 0.98 | -- | 9.92 |

Table S3 Performance of several NIR photodetectors

Supplementary References

[S1] Masuda, H. Fujino, T. Sato, N. & Yamada K. Electrical properties of Na2US3, NaGdS2 and NaLaS2. Mater. Res. Bull. 34, 1291-1300 (1999).

[S2] Chen, G. Ohulchanskyy, T. Y. Kachynski, A. Ågren, H. & Prasad, P. N. Intense visible and near-Infrared upconversion photoluminescence in colloidal LiYF4:Er3+ nanocrystals under laser excitation of 1490 nm. ACS Nano 5, 4981-4986 (2011).

[S3] Saran, R. & Curry, R. J. Lead sulphide nanocrystal photodetector technologies. Nat. Photonics 10, 81-92 (2016).

[S4] An, X. Liu, F. Jung, Y. J. & Kar, S. Tunable graphene-silicon heterojunctions for ultrasensitive photodetection. Nano Lett. 13, 909-916 (2013).

[S5] Ageno, W. Eikelboom, J. & Lip. G. Y. H. Dabigatran in clinical practice: contemporary overview of the evidence. Int. J. Cardiol. 220, 417-428 (2016).

[S6] Dias, S. Kumawat, K. Biswas, S. & Krupanidhi, S. B. Solvothermal synthesis of Cu2SnS3 quantum dots and their application in near-infrared photodetectors. Inorg. Chem. 56, 2198-2203 (2017).

[S7] Huang, F. et al. Towards high performance broad spectral response fullerene based photosensitive organic field-effect transistors with tricomponent bulk heterojunctions. Carbon 118, 666-674 (2017).

[S8] Na, J. Park, K. Kim, J. T. Choi, W. K. & Song, Y. W. Air-stable few-layer black phosphorus phototransistor for near-infrared detection. Nanotechnology 28, 085201 (2017).

[S9] Kataria, M. et al. Transparent, wearable, broad band, and highly sensitive upconversion nanoparticles and graphene based hybrid photodetectors. ACS Photonics 5, 2336-2347 (2018).

[S10] Wu, J. et al. Enhanced performance of a graphene/GaAs self-driven near-infrared photodetector with upconversion nanoparticles. Nanoscale 10, 8023-8030 (2018).

[S11] Chitara, B. Panchakarla, L. S. Krupanidhi, S. B. & Rao, C. N. R. Infrared photodetectors based on reduced graphene oxide and graphene nanoribbons. Adv. Mater. 23, 5419-5424 (2011).

[S12] Xiang, H. et al. Heavy-metal-free flexible hybrid polymer-nanocrystal photodetectors sensitive to 1.5 μm wavelength. ACS Appl. Mater. Inter. 11, 42571-42579 (2019).

[S13] Zhao, X. Song, L. Zhao, R. & Tan, M. C. High-performance and flexible Shortwave infrared photodetectors using composites of rare earth-doped nanoparticles. ACS Appl. Mater. Inter. 11, 2344-2351 (2019).