Supporting information

Determination of the activation energies of phase transition for calcium orthophosphates based on powder X-ray diffraction data

Kateryna Vasylenko1, Yuriy Sakhno2*; Deb Jaisi2; and Mykola Nikolenko1*

1Faculty of Chemical Technologies and Ecology, Ukrainian State University of Chemical Technology, Dnipro, Ukraine, 49005

2Department of Plant and Soil Sciences, University of Delaware, Newark, Delaware, 19716

Corresponding author:

Mykola Nikolenko: n_nikolenko@ukr.net,

Fig. SI 1. The X-ray diffraction pattern of calcium orthophosphate precipitated at pH 9, temperature 20 °C and initial ratio Ca/P = 1.5. Aging conditions in mother solution: 24 hours at temperature 20 °C with initial heat treatment during 6 hours at 250 0С in a high-pressure reactor. The figure shows dicalcium phosphate anhydrous (PCPDFWIN No. 77-0128) with the blue lines and hydroxyapatite (PCPDFWIN No. 74-0566) with the magenta lines.

Fig. SI 2. The X-ray diffraction pattern of calcium orthophosphate precipitated at pH 10, temperature 20 °C and initial ratio Ca/P = 1.5. Aging conditions in mother solution: 24 hours at temperature 20 °C with initial heat treatment during 6 hours at 250 0С in a high-pressure reactor. The figure shows dicalcium phosphate anhydrous (PCPDFWIN No. 77-0128) with the blue lines and hydroxyapatite (PCPDFWIN No. 74-0566) with the magenta lines.

Fig. SI 3. The X-ray diffraction pattern of calcium orthophosphate precipitated at pH 11, temperature 20 °C and initial ratio Ca/P = 0.5. Aging conditions in mother solution: 24 hours at temperature 20 °C. The figure shows dicalcium phosphate anhydrous (PCPDFWIN No. 77-0128) with the blue lines and hydroxyapatite (PCPDFWIN No. 74-0566) with

the magenta lines.

Fig. SI 4.  Red curve is diffractogram of pure HA maturated at 50С. Grey bars show the results of the calculation of activation energies for this sample.