Photorefractive and pyroelectric photonic memory and long-term stability in thin-film lithium niobate microresonators

Xinyi Ren1,2, Chun-Ho Lee1,2, Kaiwen Xue1, Shaoyuan Ou1, Yue Yu1, Zaijun Chen1, and Mengjie Yu1*

1Ming Hsieh Department of Electrical and Computer Engineering, University of Southern California, Los Angeles, California 90089, USA

2These authors contributed equally: Xinyi Ren, Chun-Ho Lee.

E-mail: mengjiey@usc.edu

Supplementary Information

Section 1: Experimental setup

Section 2: Thermo-optic bistability and fast-relaxation PR in X-cut LN microresonators

Section 3: PE and TO response in different orientations devices

Section 4: Supplementary tables

1. Experimental setup

Figure S1 illustrates the schematic for the PR characterization setup, which consists of the control and probe laser beam paths for excitation and monitor, respectively. An erbium doped fiber amplifier is placed after the control laser to amplify and adjust the injecting optical power. Two wavelength division multiplexers are used to combine and separate the control and probe light at near 1546 nm and 1550 nm, respectively. By adjusting the polarization controller and the polarizer, we can pump light at the TE or transverse magnetic (TM) mode in the waveguide. The transmitted control light is monitored by a power meter, while the transmission spectrum of the probe light is recorded by a data acquisition card. The chip is placed on a TEC to keep at a stable temperature, preventing temperature-induced drifts during the photorefraction measurement.

Figure S1. Experimental setup for characterization the PR effect. EDFA, erbium-doped fiber amplifier; ISO, isolator; PC, polarization controller; WDM, wavelength division multiplexer; TEC, thermo-electric controller; P, polarizer; PD, photodetector; DAC, data acquisition card.

2. Thermo-optic bistability and fast-relaxation PR in X-cut LN microresonators

Figure S2 shows the transmission spectrum of one optical resonance in a X-cut LN microresonator. Increasing the input power from -7.5 dBm to 5.2 dBm in the waveguide, the thermo-optic bistability is observed. The black arrow shows the blue shift trend due to the PR. However, when the high-power light is turned off, the resonance is restored to the initial position.

Figure S2. Forward and backward transmission spectra under different injection power in X-cut microresonators.

3. PE and TO response in different orientations devices

For X cut TE mode, we record the index change when heating up (red solid dots). It is followed by the subsequent temperature decrease (red cross dots), in which the index change still follows the original linear function. Thus, the PE effect in the X-cut LN also shows the rapid relaxation and the TO effect contributes to dn/dT of . Furthermore, we repeat this process in the X-cut for the TM mode with an extracted dn/dT of . The difference is due to the different TO coefficients for ordinary and extraordinary conditions, which agree with the literature [27].

Figure S3. The measured wavelength shift in the X-cut device with different polarization modes (red and green dots). The index change is due to the TO effect and shows no hysteresis when the temperature is ramped up and down. Solid dots: temperature ramp-up; Cross dots: temperature ramp-down.

4. Supplementary tables

Table 1. Fitted parameters of the PE relaxation

| Fit item | a1 | a2 | T1 [h] | T2 [h] |
| --- | --- | --- | --- | --- |
| 70 ℃ |  |  | 1.72 | 4.19 |
| 66 ℃ |  |  | 0.56 | 3.06 |
| 63 ℃ |  |  | 2.25 | 0.18 |
| 54 ℃ |  |  | 1.16 | 3.71 |

Table 2. Summary of PR and PE effects in LN microresonators

| Effect | Cut | Mode | dn/dT [/℃] | Recovery time |
| --- | --- | --- | --- | --- |
| PRa) | Z-cut | TE | / | > 20 h |
|  | X-cut | TE | / | fast |
| PEb) | Z-cut | TE |  | >10 h |
| TOc) | X-cut | TE |  | fast |

a) Photorefractive; b) Pyroelectric; c) Thermo-optic;