Highly-sensitive detection of CP-type synthetic cannabinoids from e-cigarettes by novel Zn/Bi bimetallic organic framework-derived ZnO-Bi2O3 heterojunctions sensing platform

Haiou Chena, Ying Hea, Shimeng Duana, Anyun Xua, Meng Lia, Yanming Renb, Ruilin Zhangb, Xiangjun Yanga, Shixiong Wanga,*, Huiping Baia,*

a School of Chemical Science and Engineering; School of Material and Energy; Yunnan Key Laboratory of Micro/Nano Materials & Technology; Yunnan University, Kunming 650091, China

b NHC Key Laboratory of Drug Addiction Medicine, School of Forensic Medicine, Kunming Medical University, Kunming 650050, China

*Corresponding author.

E-mail addresses: baihuiping@ynu.edu.cn; wangshixiong@ynu.edu.cn.

Fig S1. N2 adsorption-desorption isotherms of synthesized ZnBi-BTC (a) and ZnO-Bi2O3 (b), the XRD patterns of ZnBi-BTC (c).

According to the literature, the XRD peaks marked with blue pentagrams represent Bi-BTC synthesis,1 while the XRD peaks of Zn-BTC are represented by green triangles.2

Fig S2. DPV responses on bare SPE with different concentration (a) and the calibration curve (b) of CP47,497; DPV responses with different concentration (c) and the calibration curve (d) of CP55,940 in pH 9 BBS.

Fig S3. SEM images of ZnO-Bi2O3 synthesized with different methanol and DMF volume ratio: 1:0 (a,f), 2:1 (b,g), 1:1 (c,h), 1:2 (d,i), 0:1 (e,k).

Fig S4. SEM images of ZnO-Bi2O3 at different Zn and Bi molar ratio 1:0 (a,e), 3:1(b,f), 1:1 (c,g) and 0:1(d,h).

Fig S5. SEM images of ZnO-Bi2O3 after calcination at 400 ℃ (a,d), 500 ℃ (b,e), 600 ℃ (c,f) for 2 hours.

Fig S6. TGA profile of ZnBi-BTC

Table S1. Overview of CP47,497of the oxidation products observed in the UHPLC-LTQ/Orbitrap HRMS analysis and their corresponding information.

| Compound | Retention time (min) | Measured m/z [M+Na]+ | Theoretical m/z [M+Na]+ | Chemical formula | Structure |
| --- | --- | --- | --- | --- | --- |
| CP47,497 | 1.13 | 341.2451 | 341.2451 | C21H34O2 |  |
| P3 | 1.43 | 338.2300 | 339.2299 | C21H32O2 |  |
| P4 | 1.43 | 338.2300 | 339.2299 | C21H32O2 |  |
| P5 | 1.43 | 338.2300 | 339.2299 | C21H32O2 |  |

Fig S7. HRMS spectra of CP47,497 (m/z 341.2451, C21H34O2Na)

OR

OR

Fig S8. HRMS spectra of P4, P5 and P6 (m/z 339.2300, C21H32O2Na)

Table S2. Overview of CP55,940 of the oxidation products observed in the UHPLC-LTQ/Orbitrap HRMS analysis and their corresponding information.

| Compound | Retention time (min) | Measured m/z [M+Na]+ | Theoretical m/z [M+Na]+ | Chemical formula | Structure |
| --- | --- | --- | --- | --- | --- |
| CP55,940 | 1.06 | 399.2862 | 399.2870 | C24H40O3 |  |
| K3 | 1.53 | 397.2715 | 397.2713 | C24H38O3 |  |
| K4 | 1.53 | 397.2715 | 397.2713 | C24H38O3 |  |
| K5 | 1.53 | 397.2715 | 397.2713 | C24H38O3 |  |
| K6 | 1.53 | 397.2715 | 397.2713 | C24H38O3 |  |

Fig S9. HRMS spectra of CP55,940 (m/z 399.23862, C24H40O3Na)

OR

OR

Fig S10. HRMS spectra of K3, K4, K5 and K6 (m/z 397.2715, C24H38O3Na)

LC-MS/MS detection conditions.

Column conditions: Column: Shimadzu Shim pack Velox PFPP (2.1 mm x 100 mm, 2.7 μm), column temperature 40 ℃, mobile phase A is 10mmol ammonium acetate aqueous solution (containing 5% methanol), and mobile phase B is methanol; Gradient elution, elution procedure: 0-2 min, 20% B, 2-5 min, 20-95% B, 5-7 min, 95% B, 7-7.1 min, 95-20% B, 7.1-10 min, 20% B; The injection volume is 5 μL; The flow rate is 0.3 mL/min.

MS detection conditions: Multi reaction monitoring (MRM) negative ion mode; Atomization gas flow rate: 3 L/min; DL temperature: 250 ℃; Heating block temperature: 400 ℃; Dry gas flow rate: 15 L/min; Converting the voltage of the tanner pole: 6.0 kV; CID gas: 230kPa.

Fig S11. MRM chromatogram of e-cigarettes sample 1 containing CP 47,497

Fig S12. MRM chromatogram of e-cigarettes sample 2 containing CP 47,497

Fig S13. MRM chromatogram of e-cigarettes sample 3 containing CP 47,497

Fig S14. MRM chromatogram of e-cigarettes sample 1 containing CP 55,940

Fig S15. MRM chromatogram of e-cigarettes sample 2 containing CP 55,940

Fig S16. MRM chromatogram of e-cigarettes sample 3 containing CP 55,940

References

1.	Nguyen V H, Van Tan L, Lee T D Nguyen (2021) Solvothermal synthesis and photocatalytic activity of metal-organic framework materials based on bismuth and trimesic acid, Sustain. Chem Pharm 20: 100385. https://doi.org/10.1016/j.scp.2021.100385

2.	Wang X, Ma X, Wang H, Huang P, Du X, Lu X (2017) A zinc(II) benzenetricarboxylate metal organic framework with unusual adsorption properties, and its application to the preconcentration of pesticides. Microchim Acta 184: 3681-3687. https://doi.org/10.1007/s00604-017-2382-1