Collagen-Coated Superparamagnetic Iron Oxide Nanoparticles as a Sustainable Catalyst for Spirooxindole Synthesis

Shima Ghanbari1, Maryam Esmkhani1, Shahrzad Javanshir 1*

1 Heterocyclic Chemistry Research Laboratory, Department of Chemistry, Iran University of Science and Technology, 16846-13114, Tehran, Iran

Figure S 1: FT-IR spectra of the Fe3O4@SiO2/ECH/IG, Fe3O4@SiO2, Fe3O4 and reused Fe3O4@SiO2/ECH/IG.	2

Figure S 2: BET analysis of Fe3O4@SiO2/ECH/IG.	2

Figure S 3: Recyclability of Fe3O4@SiO2/ECH/IG	3

Table S 1: Effect of solvent on model reaction in the presence of Fe3O4@SiO2/ECH/IG	4

Table S 2: Investigation of different types of catalyst in model reaction	4

Table S 3: Investigation the amount of catalyst	4

Figure S 1: FT-IR spectra of the Fe3O4@SiO2/ECH/IG, Fe3O4@SiO2, Fe3O4 and reused Fe3O4@SiO2/ECH/IG.

Figure S 2: BET analysis of Fe3O4@SiO2/ECH/IG.

Figure S 3: Recyclability of Fe3O4@SiO2/ECH/IG

Table S 1: Effect of solvent on model reaction in the presence of Fe3O4@SiO2/ECH/IG

| Entry | Solvent | Time(min) | Yield(%) |
| --- | --- | --- | --- |
| 1 | Ethanol | 30 | 92 |
| 2 | water | 30 | 83 |
| 3 | EtOH/water (1:1) | 30 | 94 |
| 4 | CH3CN | 30 | 21 |
| 5 | CHCl3 | 30 | 17 |
| 6 | MeOH | 30 | 61 |

*Reaction condition: Isatin 1 (1 mmol), 2 (1 mmol), 1,3-dicarbonyl 3 (1 mmol), 10 mg catalyst, and 3 ml solvent at 60 °C.

Table S 2: Investigation of different types of catalyst in model reaction

| Entry | Catalyst | (C°)Temperature | (%)yield |
| --- | --- | --- | --- |
| 1 | Fe3O4@SiO2/ECH/IG | rt | Trace |
| 2 | Fe3O4@SiO2/ECH/IG | 40 | 69a |
| 3 | Fe3O4@SiO2/ECH/IG | 60 | 83a |
| 4 | Fe3O4@SiO2/ECH/IG | 80 | 78a |
| 5 | Fe3O4@SiO2/ECH/IG | 60 | 94a |
| 6 | IG | 60 | 91b |
| 7 | Fe3O4 | 60 | 74b |
| 8 | Fe3O4@SiO2 | 60 | 75b |
| 9 | Fe3O4@SiO2-ECH | 60 | 85b |

*Reaction conditions: isatin (1 mmol), malononitrile (1 mmol), dimedone (1 mmol), catalyst (0.01 g) in EtOH/water (1:1) 3ml

a 10min 	   b 30min

Table S 3: Investigation the amount of catalyst

| Entry | (mg) Catalyst | (%)Yield |
| --- | --- | --- |
| 1 | 3 | 66 |
| 2 | 5 | 79 |
| 3 | 10 | 94 |
| 4 | 15 | 94 |

*Reaction condition: Isatin 1 (1 mmol), 2 (1 mmol), 1,3-dicarbonyl 3 (1 mmol), and 3 ml solvent at 60°C for 30 min.