Supporting Information

CO2 adsorption on a water-resist HKUST-1 by incorporation of Graphene Oxide

Sandra Loera-Sernaa*, Jonathan Cortés-Suáreza, Roque Sanchez-Salasa, D. Ramírez-Rosalesb, M. Oliver-Tolentinoc, and Enrique V. Ramos-Fernándezd

a Universidad Autónoma Metropolitana-Azcapotzalco, Área de Química de Materiales, Av. San Pablo 180, Col. Reynosa Tamaulipas, 02200, Ciudad de México, Mexico.

b Instituto Politécnico Nacional, ESFM-Departamento de Física, UPALM Edif. 9 Zacatenco, GAM, Ciudad de México, 07738, Mexico

c CONACYT-Universidad Autónoma Metropolitana-Iztapalapa, Departamento de Química, CP 09340 México, México

d Laboratorio de Materiales Avanzados, Departamento de Química Inorgánica- Instituto Universitario de Materiales, Universidad de Alicante, Ctra. San Vicente- Alicante s/n, E-03690 San Vicente del Raspeig, Spain

*sls@azc.uam.mx

ORCID: SLS: 0000-0001-9562-3195, RSS: 0000-0001-6393-9152, DRR: 0000-0001-7815-2029, MOT: 0000-0001-8454-0837, EVRF: 0000-0001-6357-0383.

# Fig. S1. FTIR, and SEM micrograph from GO. The spectra bands are located at 3430 cm-1 (O-H stretching vibrations), 1726 cm-1 (C=O stretching vibrations from carbonyl and carboxylic groups), 1226 cm-1 (C-OH stretching vibrations) and 1103 cm-1 (C-O in epoxy stretching vibrations); these stretching modes are typically found in GO and are assigned to oxygen species created during the synthesis. SEM morphology from the GO layers shows a heterogeneous distribution at the GO material with the characteristic laminar surface.

# Fig. S2. Morphology and EDX scanning micrographs of GO-Culow mapping of Cu, O, and C.

| # Sample | # C (wt.%) | # O (wt.%) | # S (wt.%) | # Cl (wt.%) | # Cu (wt.%) |
| --- | --- | --- | --- | --- | --- |
| # GO | # 62.1 | # 33.6 | # 3.7 | # 0.6 |  |
| # GO-Culow | # 49.4 | # 42.8 | # 1.0 | # 0.2 | # 6.6 |
| # GO-Cuhigh | # 41.2 | # 43.8 | # 1.2 | # 0.1 | # 13.7 |

Fig. S3. EDX elemental scanning identification measured on GO, GO-Culow, and GO-Cuhigh samples where carbon, oxygen, sulfur, chlorine, and copper wt.% peaks signals were detected and quantified.

Fig. S4. a) Galvanostatic profile of GO@HKUST-1low at 0.25 Ag-1; b) charge retention for 1700 galvanostatic cycles.

Fig. S5. TGA on air conditions mass loss of HKUST-1 and GO@HKUST-1high.

Fig. S6. XDR of HKUST-1 and GO@HKUST-1high after the water adsorption test, moreover GO@HKUST-1high sample before the test is compared.