Supplementary material for:

Spent lithium-ion battery recycling: multi-stage synergistic deep removal of impurities and lithium extraction

Wen-bo LOUa, Dong-yan LIUb*, Yun WANGa, Da ZHAOa, Zi-cheng SUNa, Yi ZOUa, Sheng-yan WANGb, Quan-guo CHENGa, Jian-zhong LIc, Hong-hui LIUd

a College of Environment, Shenyang University, Shenyang 110044, China

b Normal College, Shenyang University, Shenyang 110044, China

c School of Metallurgy, Northeastern University, Shenyang 110819, China

d School of Chemical Safety, North China Institute of Science and Technology, Langfang 065201, China

*Corresponding author: dy_liu1991@163.com

Fig. S1 Variation trend of ionic forms of elements ((a) ~ (g): Cu, Al, Fe, Li, Mg, Ni, Zn) in solution with pH

In Fig. S1, it is plotted the relationship between the percentages of ionic forms of each metal over the total elemental amount versus ph in the liquid-phase system. Let's take Eq. (37) as an example to illustrate the plotting of Fig. S1b

Eq.（37）

The equations related to it in Table 3 are Eq.（5）, Eq.（6）, and Eq.（19）.

Selected data of Table 3 The potential reaction equations of metal ions in solution

| NO. | Equations | lg K |
| --- | --- | --- |
| 5 |  | 9.27 |
| 6 |  | 33.03 |
| 19 |  | -14.00 |

For Eq. (5) there exists an equilibrium equation:

After conversion, it is

(lgK5=9.27)          Eq.（S1）

Similarly, for Eq. (6) there is:

(lgK6=33.03)        Eq.（S2）

For Eq. (19) there always exists an equilibrium equation:

(lgK19=-14.00)

After conversion, it is

Eq.（S3）

Bringing Eq. (S1), Eq. (S2) and Eq. (S3) into Eq. (37) leads to

Eq.（S4）

Then the relation with ph for the percentage of total Al element in the form of Al3+ is

Eq.（S5）

Likewise, Al(OH)4- and Al(OH)2+ are related to pH as follows:

Eq.（S6）

Eq.（S7）

Subsequently, the different pH values are submitted into the Eq.（S5~S7）to obtain the corresponding results, and the plotting leads to Fig. S1b.

Fig. S2 The curve of lg[Me]T vs. pH in Me-H2O system at 25oC without phosphate

Fig. S3 The curve of impurity content in precipitates vs. temperature

Table.S1 The potential reaction equations of metal ions in precipitation process

| NO. | Equations | Coefficient of anion depletion by metal ions |
| --- | --- | --- |
| Eq.（S8） |  | 1/3 |
| Eq.（S9） |  | 1 |
| Eq.（S10） |  | 2/3 |
| Eq.（S11） |  | 2/3 |
| Eq.（S12） |  | 2/3 |
| Eq.（S13） |  | 2/3 |
| Eq.（S14） |  | 1 |
| Eq.（R15） |  | 2 |
| Eq.（S16） |  | 3 |
| Eq.（S17） |  | 2 |
| Eq.（S18） |  | 2 |
| Eq.（S19） |  | 2 |
| Eq.（S20） |  | 3 |