Table 1 leaching processes of spent NCM materials with inorganic acids

| Raw material | Leaching agent + reducing agent | Liquid-solid ratio(mL:g) | Time (min) | Temperature (oC) | Leaching results |
| --- | --- | --- | --- | --- | --- |
| NCM [29] | 4M HCl | 50:1 | 60 | 80 | Li, Ni, Co, Mn＞99% |
| NCM [30] | 1M H2SO4+5vol.%H2O2 | 50:1 | 240 | 95 | Li:94.5%, Ni:96.4% Co:79.2%, Mn:84.6% |
| NCM [31] | 0.8M H2SO4+0.075M Na2S2O3 | 10:1 | 90 | 70 | Li:99.0%, Ni:98.6% Co:97.9%, Mn:99.1% |
| NCM [32] | 1 M H2SO4 and 0.5 M HNO3+ 2% w/v glucose | 10:1 | 45 | 50 | Li:93.2%,Co:90.5%, Ni:82.8%, Mn: 77.7% |

Table 2 Content of elements in lithium-containing mother liquor

| Elements | Al | Mg | Cu | Zn | Ni | Fe | P | Li |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Content/ g/L | 0.25 | 0.24 | 0.62 | 0.65 | 0.55 | 0.59 | 0.31 | 5.88 |

Table 3 The potential reaction equations of metal ions in solution

| NO. | Equations | lg K |
| --- | --- | --- |
| 1 |  | 0.36 |
| 2 |  | 4.97 |
| 3 |  | 8.55 |
| 4 |  | 11.33 |
| 5 |  | 9.27 |
| 6 |  | 33.03 |
| 7 |  | 11.87 |
| 8 |  | 21.17 |
| 9 |  | 29.67 |
| 10 |  | 7.00 |
| 11 |  | 13.68 |
| 12 |  | 17.00 |
| 13 |  | 18.5 |
| 14 |  | 4.40 |
| 15 |  | 11.30 |
| 16 |  | 14.14 |
| 17 |  | 17.66 |
| 18 |  | 2.58 |
| 19 |  | -14.00 |
| 20 |  | 12.36 |
| 21 |  | 7.20 |
| 22 |  | 2.04 |
| 23 |  | -19.66 |
| 24 |  | -38.68 |
| 25 |  | -15.26 |
| 26 |  | -11.17 |
| 27 |  | -15.78 |
| 28 |  | -32.88 |
| 29 |  | 1.92 |
| 30 |  | -10.63 |
| 31 |  | -20.01 |
| 32 |  | -32.04 |
| 33 |  | -23.98 |
| 34 |  | -31.32 |
| 35 |  | -36.98 |
| 36 |  | -21.89 |

Table 4. The pH values of impurity precipitation without phosphate

| Species | pH at the start of precipitation | pH at the end of precipitation |
| --- | --- | --- |
| Cu(OH)2 | 5.51 | 7.01 |
| Zn(OH)2 | 7.11 | 9.00 |
| Mg(OH)2 | 9.41 | 10.91 |
| Ni(OH)2 | 7.09 | 8.59 |
| Fe(OH)3 | 1.82 | 2.82 |
| Al(OH)3 | 3.75 | 4.75 |

Table 5 The pH value of conversion from phosphate to hydroxide under different [P]

| Element | The pH of conversion when [P]=0.01M | The pH of conversion when [P]=0.1M |
| --- | --- | --- |
| Al | 7.30 | 7.90 |
| Ni | 10.30 | 10.70 |
| Fe | 3.70 | 4.70 |
| Cu | 8.30 | 8.90 |
| Zn | 9.90 | 10.50 |
| Mg | 11.50 | 11.90 |

Table 6 Experimental results of practical synergistic impurity removal

| Element | pH=2.37 |  | pH=8.66 |  | pH=11.00 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Precipitation efficiency/ % | Residual content in mother liquor/ g/L | Precipitation efficiency/ % | Residual content in mother liquor/ g/L | Precipitation efficiency/ % | Residual content in mother liquor/ g/L |
| Li | 0.25 | 5.87 | 0.71 | 5.82 | 0.79 | 5.78 |
| Fe | 43.29 | 0.33 | 100.00 | 0.00 | / | / |
| Al | 18.72 | 0.20 | 100.00 | 0.00 | / | / |
| P | 100.00 | 0.00 | / | / | / | / |
| Mg | 0.02 | 0.24 | 41.15 | 0.14 | 100.00 | 0.00 |
| Zn | 16.06 | 0.55 | 100.00 | 0.00 | / | / |
| Cu | 18.81 | 0.50 | 100.00 | 0.00 | / | / |
| Ni | 20.16 | 0.44 | 100.00 | 0.00 | / | / |

Table 7 The comparison of impurities removal cost for different methods

| Element | Amount contained in 1000L/ mol | Phosphate method | Synergistic hydrolysis method |  |
| --- | --- | --- | --- | --- |
|  |  | Consumption of additional phosphate ions/ mol | Consumption of existing phosphate in the system/ mol | Consumption of hydroxide/ mol |
| Al | 9.26 | 9.26 | 1.60 | 22.99 |
| Mg | 10.00 | 6.67 | 0.00 | 19.99 |
| Cu | 9.76 | 6.51 | 1.60 | 14.72 |
| Zn | 10.00 | 6.67 | 1.37 | 15.89 |
| Ni | 9.32 | 6.21 | 1.72 | 13.49 |
| Fe | 10.54 | 10.54 | 3.69 | 20.54 |
| P | 10.00 | / | / | / |
| Li | 840.00 | 11.20 | 0.02 | / |
| T(PO43-) consumed/ mol | / | 47.05 | 10.00 | / |
| T(OH-) consumed/ mol | / | / | / | 107.62 |
| Na₃PO₄·12H₂O consumed/ kg | / | 17.89 | / | / |
| NaOH consumed/ kg | / | / | / | 4.30 |
| Cost/ yuan | / | 64.39 | / | 10.76 |