Supplementary Data File

Radiation Synthesis and Characterization of Polymeric Wet Adhesives for Attracting and Trapping Insects

M. A. Elhady1, I. M. Mousaa2, Ahmed Awadallah-F1,

1 Radiation Research of Polymer Department, Industrial Irradiation Division, National Centre for Radiation Research and Technology (NCRRT), P.O. Box 29, Nasr City , Egyptian Atomic Energy Authority, Egypt

2Radiation chemistry Department, Radiation Research Division, National Centre for Radiation Research and Technology (NCRRT), P.O. Box 29, Nasr City , Egyptian Atomic Energy Authority, Egypt

| Contents | Page |
| --- | --- |
| FTIR analysis ………………………………………………………………………………………….……….. | 2 |

FTIR analysis

Figure S1 shows the FTIR spectra of PVP, OA and PI without exposure to -rays and irradiated sample of (PVP9-PI)1/OA2-20. It can be seen that the double bond of OA or PI are exited at 1652 cm-1 before irradiation and disappeared after irradiation. This is due to a certain reaction was occurred to form the crosslinking process during the exposure of (PVP-PI)/OA to -rays.

Fig. S1. FTIR spectra of PVP, OA and PI components without irradiation of -rays and irradiated PVP9-PI)1/OA2-20 sample.