Supporting Information

Wearable electrodriven switch actively delivers macromolecular drugs to fundus in non-invasive and controllable manners

Xuan Qin,1,# Haoliang Shi,1,# Hongyang Li,1,# Binbin Chu,1 Jiawei Zhang,1 Zhen Wen1,*, Xuhui Sun1,*, Houyu Wang1,* & Yao He1,2,3,*

1 Suzhou Key Laboratory of Nanotechnology and Biomedicine, Institute of Functional Nano & Soft Materials & Collaborative Innovation Center of Suzhou Nano Science and Technology (NANO-CIC), Soochow University, Suzhou 215123, China

2 Macao Translational Medicine Center, Macau University of Science and Technology, Taipa 999078, Macau SAR, China

3 Macao Institute of Materials Science and Engineering, Macau University of Science and Technology, Taipa 999078, Macau SAR, China

* Corresponding authors. Email: wenzhen2011@suda.edu.cn (Z Wen); xhsun@suda.edu.cn (XH Sun); houyuwang@suda.edu.cn (HY Wang); yaohe@suda.edu.cn (Y He)

#These authors contributed equally to this work.

This PDF file includes

Supplementary Fig. 1. Distribution of circuit elements and size of flexible circuit boards.	4

Supplementary Fig. 2. Circuit design of the SWG.	5

Supplementary Fig. 3. Monophasic square pulse current output performance of the SWG with the EDDL attached to the rabbit eyeball surface.	6

Supplementary Fig. 4. Cytotoxicity evaluation under various stimulation conditions.	7

Supplementary Fig. 5. Infrared thermographic images under various stimulation conditions.	8

Supplementary Fig. 6. Representative confocal images showing the distribution of FITC-IgG in the fundus delivered by different stimulation times of WES (including 30 s, 2 min, 5 min and 10 min).	9

Supplementary Fig. 7. Representative confocal images showing the distribution of FITC-IgG in eyeballs delivered by different frequencies of WES.	10

Supplementary Fig. 8. Representative confocal images showing the distribution of FITC-IgG in eyeballs delivered by WES and intravitreal injection.	11

Supplementary Fig. 9. DNA origami design for imaging.	12

Supplementary Fig. 10. Zeta potential of the rDOSs and EVs.	13

Supplementary Fig. 11. Representative confocal images showing the distribution of TAMRA-rDOSs in the fundus via WES and intravitreal injection.	14

Supplementary Fig. 12. Representative confocal images showing the distribution of DiD-EVs in the fundus via WES and intravitreal injection.	15

Supplementary Fig. 13. Column plot of the relative TEER values of ARPE-19 cells over time after 10 min of WES.	16

Supplementary Fig. 14. Representative confocal images and statistical analysis of IF staining of mouse eyeballs after different treatments.	17

Supplementary Fig. 15. Optical images indicating the changes in WES-treated ARPE-19 cell junctions with potential distribution.	18

Supplementary Fig. 16. Representative fluorescence images and statistical analysis of intracellular Ca2+ in ARPE-19 cells subjected to WES.	19

Supplementary Fig. 17. Investigation of the intracellular Ca2+ dynamics after different durations of WES.	20

Supplementary Fig. 18. Individual FFA images of lesions in CNV-bearing mice before and after different treatments for 14 days.	21

Supplementary Fig. 19. Representative bright field FFA images of individual lesions in CNV mice before and after different treatments.	22

Supplementary Fig. 20. Representative ERG and statistical analysis of B waves in CNV-bearing mice on day 14 after different treatments.	23

Supplementary Fig. 21. Individual H&E-stained images of retinal sections from CNV-bearing mice on day 14 after different treatments.	24

Supplementary Fig. 22. Individual IF staining images of VEGF (green) and CD31 (yellow) in retinal sections from CNV-bearing mice on day 14 after different treatments.	25

Supplementary Fig. 23. Individual average radiance of the bioluminescence signal in tumors after different treatments for 6 days.	26

Supplementary Fig. 24. Gating strategy for CD8+ T cells and CD4+ T cells in choroidal melanoma patients after different treatments.	27

Supplementary Fig. 25. Individual fluorescence-activated cell sorting analysis of CD8+ T cells and CD4+ T cells in choroidal melanoma patients after different treatments.	28

Supplementary Fig. 26. Concentration of TNF-α in choroidal melanoma after different treatments.	29

Supplementary Fig. 27. Representative H&E-stained slices of organs from different groups.	30

Supplementary Fig. 28. Blood biochemistry and blood analysis of mice after different treatments.	31

Supplementary Table 1. Rectangular DNA origami sheets (rDOSs) and the corresponding staple strands (left to right 5’- 3’).	32

Supplementary Table 2. TAMRA-labelled strands (left to right 5’- 3’).	40

Supplementary Table 3. Detailed parameters of the theoretical simulations of WES-facilitated drug electrophoresis via COMSOL software.	41

Supplementary Fig. 1. Distribution of circuit elements and size of flexible circuit boards. The circuit is powered by lithium batteries.

Supplementary Fig. 2. Circuit design of the SWG.

The low-to-high ratio is adjusted by R1 and R2 and can be calculated as follows:

tLtH=R1R1+R2

The frequency is calculated as follows:

frequency≈1.44(R1+2R2)C

Supplementary Fig. 3. Monophasic square pulse current output performance of the SWG with the EDDL attached to the rabbit eyeball surface. The frequency is approximately 0.024 Hz.

Supplementary Fig. 4. Cytotoxicity evaluation under various stimulation conditions. a, Comparative cytotoxicity analysis of ARPE-19 cells and HUVECs exposed to 80 µA direct current (DC) or pulse current (PC) (0.024 Hz) stimulation for 10 min. b, Cytotoxicity assessment of ARPE-19 cells stimulated with SWG at different frequencies. c-d, Cytotoxicity analysis of HUVECs (c) and ARPE-19 cells (d) under WES conditions. The data are presented as the means ± SDs (n=6 per group). P < 0.05 is shown.

Supplementary Fig. 5. Infrared thermographic images under various stimulation conditions. a-b, Representative infrared thermographic images of a rat eye (a) and WES (b) during 10 min. a, Scale bar, 5 mm. b, Scale bar, 12 mm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 6. Representative confocal images showing the distribution of FITC-IgG in the fundus delivered by different stimulation times of WES (including 30 s, 2 min, 5 min and 10 min). Scale bar, 500 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 7. Representative confocal images showing the distribution of FITC-IgG in eyeballs delivered by different frequencies of WES. Scale bar, 400 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 8. Representative confocal images showing the distribution of FITC-IgG in eyeballs delivered by WES and intravitreal injection. Scale bar, 400 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 9. DNA origami design for imaging. For imaging, twenty-four TAMRA-labelled strands (orange) containing extended TAMRA fluorophores at their 5’-ends were used.

Supplementary Fig. 10. Zeta potential of the rDOSs and EVs. a, Zeta potential of the rDOSs. b, Zeta potential of the EVs. The data are presented as the means ± SDs (n=3 per group).

Supplementary Fig. 11. Representative confocal images showing the distribution of TAMRA-rDOSs in the fundus via WES and intravitreal injection. Scale bar, 400 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 12. Representative confocal images showing the distribution of DiD-EVs in the fundus via WES and intravitreal injection. Scale bar, 400 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 13. Column plot of the relative TEER values of ARPE-19 cells over time after 10 min of WES. The data are presented as the means ± SDs (n=3 per group).

Supplementary Fig. 14. Representative confocal images and statistical analysis of IF staining of mouse eyeballs after different treatments. a, Representative confocal images of IF staining of mouse eyeballs after different treatments. Scale bar, 200 µm. b, The mean fluorescence intensity of ZO-1 in RPE layers after different treatments. The data are presented as the means ± SDs (n=3 per group). P < 0.05 is shown. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 15. Optical images indicating the changes in WES-treated ARPE-19 cell junctions with potential distribution. a, Diagram depicting the treatment process and analysis of ARPE-19 cells subjected to WES. P1, P2 and P3 represent position 1, position 2 and position 3, respectively, from the positive electrode to the negative electrode. b, COMSOL simulation showing the electrical potential distribution in circular cell culture dishes under ES. c, Optical microscope images displaying changes in the cellular junctions of ARPE-19 cells from the positive electrode (+) to the negative electrode (-). Scale bar, 50 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 16. Representative fluorescence images and statistical analysis of intracellular Ca2+ in ARPE-19 cells subjected to WES. a, Representative fluorescence images of intracellular Ca2+ in ARPE-19 cells subjected to WES. Scale bar, 20 µm. Intracellular Ca2+ was detected with a Fluo-4 AM fluorescent probe. b, Statistical analysis of the dynamics of intracellular Ca2+ in response to changes in the distribution of electrical potential (n=4 per group). The data are presented as the means ± SDs. P < 0.05 is shown. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 17. Investigation of the intracellular Ca2+ dynamics after different durations of WES. a, Representative confocal images showing the changes in intracellular Ca2+ after treatment with WES for different durations. Scale bar, 20 µm. b, Statistical analysis of the mean fluorescence intensity indicating the changes in intracellular Ca2+ after treatment with different durations of WES. c, Statistical analysis of the mean fluorescence intensity indicating the dynamic changes in intracellular Ca2+ over a 5-hour period after 5 min of WES (n=4 per group). The data are presented as the means ± SDs. P < 0.05 is shown. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 18. Individual FFA images of lesions in CNV-bearing mice before and after different treatments for 14 days. Scale bar, 10 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 19. Representative bright field FFA images of individual lesions in CNV mice before and after different treatments. Red circles mark the initial area of CNV lesions. Scale bar, 10 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 20. Representative ERG and statistical analysis of B waves in CNV-bearing mice on day 14 after different treatments. The data are presented as the means ± SDs (n=6 per group). P < 0.05 is shown. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 21. Individual H&E-stained images of retinal sections from CNV-bearing mice on day 14 after different treatments. Scale bar, 100 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 22. Individual IF staining images of VEGF (green) and CD31 (yellow) in retinal sections from CNV-bearing mice on day 14 after different treatments. Blue, DAPI-labelled cell nuclei. Scale bar, 100 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 23. Individual average radiance of the bioluminescence signal in tumors after different treatments for 6 days.

Supplementary Fig. 24. Gating strategy for CD8+ T cells and CD4+ T cells in choroidal melanoma patients after different treatments.

Supplementary Fig. 25. Individual fluorescence-activated cell sorting analysis of CD8+ T cells and CD4+ T cells in choroidal melanoma patients after different treatments.

Supplementary Fig. 26. Concentration of TNF-α in choroidal melanoma after different treatments. The concentration of TNF-α was evaluated via an ELISA kit. The data are presented as the means ± SDs. The data are presented as the means ± SDs (n=5 per group). P < 0.05 is shown.

Supplementary Fig. 27. Representative H&E-stained slices of organs from different groups. The organs, including the heart, liver, spleen, lung and kidney, were collected from the mice. Scale bar, 200 µm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 28. Blood biochemistry and blood analysis of mice after different treatments. The indicators tested were as follows: red cell volume distribution width (RDW), urea, white blood cell (WBC), mean corpuscular haemoglobin (MCH), haemoglobin (HGB), alanine aminotransferase (ALT), red blood cell (RBC), platelets (PLT) and aspartate aminotransferase (AST) levels. The data are presented as the means ± SDs. P < 0.05 is shown.

Supplementary Table 1. Rectangular DNA origami sheets (rDOSs) and the corresponding staple strands (left to right 5’- 3’).

| Name | DNA Sequence |
| --- | --- |
| 1 | CAAGCCCAATAGGAAC CCATGTACAAACAGTT |
| 2 | AATGCCCCGTAACAGT GCCCGTATCTCCCTCA |
| 3 | TGCCTTGACTGCCTAT TTCGGAACAGGGATAG |
| 4 | GAGCCGCCCCACCACC GGAACCGCGACGGAAA |
| 5 | AACCAGAGACCCTCAG AACCGCCAGGGGTCAG |
| 6 | TTATTCATAGGGAAGG TAAATATT CATTCAGT |
| 7 | CATAACCCGAGGCATA GTAAGAGC TTTTTAAG |
| 8 | ATTGAGGGTAAAGGTG AATTATCAATCACCGG |
| 9 | AAAAGTAATATCTTAC CGAAGCCCTTCCAGAG |
| 10 | GCAATAGCGCAGATAG CCGAACAATTCAACCG |
| 11 | CCTAATTTACGCTAAC GAGCGTCTAATCAATA |
| 12 | TCTTACCAGCCAGTTA CAAAATAAATGAAATA |
| 13 | ATCGGCTGCGAGCATG TAGAAACCTATCATAT |
| 14 | CTAATTTATCTTTCCT TATCATTCATCCTGAA |
| 15 | GCGTTATAGAAAAAGC CTGTTTAG AAGGCCGG |
| 16 | GCTCATTTTCGCATTA AATTTTTG AGCTTAGA |
| 17 | AATTACTACAAATTCT TACCAGTAATCCCATC |
| 18 | TTAAGACGTTGAAAAC ATAGCGATAACAGTAC |
| 19 | TAGAATCCCTGAGAAG AGTCAATAGGAATCAT |
| 20 | CTTTTACACAGATGAA TATACAGTAAACAATT |
| 21 | TTTAACGTTCGGGAGA AACAATAATTTTCCCT |
| 22 | CGACAACTAAGTATTA GACTTTACAATACCGA |
| 23 | GGATTTAGCGTATTAA ATCCTTTGTTTTCAGG |
| 24 | ACGAACCAAAACATCG CCATTAAA TGGTGGTT |
| 25 | GAACGTGGCGAGAAAG GAAGGGAA CAAACTAT |
| 26 | TAGCCCTACCAGCAGA AGATAAAAACATTTGA |
| 27 | CGGCCTTGCTGGTAAT ATCCAGAACGAACTGA |
| 28 | CTCAGAGCCACCACCC TCATTTTCCTATTATT |
| 29 | CTGAAACAGGTAATAA GTTTTAACCCCTCAGA |
| 30 | AGTGTACTTGAAAGTA TTAAGAGGCCGCCACC |
| 31 | GCCACCACTCTTTTCA TAATCAAACCGTCACC |
| 32 | GTTTGCCACCTCAGAG CCGCCACCGATACAGG |
| 33 | GACTTGAGAGACAAAA GGGCGACAAGTTACCA |
| 34 | AGCGCCAACCATTTGG GAATTAGATTATTAGC |
| 35 | GAAGGAAAATAAGAGC AAGAAACAACAGCCAT |
| 36 | GCCCAATACCGAGGAA ACGCAATAGGTTTACC |
| 37 | ATTATTTAACCCAGCT ACAATTTTCAAGAACG |
| 38 | TATTTTGCTCCCAATC CAAATAAGTGAGTTAA |
| 39 | GGTATTAAGAACAAGA AAAATAATTAAAGCCA |
| 40 | TAAGTCCTACCAAGTA CCGCACTCTTAGTTGC |
| 41 | ACGCTCAAAATAAGAA TAAACACCGTGAATTT |
| 42 | AGGCGTTACAGTAGGG CTTAATTGACAATAGA |
| 43 | ATCAAAATCGTCGCTA TTAATTAACGGATTCG |
| 44 | CTGTAAATCATAGGTC TGAGAGACGATAAATA |
| 45 | CCTGATTGAAAGAAAT TGCGTAGACCCGAACG |
| 46 | ACAGAAATCTTTGAAT ACCAAGTTCCTTGCTT |
| 47 | TTATTAATGCCGTCAA TAGATAATCAGAGGTG |
| 48 | AGATTAGATTTAAAAG TTTGAGTACACGTAAA |
| 49 | AGGCGGTCATTAGTCT TTAATGCGCAATATTA |
| 50 | GAATGGCTAGTATTAA CACCGCCTCAACTAAT |
| 51 | CCGCCAGCCATTGCAA CAGGAAAAATATTTTT |
| 52 | CCCTCAGAACCGCCAC CCTCAGAACTGAGACT |
| 53 | CCTCAAGAATACATGG CTTTTGATAGAACCAC |
| 54 | TAAGCGTCGAAGGATT AGGATTAGTACCGCCA |
| 55 | CACCAGAGTTCGGTCA TAGCCCCCGCCAGCAA |
| 56 | TCGGCATTCCGCCGCC AGCATTGACGTTCCAG |
| 57 | AATCACCAAATAGAAA ATTCATATATAACGGA |
| 58 | TCACAATCGTAGCACC ATTACCATCGTTTTCA |
| 59 | ATACCCAAGATAACCC ACAAGAATAAACGATT |
| 60 | ATCAGAGAAAGAACTG GCATGATTTTATTTTG |
| 61 | TTTTGTTTAAGCCTTA AATCAAGAATCGAGAA |
| 62 | AGGTTTTGAACGTCAA AAATGAAAGCGCTAAT |
| 63 | CAAGCAAGACGCGCCT GTTTATCAAGAATCGC |
| 64 | AATGCAGACCGTTTTT ATTTTCATCTTGCGGG |
| 65 | CATATTTAGAAATACC GACCGTGTTACCTTTT |
| 66 | AATGGTTTACAACGCC AACATGTAGTTCAGCT |
| 67 | TAACCTCCATATGTGA GTGAATAAACAAAATC |
| 68 | AAATCAATGGCTTAGG TTGGGTTACTAAATTT |
| 69 | GCGCAGAGATATCAAA ATTATTTGACATTATC |
| 70 | AACCTACCGCGAATTA TTCATTTCCAGTACAT |
| 71 | ATTTTGCGTCTTTAGG AGCACTAAGCAACAGT |
| 72 | CTAAAATAGAACAAAG AAACCACCAGGGTTAG |
| 73 | GCCACGCTATACGTGG CACAGACAACGCTCAT |
| 74 | GCGTAAGAGAGAGCCA GCAGCAAAAAGGTTAT |
| 75 | GGAAATACCTACATTT TGACGCTCACCTGAAA |
| 76 | TATCACCGTACTCAGG AGGTTTAGCGGGGTTT |
| 77 | TGCTCAGTCAGTCTCT GAATTTACCAGGAGGT |
| 78 | GGAAAGCGACCAGGCG GATAAGTGAATAGGTG |
| 79 | TGAGGCAGGCGTCAGA CTGTAGCGTAGCAAGG |
| 80 | TGCCTTTAGTCAGACG ATTGGCCTGCCAGAAT |
| 81 | CCGGAAACACACCACG GAATAAGTAAGACTCC |
| 82 | ACGCAAAGGTCACCAA TGAAACCAATCAAGTT |
| 83 | TTATTACGGTCAGAGG GTAATTGAATAGCAGC |
| 84 | TGAACAAACAGTATGT TAGCAAACTAAAAGAA |
| 85 | CTTTACAGTTAGCGAA CCTCCCGACGTAGGAA |
| 86 | GAGGCGTTAGAGAATA ACATAAAAGAACACCC |
| 87 | TCATTACCCGACAATA AACAACATATTTAGGC |
| 88 | CCAGACGAGCGCCCAA TAGCAAGCAAGAACGC |
| 89 | AGAGGCATAATTTCAT CTTCTGACTATAACTA |
| 90 | TTTTAGTTTTTCGAGC CAGTAATAAATTCTGT |
| 91 | TATGTAAACCTTTTTT AATGGAAAAATTACCT |
| 92 | TTGAATTATGCTGATG CAAATCCACAAATATA |
| 93 | GAGCAAAAACTTCTGA ATAATGGAAGAAGGAG |
| 94 | TGGATTATGAAGATGA TGAAACAAAATTTCAT |
| 95 | CGGAATTATTGAAAGG AATTGAGGTGAAAAAT |
| 96 | ATCAACAGTCATCATA TTCCTGATTGATTGTT |
| 97 | CTAAAGCAAGATAGAA CCCTTCTGAATCGTCT |
| 98 | GCCAACAGTCACCTTG CTGAACCTGTTGGCAA |
| 99 | GAAATGGATTATTTAC ATTGGCAGACATTCTG |
| 100 | TTTT TATAAGTA TAGCCCGGCCGTCGAG |
| 101 | AGGGTTGA TTTT ATAAATCC |
| 102 | ACAAACAA TTTT AATCAGTA GCGACAGATCGATAGC |
| 103 | AGCACCGT TTTT TAAAGGTG GCAACATAGTAGAAAA |
| 104 | TACATACA TTTT GACGGGAG |
| 105 | GCGCATTA TTTT GCTTATCC |
| 106 | TATAGAAG TTTT CGACAAAA GGTAAAGTAGAGAATA |
| 107 | TAAAGTAC TTTT CGCGAGAA AACTTTTTATCGCAAG |
| 108 | ACAAAGAA TTTT ATTAATTA CATTTAACACATCAAG |
| 109 | AAAACAAA TTTT TTCATCAA TATAATCCTATCAGAT |
| 110 | GATGGCAA TTTT AATCAATA TCTGGTCACAAATATC |
| 111 | AAACCCTC TTTT ACCAGTAA TAAAAGGGATTCACCA GTCACACG TTTT |
| 112 | CCGAAATCCGAAAATC CTGTTTGAAGCCGGAA |
| 113 | CCAGCAGGGGCAAAAT CCCTTATAAAGCCGGC |
| 114 | GCATAAAGTTCCACAC AACATACGAAGCGCCA |
| 115 | GCTCACAATGTAAAGC CTGGGGTGGGTTTGCC |
| 116 | TTCGCCATTGCCGGAA ACCAGGCATTAAATCA |
| 117 | GCTTCTGGTCAGGCTG CGCAACTGTGTTATCC |
| 118 | GTTAAAATTTTAACCA ATAGGAACCCGGCACC |
| 119 | AGACAGTCATTCAAAA GGGTGAGAAGCTATAT |
| 120 | AGGTAAAGAAATCACC ATCAATATAATATTTT |
| 121 | TTTCATTTGGTCAATA ACCTGTTTATATCGCG |
| 122 | TCGCAAATGGGGCGCG AGCTGAAATAATGTGT |
| 123 | TTTTAATTGCCCGAAA GACTTCAAAACACTAT |
| 124 | AAGAGGAACGAGCTTC AAAGCGAAGATACATT |
| 125 | GGAATTACTCGTTTAC CAGACGACAAAAGATT |
| 126 | GAATAAGGACGTAACA AAGCTGCTCTAAAACA |
| 127 | CCAAATCACTTGCCCT GACGAGAACGCCAAAA |
| 128 | CTCATCTTGAGGCAAA AGAATACAGTGAATTT |
| 129 | AAACGAAATGACCCCC AGCGATTATTCATTAC |
| 130 | CTTAAACATCAGCTTG CTTTCGAGCGTAACAC |
| 131 | TCGGTTTAGCTTGATA CCGATAGTCCAACCTA |
| 132 | TGAGTTTCGTCACCAG TACAAACTTAATTGTA |
| 133 | CCCCGATTTAGAGCTT GACGGGGAAATCAAAA |
| 134 | GAATAGCCGCAAGCGG TCCACGCTCCTAATGA |
| 135 | GAGTTGCACGAGATAG GGTTGAGTAAGGGAGC |
| 136 | GTGAGCTAGTTTCCTG TGTGAAATTTGGGAAG |
| 137 | TCATAGCTACTCACAT TAATTGCGCCCTGAGA |
| 138 | GGCGATCGCACTCCAG CCAGCTTTGCCATCAA |
| 139 | GAAGATCGGTGCGGGC CTCTTCGCAATCATGG |
| 140 | AAATAATTTTAAATTG TAAACGTTGATATTCA |
| 141 | GCAAATATCGCGTCTG GCCTTCCTGGCCTCAG |
| 142 | ACCGTTCTAAATGCAA TGCCTGAGAGGTGGCA |
| 143 | TATATTTTAGCTGATA AATTAATGTTGTATAA |
| 144 | TCAATTCTTTTAGTTT GACCATTACCAGACCG |
| 145 | CGAGTAGAACTAATAG TAGTAGCAAACCCTCA |
| 146 | GAAGCAAAAAAGCGGA TTGCATCAGATAAAAA |
| 147 | TCAGAAGCCTCCAACA GGTCAGGATCTGCGAA |
| 148 | CCAAAATATAATGCAG ATACATAAACACCAGA |
| 149 | CATTCAACGCGAGAGG CTTTTGCATATTATAG |
| 150 | ACGAGTAGTGACAAGA ACCGGATATACCAAGC |
| 151 | AGTAATCTTAAATTGG GCTTGAGAGAATACCA |
| 152 | GCGAAACATGCCACTA CGAAGGCATGCGCCGA |
| 153 | ATACGTAAAAGTACAA CGGAGATTTCATCAAG |
| 154 | CAATGACACTCCAAAA GGAGCCTTACAACGCC |
| 155 | AAAAAAGGACAACCAT CGCCCACGCGGGTAAA |
| 156 | TGTAGCATTCCACAGA CAGCCCTCATCTCCAA |
| 157 | GTAAAGCACTAAATCG GAACCCTAGTTGTTCC |
| 158 | AGTTTGGAGCCCTTCA CCGCCTGGTTGCGCTC |
| 159 | AGCTGATTACAAGAGT CCACTATTGAGGTGCC |
| 160 | ACTGCCCGCCGAGCTC GAATTCGTTATTACGC |
| 161 | CCCGGGTACTTTCCAG TCGGGAAACGGGCAAC |
| 162 | CAGCTGGCGGACGACG ACAGTATCGTAGCCAG |
| 163 | GTTTGAGGGAAAGGGG GATGTGCTAGAGGATC |
| 164 | CTTTCATCCCCAAAAA CAGGAAGACCGGAGAG |
| 165 | AGAAAAGCAACATTAA ATGTGAGCATCTGCCA |
| 166 | GGTAGCTAGGATAAAA ATTTTTAGTTAACATC |
| 167 | CAACGCAATTTTTGAG AGATCTACTGATAATC |
| 168 | CAATAAATACAGTTGA TTCCCAATTTAGAGAG |
| 169 | TCCATATACATACAGG CAAGGCAACTTTATTT |
| 170 | TACCTTTAAGGTCTTT ACCCTGACAAAGAAGT |
| 171 | CAAAAATCATTGCTCC TTTTGATAAGTTTCAT |
| 172 | TTTGCCAGATCAGTTG AGATTTAGTGGTTTAA |
| 173 | AAAGATTCAGGGGGTA ATAGTAAACCATAAAT |
| 174 | TTTCAACTATAGGCTG GCTGACCTTGTATCAT |
| 175 | CCAGGCGCTTAATCAT TGTGAATTACAGGTAG |
| 176 | CGCCTGATGGAAGTTT CCATTAAACATAACCG |
| 177 | TTTCATGAAAATTGTG TCGAAATCTGTACAGA |
| 178 | ATATATTCTTTTTTCA CGTTGAAAATAGTTAG |
| 179 | AATAATAAGGTCGCTG AGGCTTGCAAAGACTT |
| 180 | CGTAACGATCTAAAGT TTTGTCGTGAATTGCG |
| 181 | ACCCAAATCAAGTTTT TTGGGGTCAAAGAACG |
| 182 | TGGACTCCCTTTTCAC CAGTGAGACCTGTCGT |
| 183 | TGGTTTTTAACGTCAA AGGGCGAAGAACCATC |
| 184 | GCCAGCTGCCTGCAGG TCGACTCTGCAAGGCG |
| 185 | CTTGCATGCATTAATG AATCGGCCCGCCAGGG |
| 186 | ATTAAGTTCGCATCGT AACCGTGCGAGTAACA |
| 187 | TAGATGGGGGGTAACG CCAGGGTTGTGCCAAG |
| 188 | ACCCGTCGTCATATGT ACCCCGGTAAAGGCTA |
| 189 | CATGTCAAGATTCTCC GTGGGAACCGTTGGTG |
| 190 | TCAGGTCACTTTTGCG GGAGAAGCAGAATTAG |
| 191 | CTGTAATATTGCCTGA GAGTCTGGAAAACTAG |
| 192 | CAAAATTAAAGTACGG TGTCTGGAAGAGGTCA |
| 193 | TGCAACTAAGCAATAA AGCCTCAGTTATGACC |
| 194 | TTTTTGCGCAGAAAAC GAGAATGAATGTTTAG |
| 195 | AAACAGTTGATGGCTT AGAGCTTATTTAAATA |
| 196 | ACTGGATAACGGAACA ACATTATTACCTTATG |
| 197 | ACGAACTAGCGTCCAA TACTGCGGAATGCTTT |
| 198 | CGATTTTAGAGGACAG ATGAACGGCGCGACCT |
| 199 | CTTTGAAAAGAACTGG CTCATTATTTAATAAA |
| 200 | GCTCCATGAGAGGCTT TGAGGACTAGGGAGTT |
| 201 | ACGGCTACTTACTTAG CCGGAACGCTGACCAA |
| 202 | AAAGGCCGAAAGGAAC AACTAAAGCTTTCCAG |
| 203 | GAGAATAGCTTTTGCG GGATCGTCGGGTAGCA |
| 204 | ACGTTAGTAAATGAAT TTTCTGTAAGCGGAGT |

Supplementary Table 2. TAMRA-labelled strands (left to right 5’- 3’).

| Name | DNA Sequence |
| --- | --- |
| 6-TAMRA | TTTTTATTCATAGGGAAGG TAAATATT CATTCAGT |
| 7-TAMRA | TTTCATAACCCGAGGCATA GTAAGAGC TTTTTAAG |
| 8-TAMRA | TTTATTGAGGGTAAAGGTG AATTATCAATCACCGG |
| 9-TAMRA | TTTAAAAGTAATATCTTAC CGAAGCCCTTCCAGAG |
| 10-TAMRA | TTTGCAATAGCGCAGATAG CCGAACAATTCAACCG |
| 11-TAMRA | TTTCCTAATTTACGCTAAC GAGCGTCTAATCAATA |
| 12-TAMRA | TTTTCTTACCAGCCAGTTA CAAAATAAATGAAATA |
| 13-TAMRA | TTT ATCGGCTGCGAGCATG TAGAAACCTATCATAT |
| 14-TAMRA | TTTCTAATTTATCTTTCCT TATCATTCATCCTGAA |
| 15-TAMRA | TTTGCGTTATAGAAAAAGC CTGTTTAG AAGGCCGG |
| 16-TAMRA | TTTGCTCATTTTCGCATTA AATTTTTG AGCTTAGA |
| 17-TAMRA | TTTAATTACTACAAATTCT TACCAGTAATCCCATC |
| 18-TAMRA | TTTTTAAGACGTTGAAAAC ATAGCGATAACAGTAC |
| 19-TAMRA | TTTTAGAATCCCTGAGAAG AGTCAATAGGAATCAT |
| 118-TAMRA | TTT GTTAAAATTTTAACCA ATAGGAACCCGGCACC |
| 119-TAMRA | TTTAGACAGTCATTCAAAA GGGTGAGAAGCTATAT |
| 120-TAMRA | TTT AGGTAAAGAAATCACC ATCAATATAATATTTT |
| 121-TAMRA | TTT TTTCATTTGGTCAATA ACCTGTTTATATCGCG |
| 122-TAMRA | TTTTCGCAAATGGGGCGCG AGCTGAAATAATGTGT |
| 123-TAMRA | TTTTTTTAATTGCCCGAAA GACTTCAAAACACTAT |
| 124-TAMRA | TTTAAGAGGAACGAGCTTC AAAGCGAAGATACATT |
| 125-TAMRA | TTT GGAATTACTCGTTTAC CAGACGACAAAAGATT |
| 126-TAMRA | TTT GAATAAGGACGTAACA AAGCTGCTCTAAAACA |
| 127-TAMRA | TTT CCAAATCACTTGCCCT GACGAGAACGCCAAAA |

Supplementary Table 3. Detailed parameters of the theoretical simulations of WES-facilitated drug electrophoresis via COMSOL software.

| Symbol | Value | Definition |
| --- | --- | --- |
| t | 600 s | Duration of the simulation |
| σo | 0.02 S/m | Conductivity of the ocular |
| σe | 1×106 S/m | Conductivity of the electrode |
| D | 1×10-7 m2/s | Diffusion coefficient of the drug |
| Zc | -1 | Charge of the drug |