Supporting materials

Magnetic Magnetite/Epoxy Nanocomposites with Polyaniline as Coupling Agent: Preparation, Characterization and Property

Juanna Ren,a Wenhao Dong,a Ethan Burcarb, Ashley DeMerleb, Zhe Wangb* and Hua Hou,a,*

aSchool of Materials Science and Engineering, Taiyuan University of Science and Technology, Taiyuan, Shanxi, China, 030024

b Chemistry department, Oakland University, Rochester, MI, United States, 48309

Corresponding author:

Hua Hou (Email: houhua@tyus.edu.cn ); Zhe Wang (E-mail: zhewang@oakland.edu)

Preparation of PANI@Fe3O4/epoxy nanocomposites

Firstly, the PANI@Fe3O4 nanoarpticles were immersed in Epon resin overnight without any disturbance to completely wet the nanoparticles. Then the suspension was mechanically stirred for one hour (600 rpm). All the procedures were carried out at room temperature. Secondly, the curing agent EpiCure W was added into the Epon monomers or the above prepared PANI@Fe3O4 nanoparticles Epon resin nanosuspensions with a monomer/curing agent ratio of 100/ 26.5 for one hour mechanical stirring (200 rpm). Then the solution was mechanically stirred at 70 oC for 2–3 h (200 rpm), which was essential to remove the bubbles and to prevent the sedimentation of PANI@Fe3O4 nanoparticles during the curing process. Thirdly, the solutions were poured into the silicone molds and cured at 120 oC for 5 hours. In order to remove the bubbles, the molds were put into the vacuum oven at 120 oC for 1 hour. Finally, the molds were cooled down to room temperature naturally. The PANI@Fe3O4/epoxy nanocomposites with 1, 10, and 30 wt% PANI nanoparticles were synthesized by this method. Note: Since the 30 wt% loading is very high, in order to remove the bubble in the final epoxy nanocomposites, the PANI@Fe3O4 nanoparticles were washed with acetone, then immersed in epon resin overnight. After that, the suspension was put into vacuum oven to remove the acetone at 40 oC. Then the same procedures for the preparation of epoxy composites.

SEM, XRD and FT-IR characterization

The chemical structure of the PANI@Fe3O4 nanoparticles was analyzed by a Fourier transform infrared spectroscopy (FTIR), coupled with an ATR accessory (Bruker Vector 22) in the range of 500–4000 cm1 with a resolution of 4 cm1. The XRD was measured by D/max-rB wide-angle X-ray diffractometer at a Cu Ka wavelength of 0.154 nm. The morphologies of the PANI@Fe3O4 and the fracture surface of the synthesized PANI@Fe3O4/epoxy nanocomposites were examined by a JEOL JSM-IT800 scanning electron microscopy (SEM). All the samples were sputter coated a thin layer of gold to ensure good imaging.

Mechanical property

Tensile tests were carried out following ASTM, D412-98a in a unidirectional tensile test machine (ADMET tensile strength testing system 2610). The parameters (displacement and force) were controlled by a digital controller (MTESTQuattro) with MTESTQuattro Materials Testing Software. The samples (dogbone shaped) were designed according to the ASTM standard requirement and prepared as described for epoxy nanocomposites in the molds. A crosshead speed of 1 mm/min was used and the strain (mm/mm) was calculated by dividing the jogging displacement by the original gauge length. Dynamic mechanical analysis (DMA) was performed in the three-point bending mode by using an DMA Q800 (TA Instruments) with a frequency of 1 Hz and a heating rate of 2 oC/min in the range of 30–250 oC. The sample dimensions were 60 mm×10 mm×4 mm.

Magnetic property

The magnetic properties were investigated by vibrating sample magnetometer (VSM, LakeShore 7404) at room temperature. The magnetic field is from-2T to +2T.

Thermal property

The thermal stability was studied in a thermogravimetric analysis (TG/DTA 8122,Rigaku) with a heating rate of 10 oC min1 under an air flow rate of 120 mL/min from 30 to 800 oC. Differential scanning calorimeter (DSC, Q2000, TA Instruments) measurements were implemented under a nitrogen low rate of approximately 50 mL/min at a heating rate of 10 C min1 from 25 to 300 C. The thermal conductivity was measured by Laser Flash Apparatus (LFA, NETZSCH, LFA467) at room temperature.