Supplementary information

Two-dimensional magnesium phyllosilicate as a recyclable solid base catalyst for Knoevenagel condensation

Hunsoo Park a,b, Sungjoon Kweon c, Eun-Jeong Kim a, Min Bum Park c,*, Jong-Ho Moon b,**, Hyung-Ki Min d,***

a SK biotek, Daejeon 34110, Korea

b Department of Chemical Engineering, Chungbuk National University, Cheongju 28644, Korea

c Department of Energy and Chemical Engineering, Incheon National University, Incheon 22012, Korea

d Hydrogen & C1 Gas Research Center, Korea Research Institute of Chemical Technology, Daejeon 34114, Korea

*mbpark@inu.ac.kr; **moonjongho@chungbuk.ac.kr; ***hkmin@krict.re.kr

Table S1 Binding energies of XPS peaks in Mg 2p, Si 2p, and O 1s regionsa

| Catalyst | Mg 2p |  |  | Si 2p |  |  |  | O 1s |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Peak I (Si–O–Mg) | Peak II (MgO) |  | Peak I (Si–OH) | Peak II (Si–O–Mg) | Peak III (SiO2) |  | Peak I (Mg(OH)2) | Peak II (Si–O) | Peak III (Si–O–Mg) | Peak IV (OH) |
| Mg-DML-100 | 49.9 (0.73) | 50.8 (0.27) |  | 102.7 (0.31) | 103.6 (0.57) | 104.5 (0.12) |  | 531.6 (0.19) | 532.6 (0.64) | 533.5 (0.14) | 534.5 (0.02) |
| Mg-DML-120 | 49.8 (0.87) | 50.3 (0.13) |  | 102.7 (0.31) | 103.6 (0.59) | 104.5 (0.10) |  | 531.6 (0.29) | 532.6 (0.47) | 533.5 (0.20) | 534.5 (0.04) |
| Mg-DML-140 | 49.9 (0.86) | 50.5 (0.14) |  | 102.7 (0.26) | 103.6 (0.64) | 104.5 (0.10) |  | 531.6 (0.29) | 532.6 (0.46) | 533.5 (0.21) | 534.5 (0.04) |
| Mg-DML-160 | 49.8 (0.88) | 50.5 (0.12) |  | 102.7 (0.24) | 103.5 (0.67) | 104.5 (0.09) |  | 531.6 (0.31) | 532.6 (0.45) | 533.5 (0.21) | 534.5 (0.03) |
| Mg-DML-180 | 49.9 (0.28) | 50.8 (0.72) |  | 102.7 (0.26) | 103.5 (0.58) | 104.5 (0.16) |  | 531.6 (0.29) | 532.6 (0.49) | 533.5 (0.18) | 534.5 (0.03) |

aThe values in parentheses represent the area ratio of the deconvoluted peaks.

Fig. S1 Pore size distribution curves of B-MWW and Mg-DML-x (x = 100–180)

Fig. S2 IR spectra in the hydroxyl region of B-MWW and Mg-DML-x (x = 100–180)