Supplementary Information

Interplay of In-O bond activation and stabilization for CO2 hydrogenation to methanol

Fengwang Zhaoa,＃, Ting Zengb,＃, Xiaoli Yanga,*, Qi Wangb, Yang Zhaoc, Jing Zhoud, Xiaofeng Yangc, Chunfu Lina, Haoxi Bena, Nianxue Zhaia, Youzhu Yuane, Xingyun Lia,*, Xiang-Kui Gub,*, Yanqiang Huangc,*, Xiu Song Zhaoa

- aInstitute of Materials for Energy and Environment, State Key Laboratory of BioFibers and Eco-textiles, College of Materials Science and Engineering, Qingdao University, Qingdao 266071, China

- bSchool of Power and Mechanical Engineering, Wuhan University, Wuhan 430000, China

- cState Key Laboratory of Catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China

- dZhejiang Institute of Photoelectronics & Zhejiang Institute for Advanced Light Source, Zhejiang Normal University, Jinhua 321004, China

- eState Key Laboratory of Physical Chemistry of Solid Surfaces, National Engineering Laboratory for Green Chemical Production of Alcohols-Ethers-Esters, Collaborative Innovation Center of Chemistry for Energy Materials (iChEM), College of Chemistry and Chemical Engineering, Xiamen University, Xiamen 361000, China.

Supplementary Figure 1. HAADF-STEM image of 2% Cr-In2O3.

Supplementary Figure 2. SEM and EDS elemental mapping of (a) 1% Cr-In2O3 and (b) 5% Cr-In2O3.

Supplementary Figure 3. (a) N2 adsorption-desorption isotherms and (b) BJH pore size distribution curves of In2O3 and Cr-In2O3 samples with different Cr contents.

Supplementary Figure 4. XRD patterns for the 1% Cr-In2O3, 5% Cr-In2O3 and In2O3.

Supplementary Figure 5. Cr K-edge EXAFS spectra in K space for Cr-doped samples.

Supplementary Figure 6. Comparison of Cr K edge EXAFS spectral data and fitting data of (a) 2% Cr- In2O3, (b) Cr2O3, (c) Cr foil in K space and R space, respectively.

Supplementary Figure 7. Catalytic performance of 5% Cr-In2O3, P = 5 MPa, CO2/H2 = 1/3, and WHSV = 3000 mL·gcat-1·h-1.

Supplementary Figure 8. H2-TPR profiles of In2O3 and Cr-In2O3 samples.

Supplementary Figure 9. The Electron Localization Function (ELF) contours and bader charge analysis for oxygen atoms in region I of Initial-In2O3 (111) (a) and Initial-Cr-In2O3 (111) (b). The number in the color bar represents the degree of electron localization in atomic units (a.u.).

Note: After Cr doping, the green area in the circle becomes more delocalized, specifically, around the In atom for Initial-In2O3 (111) and the Cr atom for Initial-Cr-In2O3 (111). This delocalization corresponds to a decrease in the charge of these oxygen atoms.

Supplementary Figure 10. The Crystal Orbital Hamilton population (COHP) and the Integrated values (-ICOHP) of the O-In bond for Initial-In2O3 (111) (a), and O-Cr bond for Initial-Cr-In2O3 (111) (b) in region I, respectively. Considering that the three oxygen atoms in region I are equivalent, for simplicity in explanation, we selected only one of the oxygen atoms as a representative, indicated by the triangles in local structures for the COHP analysis.

Supplementary Figure 11. The COHP analysis and -ICOHP of O-In bond for (a) Initial-In2O3 (111), and O-Cr bond for (b) Initial-Cr-In2O3 (111) in region II, respectively. Considering that the three oxygen atoms in region II are equivalent, for simplicity in explanation, we selected only one of the oxygen atoms as a representative, indicated by the triangles in local structures for the COHP analysis.

Supplementary Figure 12. The ELF contours and bader charge analysis for oxygen atoms in region II for (a) Initial-In2O3 (111) and (b) Initial-Cr-In2O3 (111), respectively. The number beside the color bar represents the degree of electron localization in atomic units (a.u.).

Note: As shown by contours in region II, after Cr doping, the electron localization degree of In atoms was enhanced and the electron density of the In-O-In pair was also increased, which shows stronger electron donating capability of In atoms during the bonding process with oxygen atoms. This is consistent with the conclusion of the COHP analysis in Supplementary Figure 11 that the In-O-In bonds are strengthened.

Supplementary Figure 13. CO2-TPD profiles of In2O3 and Cr-In2O3 samples.

Supplementary Figure 14. TEM image of In2O3 after 300 h stability test.

Supplementary Figure 15. The crystallinity of the sample calculated by the XRD Rietveld method.

Supplementary Figure 16. TEM image of (a) fresh 2% Cr-In2O3, (b) 2% Cr-In2O3 after 500 h stability test.

Supplementary Figure 17. HRTEM image of (a) fresh 2% Cr-In2O3, (b) 2% Cr-In2O3 after 500 h stability test.

Supplementary Figure 18. In 3d XPS spectra of the fresh 2% Cr-In2O3, In2O3 and catalysts after stability test.

Supplementary Figure 19. O 1s XPS spectra of the fresh 2% Cr-In2O3, In2O3 and catalysts after stability test.

Supplementary Figure 20. TG of fresh and stability-tested 2% Cr-In2O3 and In2O3.

Supplementary Figure 21. Optimized transient states of the elementary steps involved in CO2 hydrogenation to methanol on Cr-In2O3 (111) and In2O3 (111) surface. Chromium (green), Oxygen (red and pink), Indium (blue), Carbon (black) and Hydrogen (white).

Supplementary Figure 22. Optimized intermediate structures involved in CO2 hydrogenation to methanol on Cr-In2O3 (111) surface. Chromium (green), Oxygen (red and pink), Indium (blue), Carbon (black) and Hydrogen (white).

Supplementary Figure 23. Optimized intermediates structures involved in CO2 hydrogenation to methanol on In2O3 (111) surface. Oxygen (red and pink), Indium (blue), Carbon (black) and Hydrogen (white).

Supplementary Figure 24. Free energy diagram of the hydrogenation of CO2 to methanol on In2O3 (111) at 523 K and 5 MPa.

Supplementary Table 1. Cr content, specific surface area and total pore volume of Cr-In2O3 samples

| Catalysts | Cr content (wt.%)a | SBET (m2·g-1)b | Vpore (10-2 cm3·g-1)c |
| --- | --- | --- | --- |
| 1% Cr-In2O3 | 1.23 | 69.9 | 22.6 |
| 2% Cr-In2O3 | 2.04 | 56.2 | 25.2 |
| 5% Cr-In2O3 | 4.76 | 65.9 | 29.2 |
| In2O3 | - | 10.1 | 4.42 |

aCr content determined by ICP-AES.

bSpecific surface area calculated by the BET method.

cTotal pore volume determined at P/P0 = 0.99.

Supplementary Table 2. EXAFS fitting parameters at the Cr K-edge for various samples. (Ѕ02=0.724)

| Sample | Shell | CNa | R (Å)b | σ2 (Å2)c | ΔE0 (eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Cr foil | Cr-Cr | 8* | 2.495±0.007 | 0.0055±0.0009 | 5.2±1.2 | 0.0020 |
|  | Cr-Cr | 6* | 2.876±0.006 | 0.0048±0.0012 |  |  |
| Cr2O3 | Cr-O | 6.0±0.7 | 1.995±0.009 | 0.0049±0.0010 | 3.4±1.7 | 0.0191 |
|  | Cr-O-Cr | 4.1±0.4 | 2.897±0.012 | 0.0116±0.0010 | -2.6±3.1 |  |
|  | Cr-O-Cr | 3.2±0.3 | 3.472±0.034 |  | 1.0±2.3 |  |
| 2% Cr-In2O3 | Cr-O | 3.7±0.3 | 1.983±0.004 | 0.0018±0.0008 | 2.1±0.9 | 0.0067 |
|  | Cr-O-In | 5.9±0.4 | 3.603±0.011 | 0.0071±0.0021 | -10.1±1.4 |  |

aCN: coordination number.

bR: the distance to the neighboring atom.

cσ2: the Mean Square Relative Displacement (MSRD).

dΔE0: inner potential correction, R factor indicates the goodness of the fit. S02 was fixed to 0.724, according to the experimental EXAFS fit of Cr foil by fixing CN as the known crystallographic value.

*This value was fixed during EXAFS fitting, based on the known structure of Cr. Fitting range: 3.0 ≤ k (Å) ≤ 12.5 and 1.0 ≤ R (Å) ≤ 3.0 (Cr foil), 2.0 ≤ k (Å) ≤ 10.5 and 1.0 ≤ R (Å) ≤ 4.0 (2% Cr-In2O3). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02< 1.000, CN > 0; σ2 > 0 Å2, |ΔE0| < 10 eV, R factor < 0.02.

| Catalysts | P [MPa] | T [℃] | WHSV [mL·gcat-1·h-1] | XCO2a [%] | SMeOHb [%] | H2/CO2 | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ZnZrOx | 5 | 250 | 24000 | 0.8 | 88.2 | 4 | 1 |
| NiO-In2O3 | 3 | 250 | 60000 | 2.8 | 53.1 | 3 | 2 |
| Ni/In2O3 | 5 | 250 | 21000 | 5.4 | 85.0 | 4 | 3 |
| Ni/In2O3 | 5 | 280 | 24000 | 8.1 | 71.9 | 4 | 4 |
| Ir-In2O3 | 5 | 250 | 21000 | 6.2 | 89.3 | 4 | 5 |
| In2O3 | 5 | 250 | 21000 | 2.2 | 83.6 | 4 | 5 |
| Au-In2O3 | 5 | 250 | 21000 | 3.9 | 83.8 | 4 | 6 |
| Ag-In2O3 | 5 | 250 | 21000 | 2.9 | 73.9 | 4 | 7 |
| Pt-In2O3 | 5 | 250 | 21000 | 6.8 | 83.0 | 4 | 8 |
| In2O3/m-ZrO2 | 5 | 280 | 24000 | 4.8 | 84 | 4 | 9 |
| In2O3/t-ZrO2 | 5 | 280 | 24000 | 0.5 | 83 | 4 | 9 |
| Cu/m-ZrO2 | 5 | 250 | 7200 | 3.5 | 50 | 4 | 10 |
| ZnO-ZrO2 | 5 | 250 | 24000 | 1.6 | 98.22 | 4 | 11 |
| CuO/ZnO | 5 | 250 | - | 11.7 | 36.1 | 3 | 12 |
| Co3O4-In2O3 | 5 | 250 | 7500 | 6.2 | 92 | 3 | 13 |
| Co3O4-In2O3 | 5 | 250 | 7500 | 4.2 | 90 | 3 | 13 |
| Pd0.1Zn1/CNTs | 5 | 250 | 1800 | 6.22 | 95.2 | 3 | 14 |
| PdZn/ZnO/SiO2 | 5 | 260 | 30000 | 3.6 | 49.8 | 3 | 15 |
| 2Pd-ZnO | 5 | 260 | 120000 | 2.8 | 66.5 | 3 | 15 |
| N-In2O3 | 5 | 250 | 21000 | 1.1 | 80.6 | 4 | 16 |
| Cr-In2O3 | 5 | 250 | 3000 | 9.4 | 92 | 3 | This work |
| In2O3 | 5 | 250 | 3000 | 2.2 | 56 | 3 | This work |

Supplementary Table 3. Comparison of catalytic performance.

aXCO2: CO2 conversion.

bSMeOH: methanol selectivity.

Supplementary Table 4. Structural information obtained from XRD Rietveld refinement of the fresh and used samples.

| Samples | 2% Cr-In2O3 | 2% Cr-In2O3 500 | In2O3 | In2O3 300 |
| --- | --- | --- | --- | --- |
| Space group | I a -3 | I a -3 | I a -3 | I a -3 |
| a(=b=c) (Å) | 10.08 (192) | 10.06 (214) | 10.08 (192) | 10.12 (162) |
| α(=β=γ) (°) | 90 | 90 | 90 | 90 |
| Rwp | 4.59% | 5.42% | 7.17% | 4.05% |
| Rp | 3.37% | 3.38% | 4.97% | 2.77% |
| V(Å3) | 1028.33(5) | 1018.82(6) | 1026.44(5) | 1037.16(2) |
| Microstrain (%) | 0.238 | 0.221 | -0.097 | -0.027 |

Supplementary Table 5. The catalytic performance of CO hydrogenation for samples with different Cr contents.

| Catalysts | Products | Conv. CO (%)a |
| --- | --- | --- |
| 1% Cr-In2O3 | CO2, CH4 | 0.65 |
| 2% Cr-In2O3 | CO2, CH4 | 0.52 |
| 5% Cr-In2O3 | CO2, CH4 | 0.76 |
| In2O3 | CO2, CH4 | 0.99 |

aConv.CO represents the conversion of CO.

Reaction conditions: CO/H2=1/1, T=250 oC, P = 5 MPa, WHSV = 3000 mL·gcat-1·h-1.

Supplementary Table 6. The coordinated-oxygen vacancy formation energy (eV) on experimentally observed surfaces.

| In2O3 facets | Without Cr doping | With Cr doping |
| --- | --- | --- |
| (111) | 2.17 | 2.03 (↓) |
| (211) | 2.10 | 2.34 (↑) |
| (100) | 3.20 | 3.79 (↑) |

References

1	Lee, K. Y. H. et al. Atomic Pd-promoted ZnZrOx solid solution catalyst for CO2 hydrogenation to methanol. Applied Catalysis B: Environmental 304, 12 (2022).

2	Zhu, J. D. et al. Ni-In Synergy in CO2 Hydrogenation to Methanol. ACS Catalysis 11, 11371-11384 (2021).

3	Jia, X. Y., Sun, K. H., Wang, J., Shen, C. Y. & Liu, C. J. Selective hydrogenation of CO2 to methanol over Ni/In2O3 catalyst. Journal of Energy Chemistry 50, 409-415 (2020).

4	Frei, M. S. et al. Nanostructure of nickel-promoted indium oxide catalysts drives selectivity in CO2 hydrogenation. Nature Communications 12, 9 (2021).

5	Shen, C. Y. et al. Highly Active Ir/In2O3 Catalysts for Selective Hydrogenation of CO2 to Methanol: Experimental and Theoretical Studiese. ACS Catalysis 11, 4036-4046 (2021).

6	Rui, N. et al. Hydrogenation of CO2 to Methanol on a Auδ+-In2O3-x Catalyst. ACS Catalysis 10, 11307-11317 (2020).

7	Sun, K. H., Zhang, Z. T., Shen, C. Y., Rui, N. & Liu, C. J. The feasibility study of the indium oxide supported silver catalyst for selective hydrogenation of CO2 to methanol. Green Energy Environ. 7, 807-817 (2022).

8	Sun, K. et al. A highly active Pt/In2O3 catalyst for CO2 hydrogenation to methanol with enhanced stability. Green Chemistry 22, 5059-5066 (2020).

9	Frei, M. S. et al. Role of Zirconia in Indium Oxide-Catalyzed CO2 Hydrogenation to Methanol. ACS Catalysis 10, 1133-1145 (2020).

10	Witoon, T., Chalorngtham, J., Dumrongbunditkul, P., Chareonpanich, M. & Limtrakul, J. CO2 hydrogenation to methanol over Cu/ZrO2 catalysts: Effects of zirconia phases. ‌Chemical Engineering Journal 293, 327-336 (2016).

11	Wang, J. J. et al. A highly selective and stable ZnO-ZrO2 solid solution catalyst for CO2 hydrogenation to methanol. Science Advances 3, 10 (2017).

12	Fujitani, T. et al. Development of an active Ga2O3 supported palladium catalyst for the synthesis of methanol from carbon dioxide and hydrogen. Applied Catalysis A: General 125, 199-202 (1995).

13	Zhang, H., Mao, D. L., Zhang, J. X. & Wu, D. F. Regulating the crystal structure of layered double hydroxide-derived Co-In catalysts for highly selective CO2 hydrogenation to methanol. ‌Chemical Engineering Journal 452, 11 (2023).

14	Liang, X. L., Xie, J. R. & Liu, Z. M. A Novel Pd-decorated Carbon Nanotubes-promoted Pd-ZnO Catalyst for CO2 Hydrogenation to Methanol. Catalysis Letters 145, 1138-1147 (2015).

15	Zabilskiy, M. et al. Mechanistic Study of Carbon Dioxide Hydrogenation over Pd/ZnO-Based Catalysts: The Role of Palladium-Zinc Alloy in Selective Methanol Synthesis. Angewandte Chemie International Edition 60, 17053-17059 (2021).

16	Yang, Y., Shen, C., Sun, K., Mei, D. & Liu, C.-j. Enhanced Surface Charge Localization Over Nitrogen-Doped In2O3 for CO2 Hydrogenation to Methanol with Improved Stability. ACS Catalysis 13, 6154-6168 (2023).

＃These authors contribute equally to this manuscript.

*Corresponding authors: xlyang@qdu.edu.cn (X. Yang), xingyun_2008@sina.cn (X. Li), xiangkuigu@whu.edu.cn (X. Gu), yqhuang@dicp.ac.cn (Y. Huang)