Carob Plant Extract as Naturally Products Corrosion Inhibitor for Copper-Nickel Alloys in Brine Solutions

Abd El Aziz S. Fouda1*, Mona Nageeb2, Mohamed F. Atia3, Ghalia A. Gaber2*, Amal S. I. Ahmed2, Ahmed A El-Hossiany1,4

1Chemistry Department, Faculty of Science, Mansoura University, Mansoura -35516, Egypt

Email: asfouda@mans.edu.eg

2Department of Chemistry, Faculty of Science (Girls), Al-Azhar University, P.O. Box: 11754, Yousef Abbas Str., Nasr City, Cairo, Egypt

3Institute of Aviation Engineering and Technology, Cairo, Egypt.

4 Delta for Fertilizers and Chemical Industries, Talkha, Egypt.

Fig. S1. Temkin isotherm plot for the corrosion of Cu-Ni alloys in 3.5 % NaCl solution in the absence and presence of different doses of Carob at 25oC

Fig. S2.  Freundlich isotherm plot for the corrosion of Cu-Ni alloys in 3.5 % NaCl solution in the absence and presence of different doses of Carob at 25oC

Temkin adsorption isotherm

The surface coverage (θ) is connected to the inhibitor dose (C) and the adsorption equilibrium constant Kads as shown in Eq. 1 [37].

Exp (−2a θ) = Kads × C                       (1)

where a is the attractive parameter and K is the adsorption equilibrium constant. From Fig. S1 linear plots are obtained, which affirms that the adsorption obeys the Temkin adsorption isotherm. Adsorption parameters obtained from this Figure are shown in Table S1.

Freundlich adsorption isotherm

According to the Freundlich isotherm, θ is related to the inhibitor dose C by Eq. 2 [38].

log θ = log Kads + nlog C                         (2)

where n is the empirical constant, and the other constants have the same meaning. Fig. S2 shows straight lines relation of log θ against log C with slope n and intercept log Kads. The deduced adsorption parameters Kads, n, and ΔG0ads are shown in Table S1. The obtained values of the correlation factor are far from unity. The adsorption process was studied using Langmuir, Freundlich, and Temkin isotherms. The adsorption studies clearly indicated that the experimental data satisfied the Langmuir Freundlich, and Temkin adsorption isotherms with good linearity. The chosen criteria of the best-fit isotherm are based on the higher correlation coefficient. The higher value of Kads indicates that the inhibitor is strongly adsorbed on the Cu-Ni surface.

Table S1. Values of parameters of Langmuir adsorption isotherm for two Cu-Ni alloys with the addition of Carob in 3.5 % NaCl solution

| Isotherm | Corros Tech. | Cu-10Ni |  |  |  | Cu-30Ni |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | slope | Kads | R2 | -∆Goads | slope | Kads | R2 | -∆Goads |
| ##### Langmuir | WL | 9.209x10-4 | 21.997 | 0.9953 | 17.608 | 9.754x10-4 | 10.871 | 0.9221 | 15.86 |
|  | PDP | 1.432x10-3 | 30.713 | 0.9999 | 18.436 | 1.032x10-3 | 15.305 | 0.9986 | 16.71 |
|  | EIS | 8.240x10-4 | 13.323 | 0.9746 | 16.366 | 8.696x10-4 | 14.932 | 0.9843 | 16.65 |
| Temkin | WL | 0.488 | 0.267 | 0.9684 | 6.680 | 0.470 | 0.069 | 0.8437 | 3.33 |
|  | PDP | 0.212 | 0.207 | 0.9881 | 6.046 | 0.065 | 1.083 | 0.6943 | 10.15 |
|  | EIS | 0.684 | 0.033 | 0.9412 | 1.445 | 0.603 | 0.029 | 0.9506 | 1.15 |
| Freundlich | WL | 0.286 | 0.138 | 0.9729 | 19.003 | 0.337 | 0.207 | 0.8871 | 6.05 |