Supplementary Material for

Polarization vortices of thermal emission

Ye Zhang1,5, Qiang Wang1,5✉, Meng Xiao2,3✉, Tao Liu2, Fan Zhong4, Zhenxin Lai1, Shining Zhu1, Hui Liu1✉

1 National Laboratory of Solid State Microstructures, School of Physics, Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing 210093, China.

2 School of Physics and Technology, and Key Laboratory of Artificial Micro- and Nano-structures of Ministry of Education, Wuhan University, Wuhan 430072, China.

3 Wuhan Institute of Quantum Technology, Wuhan 430206, China.

4 School of Physics, Southeast University, Nanjing 211189, China.

5 These authors contributed equally: Ye Zhang, Qiang Wang.

This PDF file includes:

I. 	Details about unpolarized thermal emission spectra and a zoom-in

II.	The link between emission angles and the momentum

III.	Extracted Q factors along the Γ-X line

IV.	Details about polarized thermal emission spectra

V.	Extraction of the emitted linear polarization

VI.	Details about the accidental BIC

VII.	Supplemental figures

Figs. S1 to S7

References

Section I.	Details about unpolarized thermal emission spectra and a zoom-in

Details of unpolarized thermal emission spectra are plotted in Fig. S2. In Fig. S2a, b, detailed spectral lines are plotted across various angles, ranging from 0° to 40° along the Γ-X and Γ-M directions. In Fig. S2b, the resonance frequencies of BICs are highlighted with dashed lines at θ = 0°, corresponding to the Γ point. Arrows denote the modes of the first and fourth bands, evidently illustrating their attenuation and shift when approaching BICs. Moreover, the experimental emission intensities of each band are extracted from the polarized spectra in Fig. 3a, b, and the emission peak intensity of total emission (sum of both polarizations) is shown in Fig. S2c. It is clear that the lowest emission signal for the 1st and 4th bands is reached at the zone center, which is the positions of the BICs. On the other hand, the emission peaks are the corresponding highest for the 2nd and 3rd bands. In addition, we also show a zoom in view of the thermal emission spectra in Fig. 2c with a different color bar in Fig. S2d.

Notably, the emission intensity from the fourth band is relatively subdued compared to that from other bands. The emission rate of this PCS is determined by two dominant factors: the absorption/emission coefficient of the material (Ge in our case) and the inner product of the eigenmodes and the radiative modes in the free space. The first factor does not change much for the four bands, and hence the second factor largely determines the emission strength. The 2nd and 3rd bands are radiative modes at the Γ point, hence we only compare the 1st and 4th bands where the modes are BICs at the zone center. As depicted in Fig. S1a, b, the modes of the 1st and 4th bands exhibit different representations of the symmetry group. At the zone center, the mode of the 1st band maintains C4 = -1, while the mode of the 4th band exhibits C4 = 1. C4 = 1 leads to a faster variation of the field in the azimuthal direction, resulting in a relatively smaller inner product. In Fig. S2e, we plot the inner products for the four bands along M-Γ-X. It is evident that the radiation coefficient of the 4th band is much smaller compared with other modes, which further subdues the emission compared to the other bands.

Section II.	The link between emission angles and the momentum

At the start of the configuration, the lattice vectors of the sample aligned with the x-axis and y-axis. The angle φ, rotated around the z-axis in the x-y plane, was adjusted using the manual rotator with a step of 5° from 0° to 90°. Another angle, θ, rotated around the y-axis in the x-z plane, was controlled by the motorized rotator with a step of 1° from 0° to 40°. These two emission angles are connected to the momentum space in the formulation

kx=k∥⋅cosφky=k∥⋅sinφ ,               	    (1)

where k∥=ω0∙sinθc represents the projection of momentum onto the x-y plane, as illustrated in Fig. S3.

Section III.	Extracted Q factors along the Γ-X line

In our study, we favor BIC for its topological nature of polarization vortex to achieve a polarized vortex thermal emitter for the first time, as shown in BOX. 1. The PCS hosts perfect BICs and guided resonance modes surrounding the BICs are excited to provide all linearly polarized thermal emissions. The emission spectra from our system do not exhibit very high Q factors due to intrinsic material losses and the off-centering of k vectors away from the Γ point (where the Q factor decreases rapidly). In Fig. S4, the emissivity and the fitted Q factor of the 1st band are plotted as the emission angle approaching normal. It is clear that as the Q factor increases at smaller emission angles θ, the emission power actually decreases. Therefore, further increasing the Q factor would reduce the emissivity in this work, which does not align with our goal of realizing a thermal emitter with high thermal flux.

|  | BIC in Optics |  |
| --- | --- | --- |
| Application fields | High-Q factor | Polarization Vortex mode |
| Nonlinear Optics and Laser | 1-6 | 7-10 |
| Thermal emissions | Much higher Q will reduce thermal emission efficiency | Reported by this work |

BOX. 1. Different characteristics of BICs for applications in optics.

Section IV.	Details about polarized thermal emission spectra

The thermal emission spectra obtained for different orientations of the linear polarizer (α = 0° & α = 90° and α = 45° & α = 135°), combined with varying emission angles (φ = 0° and φ = 45°), are compared with absorption spectra simulated using the Finite-Difference Time-Domain (FDTD) method (Fig. S5). The dispersions simulated by COMSOL are represented with dashed lines, revealing concordance with both the emission and absorption spectra. Notably, the polarization vectors for the bands of interest are clearly identified along the Γ-X and Γ-M directions. Along the Γ-X line, the first and fourth bands exhibit horizontal polarization vectors, while along the Γ-M line, the polarization vectors of the first band adopt an anti-diagonal orientation, whereas those of the fourth band assume a diagonal alignment.

Section V.	Extraction of the emitted linear polarization

Given that the intensity of thermal emission is a scalar value, we inferred the direction of the electric field by utilizing the measured intensity of thermal emission (I), emission angle (φ) and the polarization orientation (α), expressed as

Ei=±Ii∙cos(φ+αi)∙ex+sin(φ+αi)∙ey.	(2)

Here, i indicates the index of angle α = [0°,45°,90°,135°], and ex, ey are the basic vectors in the kx-ky plane. Thus, for the orthogonal set with α = 0° and α = 90°, the possible synthesized polarization vectors can be described as

S1A=E1+E3S1B=E1-E3.	(3)

Similarly, the possible composite vectors for α = 45° and α = 135° are

S2A=E2+E4S2B=E2-E4.	(4)

For a specific polarization, one identical vector can be obtained by the two orthogonal sets. Comparing the four composite vectors, we chose the two with the smallest difference, considering them to be the closest to the actual values—such as S1B in Fig. S6a and S2A in Fig. S6b. The representation of the polarization state of thermal emission was determined by the average vector of S1B and S2A, and the difference between them was defined as the error bar in experiments.

Section VI.	Details about the accidental BIC

The BIC-3 at kx=0.17 in the third band undergoes tuning from a single resonance11 as the number of radiation channels is reduced. The electric field distribution maintains C2 symmetry12 as shown in Fig. S7a. As a “topologically protected” BIC, it exhibits robustness to geometric parameters, including lattice spacing and the thickness of the photonic crystal. The parameters chosen for confirmatory experiments are indicated with stars in Fig. S7b. The measured thermal emission spectra provide brief confirmation of the robustness, with BIC-3 showing a slight shift in the Γ-X line (see in Fig. S7c, d).

Section VII.	Supplemental figures

FIG. S1 | Electric field patterns of symmetry-protected BICs. a, b Electric field profiles depicting the eigenmodes of BIC-1 and BIC-2. The color maps represent the Ez profile, and the white arrows indicate the direction of the in-plane electric field components (Ex and Ey).

FIG. S2 | Details of unpolarized thermal emission. a, b Measured unpolarized thermal emission spectra and spectral lines of interest, denoted by dashed lines in measured spectra. The blue and green arrows highlight the shift of emission peaks for the first and fourth bands, respectively. The resonance frequencies of BIC-1 and BIC-2 are indicated by the longitudinal lines. c Extracted emission intensities of each band along M-Γ-X directions. d A zoom-in of Fig.2c with a different color bar. e The simulated inner product of the eigenmodes of four bands with the modes in free space along M-Γ-X directions. In simulation, this can be obtained from the |E|2 of the far field domain in COMSOL.

FIG. S3 | Schematics of radiation field decomposition for resonances of a PCS. a The wave vector is projected onto the x-y plane, corresponding to θ and φ. The spatially averaged Bloch part of the electric field E is then projected onto the x-y plane, resulting in the polarization vector (Ex,Ey).

Fig. S4 | The measured emissivity at different emission angles. a The measured emissivity at different θ and the related Q factor of the 1st band are labelled.

FIG. S5 | Details of measured thermal emission spectra and simulated absorption spectra. a, b Measured thermal emission spectra and simulated absorption spectra for varying α (α=0° & α=90°, α=45° & α=135°) with diverse φ (φ=0° and φ=45°). Dashed lines indicate the simulated dispersions of the guided resonance modes.

FIG. S6 | Schematic diagrams of extracting polarization vectors from experimental data. a, b Schematic diagrams of synthetic polarization vectors with α=0° & α=90° and α=45° & α=135°. The blue arrows indicate the in-plane wave vector k∥, parallel to the horizontal line at the emission angle φ. The orange arrows indicate the electric field vectors, with the amplitude derived from the measured emission intensity and the direction determined by the angles α and φ. The green arrows indicate the polarization vectors, synthesized from the electric field vectors of the same or opposite direction.

FIG. S7 | Electric field pattern of BIC-3 and its robustness to structural parameters. a The electric field profile of the eigenmode of BIC-3. The color map represents the Ez profile, and the white arrows indicate the direction of the in-plane electric field components (Ex and Ey). b The robust existence of BIC-3 under different thickness of Ge. c, d The measured thermal emission spectra for hGe = 1.3 μm and hGe = 1.6 μm when α = 0°, featuring BIC-3 at kx = 0.17 and kx = 0.18 as indicated by the purple arrows.

References

1.	Kodigala, A., et al. Lasing action from photonic bound states in continuum. Nature 541, 196-199 (2017).

2.	Jin, J., et al. Topologically enabled ultrahigh-Q guided resonances robust to out-of-plane scattering. Nature 574, 501-504 (2019).

3.	Liu, Z., et al. High-Q Quasibound States in the Continuum for Nonlinear Metasurfaces. Phys. Rev. Lett. 123, 253901 (2019).

4.	Hwang, M.-S., et al. Ultralow-threshold laser using super-bound states in the continuum. Nat. Commun. 12, 4135 (2021).

5.	Zhang, X., Liu, Y., Han, J., Kivshar, Y., Song, Q. Chiral emission from resonant metasurfaces. Science 377, 1215-1218 (2022).

6.	Chen, Y., et al. Observation of intrinsic chiral bound states in the continuum. Nature 613, 474-478 (2023).

7.	Huang, C., et al. Ultrafast control of vortex microlasers. Science 367, 1018-1021 (2020).

8.	Wang, B., et al. Generating optical vortex beams by momentum-space polarization vortices centred at bound states in the continuum. Nat. Photonics 14, 623-628 (2020).

9.	Han, S., et al. Electrically-pumped compact topological bulk lasers driven by band-inverted bound states in the continuum. Light Sci. Appl. 12, 145 (2023).

10.	Zhai, Z., et al. Multimode Vortex Lasing from Dye–TiO2 Lattices via Bound States in the Continuum. ACS Photonics 10, 437-446 (2023).

11.	Hsu, C. W., Zhen, B., Stone, A. D., Joannopoulos, J. D., Soljačić, M. Bound states in the continuum. Nat. Rev. Mater. 1, 1-13 (2016).

12.	Sakoda, K. Optical Properties of Photonic Crystals, 2nd edn, vol. 2.(Springer, 2005).