Supplementary materials

Efficient removal of Perfluorooctane sulfonate (PFOS) from aquatic environment using carbon black/chitosan beads composite

Zeynab Salimi Torkmani (a.salimi77@ut.ac.ir ), Wooriya Tarokh (wooriya.tarokh@ut.ac.ir ), Majid Baghdadi* (m.baghdadi@ut.ac.ir)

Department of Environmental Engineering, Graduate Faculty of Environment, University of Tehran, Tehran, Iran

Corresponding Author: Majid Baghdadi (ORCID 0000-0001-9816-764X)

Email: m.baghdadi@ut.ac.ir; P.O.Box: 1417853111; Phone: +98 21 61112778;

Fax:  +98 21 66407719

Tables S1

Figure S1-S2-S3

| Table S1 |  |  |  |
| --- | --- | --- | --- |
| Thermodynamic variables of PFOS adsorption |  |  |  |
| T (k) | ΔG (J mol-1) | ΔH (J mol-1) | ΔS (J mol-1) |
| 278 | -632.5182074 | 14741.94 | 55.287261 |
| 283 | -922.3539484 |  |  |
| 303 | -1931.143183 |  |  |
| 313 | -2620.471598 |  |  |

Fig. S1. The effect of temperature (CBCHB dosage: 3g, PFOS concentration 5 mg L-1, pH: 2, contact time: 15 min)

Fig. S2a, b. comparison between different isotherm models with experimental data in pH=2 and 6, respectively.

Fig. S2. Comparison of different kinetic models with experimental data

Fig. S3. Regeneration performance of CBCHB in PFOS removal