Preparation of a novel cellulose/4- (ω (methyimidazole) alkyloxy) -4'- cyano azobenzene liquid crystal solution and its fiber

Jun Song1,2* · Chuanmeng Li1 · Mengdie Wang1 · Jicheng Shan1 · LinFeng Wang2 · Xuerong Wang1 · Haijing Zhu1 · Bin Li1 · Chunzu Cheng3 · Ting Li3

1, Key Laboratory of Tianjin City Advanced Fiber and Energy Storage, School of Materials Science and Engineering, TianGong University, Tianjin 300387, China

2, School of Textile Science and Engineering, Tiangong University, Tianjin 300387, China

3, State Key Laboratory of Biobased Fiber Manufacturing Technology, China Textile Academy, Beijing 100025, China

*Corresponding author: Dr. Jun Song, E-mail: sjhb2000@163.com

Figure S1 Chemical reaction pathway diagram of CAB

Figure S2 a, b, and c represent the total ion chromatograms (TICs) of gas chromatography-mass spectrometry (GC-MS) for cyanoazobenzenol, the liquid crystal intermediate, and 1,6-liquid crystal, respectively. Figures d, e, and f correspond to the GC-MS spectra of cyanoazobenzenol, the liquid crystal intermediate, and 1,6-liquid crystal, respectively.

Figure S3 POMs of 3wt% CaB/AMIMCl solution at 30-80 ℃

Figure S4 POMs of 6wt% cellulose/AMIMCl solution at 30-80 ℃

Figure S5 POMs of 6wt%/cellulose/1wt% CaB/AMIMCl solution at 30-80 ℃

Figure S6 POMs of 6wt% cellulose/2wt% CaB/AMIMCl solution 30-80 ℃

Table S1 Physical properties of different cellulose regenerated fibres

| Solvent | Cellulose content (wt%) | Breaking strength (cN/dtex) | Elongation (%) | Refs. |
| --- | --- | --- | --- | --- |
| NMMO | 13.5 | 4.3 | 11 | Hauru et al. (2014) |
| Liquid ionic-CaB | 6 | 3.16 | 7.28 | Our work |
| Liquid ionic | ≤13.2 | 4.4-5.3 | 11-15 | Kosan et al. (2008) |
| LiCl/DMAc | 7 | 2.95 | 6 | Hong et al. (1998) |
| Cuprammonium | 8 | 2.5 | 13 | Sayyed et al. (2019) |
| Viscose | 20 | 2.2 | 17 | Zhang et al. (2018) |