2. Materials and methods

2.12. Antioxidant activities

2.12.1. ABTS•+ radical scavenging activity

The ABTS•+ scavenging activity of the CP hydrogels was measured as previously described, with some modifications [1]. To generate ABTS•+, 200 mL of a 7 mM ABTS solution was mixed with 3.52 mL of a 2.45 mM K2S2O8 solution at RT in the dark for 12–16 h. The resulting ABTS•+ solution was then diluted with distilled water until its absorbance reached 0.7 ± 0.02 at 734 nm. Next, 0.02 g of CP/CP hydrogel powder was immersed in 5 mL of the diluted ABTS•+ solution for 30 min at RT in the dark. The mixture was then centrifuged at 1000 rpm for 10 min to remove the hydrogel solids. The ABTS•+ activity was calculated by measuring the UV absorbance at 734 nm, using water as a blank. Eq (3) was used to evaluate the ABTS•+ radical scavenging rate:

ABTS•+ radical scavenging rate % = Ablank-AsampleAsample × 100      (3)

where Ablank and Asample are the absorbances of the ABTS•+ solution before and after CP/CP hydrogel sample was added, respectively.

2.12.2. DPPH radical scavenging activity

The DPPH radical scavenging activity of the CP hydrogels was assayed according to a previously described method, with minor modifications [1]. A 5 mL aliquot of 100 mM DPPH ethanol solution was mixed with 0.02 g of CP/CP hydrogel powder and reacted in the dark for 30 min, followed by centrifugation at 1000 rpm for 10 min to remove the hydrogel solids. The DPPH radical scavenging activity of the samples was calculated by measuring the absorbance at 517 nm using Equation (4):

DPPH radical scavenging rate % = 1-A1-A2A3 × 100               (4)

where A1 and A2 are the absorbances of the solutions with and without DPPH, respectively, and A3 is the absorbance of the DPPH solution without sample.

2.13. Bacterial penetration assay

The CP hydrogels were sterilized using UV light for 30 min and washed three times with sterile PBS (pH 7.4) before the experiment. The strains chosen for the experiments were common harmful bacteria: Escherichia coli (E. coli) and Staphylococcus aureus (S. aureus). E. coli and S. aureus were cultured aerobically at 37°C and shaken at 150 rpm for 10 h. The suspensions were then diluted to 1 × 109 CFU/mL. The CP hydrogels were cut into disks (10 mm in diameter) and placed on agar petri dishes. Then, 50 μL of diluted bacterial suspension was evenly added to the center of the surface of each hydrogel disk. After incubation for 24 h at 37°C, the hydrogel disk was gently removed with tweezers and the agar under each sample was cut with a knife and placed into a test tube containing 5 mL of PBS. The bacteria were separated from the agar using an ultrasonic cleaner, and bacterial counts were determined by routine CFU analysis on agar petri dishes at different dilutions [2].

References

1.	C. Xu, S. Guan, J. Xu, W. Gong, T. Liu, X. Ma, C. Sun, Carbohydr. Polym. 252, 117210 (2021). https://doi.org/10.1016/j.carbpol.2020.117210

2.	R. Xu, G. Luo, H. Xia, W. He, J. Zhao, B. Liu, J. Tan, J. Zhou, D. Liu, Y. Wang, Z. Yao, R. Zhan, S. Yang, J. Wu, Biomaterials. 40, 1-11 (2015). https://doi.org/10.1016/j.biomaterials.2014.10.077