Supporting Information for

Bioelectrochemical Intercalation for Scalable Lithium Recovery

Kohei Shimokawa,1,2,3†* Duyen Minh Pham,†3,4 Heng Yi Teah,5 Xizi Long,3 Yasunori Kikuchi,5,6,7* and Akihiro Okamoto3,4,8,9*

1Frontier Research Institute for Interdisciplinary Sciences, Tohoku University, 6-3 Aramaki Aza Aoba, Aoba-ku, Sendai, 980-8578, Japan.

2Institute for Materials Research, Tohoku University, 2-1-1 Katahira, Aoba-ku, Sendai, 980-8577, Japan.

3International Center for Materials Nanoarchitectonics (WPI-MANA), National Institute for Materials Science, 1-1 Namiki, Tsukuba, 305-0044, Japan.

4Research Center for Macromolecules and Biomaterials, National Institute for Materials Science, 1-1 Namiki, Tsukuba, 305-0044, Japan.

5Presidential Endowed Chair for “Platinum Society”, the University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan.

6Department of Chemical System Engineering, the University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan.

7Institute for Future Initiatives, the University of Tokyo, 7-3-1 Hongo Bunkyo-ku, Tokyo 113-8654, Japan.

8Graduate School of Chemical Sciences and Engineering, Hokkaido University, North 13 West 8, Kita-ku, Sapporo, 060-8628, Japan.

9Graduate School of Science and Technology, University of Tsukuba, 1-1-1 Tennodai, Tsukuba, 305-8577, Japan.

†These authors contributed equally to the work.

*Email: kohei.shimokawa.b7@tohoku.ac.jp; ykikuchi@ifi.u-tokyo.ac.jp; okamoto.akihiro@nims.go.jp

Table 1 | Previously reported Li recovery methods.

| method | material | Li source (concentration)1 | process time | reference2 |
| --- | --- | --- | --- | --- |
| lime-soda evaporation process | - | Li-rich brine (30–550 mM) | 1–2 years | [9] |
| electrochemical intercalation | λ-MnO2 | LiCl solution (0.05–200 mM) | several hours | [5] |
| electrical ion pump (membrane type) | Li ionic superconductor | seawater (~0.030 mM) | 100 hours/5 cycles | [22] |
| electrochemical intercalation | TiO2 coated LiFePO4 | seawater (~0.026 mM) | several hours (Li/Na 1/1) | [11] |
| electrochemical ion pump (battery type) | λ-MnO2 | artificial brine (30 mM) | 1 hour | [13] |
| ion exchange (adsorption) | H2TiO3 | brine (~230 mM) | 24 hours | [19] |
| electrochemical ion pump (battery type) | λ-MnO2 | artificial brine (100 mM) | 11 hours | [12] |
| electrochemical intercalation | λ-MnO2 film on Pt | artificial brine (30 mM) | 2 hours | [14] |
| ion exchange (adsorption) | granulated λ-MnO2 | Li-spiked seawater (~4 mM) | several days | [18] |
| electrochemical intercalation | LiFePO4 | LiCl solution (5 mM) | several hours | [15] |
| electrochemical intercalation | LiNi1/3Co1/3Mn1/3O2 | LiCl solution (30 mM) | 20 min/step | [16] |
| electrochemical intercalation | LiNi0.5Mn1.5O4 | LiCl solution (30 mM) | 20 min/step | [17] |
| ion exchange (adsorption) | H1.6Mn1.6O4 | seawater (~0.024 mM) | 2 days (61% recovery) | [20] |
| ion exchange (adsorption) | H1.6Mn1.6O4 | brine (~230 mM) | 8 hours | [21] |

1Concentration of Li provided in each paper is converted into a value in the unit of mM.

2The reference numbers are corresponding to those in the main article.

Fig. 1 ¦ Concept of bioelectrochemical intercalation. Shewanella oneidensis MR-1, electrogenic bacteria, provides electrons outside the cell by extracellular electron transport (EET). On the other hand, λ-MnO2 with a spinel structure is a Li-ion sieve that prevents the intercalation of larger ions (e.g., Na+, K+, Ca2+). In this method, agglomerates composed of MR-1 and λ-MnO2 spontaneously form on the bottom of the reactor, and Li+ in the solution intercalate into λ-MnO2 due to the charge compensation for electrons supplied by MR-1.

Fig. 2 ¦ Diffusion paths of Li ions in λ-MnO2. (a) Crystal structure of λ-MnO2 with (b) the three-dimensional diffusion paths of Li ions in the spinel lattice. The pictures viewed directly above are shown in (c) and (d). There are two sites for cations to sit in the spinel lattice, 8a and 16c in the space group Fd3m, and they form the three-dimensional network for diffusion. Visualization was carried out by using VESTA[S1].

Fig. 3 ¦ Synthesis of λ-MnO2 nanoparticles. (a) XRD profiles for the materials before and after the acid leaching process for LiMn2O4. Rietveld analysis using the program RIETAN-FP[S2] revealed that the lattice constant was reduced to ~8.037 Å, in good agreement with that of reported λ-MnO2.[S3,S4] (b) SEM image of the prepared λ-MnO2 nanoparticles.

Fig. 4 ¦ Size of dispersed λ-MnO2. Size distribution of the prepared λ-MnO2 nanoparticles dispersed in water determined by using a nanoparticle tracking analyzer. The average and median values were smaller than those of LiMn2O4 synthesized via the same route,[S5] suggesting that the particle size downscaled during the acid leaching process.

Fig. 5 ¦ Dry weight after microbial reduction. Comparison of the dry weight after microbial reduction for 2 days between spinel- and tunnel-structured MnO2. The dry weight of the mixture of materials/microbes was 68 mg when we used λ-MnO2 in LiCl/PBS, while it remarkably decreased for other conditions especially for tunnel-structured MnO2, suggesting dissolution by the microbial reduction.

Fig. 6 ¦ Crystal structures of tunnel-structured MnO2. XRD profiles of the tunnel-structured MnO2 (α, γ) before and after microbial reduction in 50 mM LiCl/PBS. Little change in the crystal structure was indicated while the intensity of diffraction peaks decreased, indicating that dissolution is preferential to the Li intercalation reaction.

Fig. 7 ¦ DAPI-staining image. Bright-field and fluorescence microscopy for resuspended precipitation prepared in (a–c) 10 mM LiCl/PBS solution and (d–f) PBS without LiCl. DNA-stained MR-1 cells were indicated in the agglomerates formed in LiCl/PBS. In contrast, there were few agglomerates in the absence of LiCl. Although we found one big particle, microbes were not involved.

Fig. 8 ¦ Microbial reduction of λ-MnO2 in PBS without LiCl. XRD profiles of the materials after microbial reduction of λ-MnO2 nanoparticles in PBS without LiCl, together with that of as-synthesized λ-MnO2 for comparison. Peak shift was not observed while the intensity significantly decreased, suggesting dissolution of the material due to the lack of Li in the solution.

Fig. 9 ¦ Bioelectrochemical Li recovery with different OD values. (a) Composition determined by ICP-OES and (b) XRD profiles of the materials before and after bioelectrochemical Li recovery from LiCl/PBS solution with different OD values of MR-1 (0, 0.005, 0.01, 0.1, and 0.3), where the concentration of Li and reaction time were 10 mM and 24 h, respectively. Composition and crystal structure become closer to those of LiMn2O4 with the increase in OD values, indicating that MR-1 accelerates Li intercalation into λ-MnO2.

Fig. 10 ¦ Metabolic pathway of microbial lactate consumption. Production of CO2 and acetate was measured in the culture bottle containing PBS (50 mL), MnO2 (500 mg), lactate (50 mM), LiCl (70 mM), and MR-1 (OD 0.3). Without LiCl, there was little CO2 and no acetate production, indicating that all lactate was consumed for Li intercalation. Each condition was replicated three times and each timepoint was conducted independently by different sets of the culture bottles with the same starting components. CO2 and acetate production during the bioelectrochemical Li intercalation suggests an NADH-dependent metabolic pathway for microbial electron generation.

Fig. 11 ¦ Chemical reduction by lactate without MR-1. XRD profiles of the materials before and after the abiotic chemical reduction by lactate in 50 mM LiCl/PBS solution. The lattice constant of the obtained material was determined by Rietveld analysis[S2] to be ~8.21 Å, which is smaller than that of LiMn2O4 (~8.24 Å).[S3,S4] In addition, the peak intensity significantly decreased, indicating the loss of crystallinity during the reaction.

Fig. 12 ¦ Difference in diffusion length for Li and Mg ions in λ-MnO2. Roughly estimated diffusion length for Li and Mg in the spinel lattice at room temperature displayed in (a) linear and (b) logarithmic graphs. The activation energies of Li and Mg were assumed to be 550 and 850 meV, respectively, according to a previous computational study[S6]. Diffusion coefficient, D, was estimated by the following equation: D = νa2exp(-E/kT), where ν, a, E, k, and T are attempt frequency, jump path distance, activation energy for migration, the Boltzmann constant, and temperature, respectively. ν and a were assumed to be 1014 s-1 and 1 Å, respectively, just to compare the order of diffusion length for Li and Mg. The diffusion length shown in the graphs was calculated by Dt, where t is time. The difference in the order of diffusion length between them is 100–1000, which is consistent with the selectivity of Li/Mg in our experiments.

Fig. 13 ¦ Experimental setup for making intermediate states. (a) Details of the experimental setup with limited amounts of Li to prepare materials with intermediate states used for XRD and XANES analyses, where MR-1 (OD: 0.3) and 50 mg of λ-MnO2 are put into a glass bottle filled with 50 mL of LiCl/PBS solution. (b) Theoretical composition after Li recovery depending on the concentration of LiCl in PBS. The amounts of Li in the reactor are insufficient to reach the end state if the concentration is below approximately 5 mM. Note that the remained Li in the initial state of λ-MnO2 after acid leaching was not considered in this estimation.

Fig. 14 ¦ Crystal structures of the materials with intermediate states. XRD profiles for the materials after bioelectrochemical Li recovery with different amounts of Li in the reactor (see Supplementary Fig. 13). Intermediate states between λ-MnO2 and LiMn2O4 were obtained in the Li-limited conditions as we predicted, and the phase change behavior indicating a two-phase existence in the initial stage of Li intercalation is consistent with a previous report[S7].

Fig. 15 ¦ Electronic structures of the materials with intermediate states. (a) XANES spectra for the materials after bioelectrochemical Li recovery with different amounts of Li in the reactor (see Supplementary Fig. 13) and (b,c) their enlarged views. The materials with sufficient amounts of Li showed almost the same profiles as that of LiMn2O4 in both the white line and pre-edges. In contract, those with limited amounts of Li were intermediate states between λ-MnO2 and LiMn2O4, which is consistent with a previous report[S8].

Fig. 16 ¦ Composition of the materials prepared in Li-limited conditions. ICP results for the materials after bioelectrochemical Li recovery in the PBS solutions with limited amounts of Li in the reactor (see Supplementary Fig. 13), together with those of as-synthesized LiMn2O4 and λ-MnO2. The compositions of Li in the materials after bioelectrochemical Li recovery were in excellent agreement with the theoretical values indicated by red bars, which are the sum of initial Li in as-prepared λ-MnO2 and dissolved Li in the solution, suggesting that almost all Li ions were collected into λ-MnO2 even from lower concentrated solutions.

Fig. 17 ¦ Distribution of elements in MR-1/nanoparticles composite. STEM–EDS mapping images for the dispersed agglomerates after bioelectrochemical Li recovery. Mn was detected only outside the cell along with O mainly keeping the morphology of nanoparticles, supporting our concept of bioelectrochemical intercalation driven by EET.

Fig. 18 ¦ Nanosheets observed around microbes. (a) Cross-sectional TEM image for a dispersed composite of MR-1 and nanoparticles after bioelectrochemical Li recovery. Although the morphology of nanoparticles was mostly kept after Li recovery experiments, nanosheets were also found near microbes. This morphology is similar to that of a reported hydrated Mn phosphate[S9]. (b) STEM and (b) EELS mapping images for the nanosheets along with nanoparticles. EELS analysis revealed that the nanosheets consist of Mn2+, which is consistent with the valence state of the hydrated Mn phosphate (i.e., Mn3(PO4)2·3H2O).

Fig. 19 ¦ Agglomerate used for FIB–SEM–EDS analysis. SEM image for the agglomerate before FIB milling. We selected a relatively small agglomerate because it is suitable for processing and preparing a cross-section. Microbes were found on the surface of the agglomerate in addition to those inside.

Fig. 20 ¦ Distribution of elements on the cross-section of agglomerate. (a) EDS mapping for the agglomerate after FIB milling and (b) corresponding SEM image. In addition to Mn and O from oxide particles, Os indicating stained OM c-Cyts was detected even inside the agglomerate, suggesting that secretions from microbes were distributed across the particles and secure electronic conductivity.

Fig. 21 ¦ Potential change during Li insertion into MnO2 polymorphs. Based on data provided in a previous computational study[S10], we prepared a diagram showing the predicted potential change in Li intercalation into MnO2 polymorphs. λ-MnO2 has the highest potential for accommodating Li ions up to the composition of LiMn2O4, and the two-phase reaction of LiMn2O4/Li2Mn2O4 undergoes at a lower potential. In contrast, tunnel-structured MnO2 (e.g., α, β, γ) showed much lower potentials compared to λ-MnO2 at the beginning of Li intercalation. The above results are consistent with the fact that λ-MnO2 is synthesized via LiMn2O4;[S4] namely, it is stabilized by Li.

Fig. 22 ¦ Reaction pathways during bioelectrochemical Li recovery. Schematic diagram for discussing the reaction mechanism during the reduction of (a,b) tunnel-structured and (c,d) spinel-structured MnO2 in the environments of LIBs and seawater. Li intercalation into tunnel-structured MnO2 proceeds in LIBs as 3–3.5 V class cathode materials (i.e., approximately 0–0.5 V vs SHE) according to Supplementary Fig. 22 and previous experimental reports[S11–S13]. However, in dilute Li aqueous solution such as seawater, the potential for Li intercalation becomes lower than that for dissolution of MnO2, which is approximately 0.4 V vs SHE at neutral pH.[S14] In the case of spinel-structured MnO2 (i.e., λ-MnO2), the potential for Li intercalation is higher than that of the dissolution of MnO2. In addition, the reductive potential of MR-1 (i.e., approximately -0.2 V vs SHE) is suitable for obtaining a large driving force of Li intercalation into λ-MnO2 while preventing the over-lithiation to form Li2Mn2O4. (e) Summary of the reaction pathways of λ-MnO2 during bioelectrochemical Li recovery from seawater.

Fig. 23 ¦ Lactate consumption during Li recovery from seawater. Concentration of lactate measured by ion chromatography during Li recovery from seawater with MR-1. Lactate was gradually consumed for 9 h and then the concentration became constant. The concentration of Li (see Fig. 4b in the main article) was not largely changed after the activity of microbes was settling down, suggesting that Li was stably stored in the material even without microbial activity once it was inserted electrochemically.

Table 2 | Mass% of each element measured by ICP-OES.

|  | Li | Mg | Na | K | Ca |
| --- | --- | --- | --- | --- | --- |
| As-prepared λ-MnO2 (sample 1) | 0.29 | 0.007 | 0.01 | <0.005 | <0.005 |
| As-prepared λ-MnO2 (sample 2) | 0.29 | 0.007 | 0.01 | <0.005 | <0.005 |
| As-prepared λ-MnO2 (sample 3) | 0.29 | 0.007 | 0.02 | <0.005 | <0.005 |
| After being soaked in seawater (sample 4) 1 | 0.33 | 0.03 | 0.05 | 0.01 | 0.06 |
| After being soaked in seawater (sample 5) 1 | 0.33 | 0.03 | 0.05 | 0.01 | 0.06 |
| After being soaked in seawater (sample 6) 1 | 0.33 | 0.03 | 0.06 | 0.01 | 0.07 |
| After microbial Li recovery from seawater (sample 7) 2 | 0.79 | 0.04 | 0.06 | 0.01 | 0.07 |
| After microbial Li recovery from seawater (sample 8) 2 | 0.85 | 0.04 | 0.07 | 0.01 | 0.07 |
| After microbial Li recovery from seawater (sample 9) 2 | 0.81 | 0.04 | 0.05 | 0.01 | 0.07 |

1 30 mg λ-MnO2 was just soaked in 500 mL seawater for 24 h.

2 500 mL seawater was bioelectrochemically treated with 30 mg λ-MnO2 and MR-1 for 24 h.

Table 3 | Molar ratio of Li/M (M = Mg, Na, K, Ca) bioelectrochemically intercalated into the material.

|  | Mg | Na | K | Ca |
| --- | --- | --- | --- | --- |
| Calculated from the averaged values of samples 4–6 and 7–9 | 170 | 242 | - | 422 |

Fig. 24 ¦ Li recovery from seawater with riboflavin. Concentration of Li before and after bioelectrochemical Li recovery from seawater with and without 2 mM riboflavin. The Li recovery kinetics was substantially increased by spiking a tiny amount of riboflavin, suggesting the enhanced current generation of MR-1 as also observed in the LiCl/PBS system. Error bars present the standard error of means (n = 3).

Fig. 25 ¦ Regeneration of l-MnO2 by Na2S2O8. XRD profiles showing the reversibility of bioelectrochemical Li intercalation and following chemical Li leaching by using an oxidant, Na2S2O8[S15]. The peak positions clearly shifted to higher angles and became almost the same as those of original l-MnO2 after the oxidation process, indicating high reversibility in the structure change.

Fig. 26 ¦ Mn loss in the Li-reaching unit and efficiency of the Mn-removal unit. The concentrations of Mn after the Li-reaching and Mn-removal processes. The amount of Mn loss (0.0012%) was calculated from the concentration of soluble Mn (0.46 mg/L) in the effluent of the Li-leaching unit (40 mL) and the starting amount of LiMn2O4 (5 g). Based on this result, it was assumed that 99.9% of l-MnO2 could be recycled in our Li2CO3 production process. After increasing the pH to 11, all soluble Mn was precipitated and removed by filtration, resulting in an effluent Mn concentration below the detection limit (<0.005 mg/L).

Fig. 27 ¦ Material obtained by the Li2CO3-precipitation process. (a) XRD and (b) ICP results for the material obtained through our bioelectrochemical Li recovery and Li2CO3-precipitation processes, roughly explained as follows. Li1-xMn2O4 was collected after bioelectrochemical Li recovery from LiCl/PBS and then it was washed with water (water/Li1-xMn2O4 = 10 w/w). A calculated amount of water and Na2S2O8 were added and heated in the Li-leaching step. Subsequently, pH was adjusted and Na2CO3 was added to the solution in the Mn-removal and Li2CO3-precipitation steps, respectively. Hot water wash was carried out before drying the obtained material. The XRD profiles indicate crystalline Li2CO3, whose purity was ~98% based on ICP for two different batches. These results suggest that a small amount of water is enough to wash the material and the organic contamination is not a serious issue in our method.

Table 4 | Industrial Li2CO3 market price. As of 2024.

|  | Price (USD/kg Li2CO3) | References |
| --- | --- | --- |
| 98% Li2CO3 | 7.4 | https://www.intratec.us/chemical-markets/lithium-carbonate-price |
| 99.2% Li2CO3 | 9.9 | https://www.metal.com/Lithium/201905160001 |
| 99% Li2CO3 | 8.9–16.9 | https://yujianghuagong.en.made-in-china.com/product/MnCpSPUYnBkj/China-Hot-Sale-CAS-554-13-2-99-Purity-Industrial-Grade-Lithium-Carbonate.html |

Fig. 28 ¦ Breakdown of the production cost of Li2CO3. The calculated production cost of Li2CO3 in our bioelectrochemical Li recovery method. The raw materials, which contributed significantly to the total cost, include l-MnO2, lactate, soybean meal, Na2S2O8, NaOH/HCl, and Na2CO3. The cost for Na2S2O8 accounted for approximately 60% of the total raw material cost.

Fig. 29 ¦ Cation-exchange membrane cell. (a) Setup of our prototype system with a cation-exchange membrane. LiCl was not included in the bottle but dissolved in the solution filling the beaker. (b) The change in color before and after the Li recovery process, where the concentration of LiCl and processing time were 10 mM and 24 h, respectively. The disappearance of a characteristic red color suggests Li intercalation into λ-MnO2. Note that the precipitates formed during the Li recovery process were firmly dispersed to show the color of particles. (c) XRD profiles before and after the experiments. The peak positions clearly shifted to be almost the same as those of LiMn2O4, indicating Li recovery via the membrane filter.

Fig. 30 ¦ A cradle-to-gate life cycle system boundary of the modelled system. The Li intercalation (in blue) and the Li2CO3 precipitation (in green) are based on the experiments in this study. Recycling paths for the λ-MnO2 and water are included for a practical design. This prospective system is used as the basis for the environmental LCA and TEA.

Table 5 | The efficiency of Li intercalation and Li2CO3 precipitation. We developed two cases in this study: SIMULATION (industrial scale) and LAB (laboratory scale).

| Process | SIMULATION | LAB |
| --- | --- | --- |
| Li intercalation | 90% | 80% |
| Li2CO3 precipitation (= leaching × precipitation) | 58.5% = (90 × 65)% | 48% = (80 × 60)% |

Table 6 | Life cycle inventory data of Li intercalation for 1 kg Li2CO3 production. The SIMULATION is presented in the main text. The LAB is based on lab experiment procedure.

|  | Unit | SIMULATION | LAB |
| --- | --- | --- | --- |
| Input |  |  |  |
| Brine, 0.15 wt.% Li | kg | 237.887 | 326.165 |
| λ-MnO2 | kg | 0.080 | 1.961 |
| Sodium lactate | kg | 0.432 | 1.580 |
| Soybean meal | kg | 0.300 | 0.300 |
| Water | kg | 21 | 30587 |
| Electricity, pumping brine | kWh | 0.0974 | 0.1335 |
| Electricity, pumping groundwater | kWh | 0.0068 | 2.5042 |
| Electricity, heating (30 °C) | kWh | 1.4584 | 1.4584 |
| Electricity, dewatering | kWh | 0.0024 | 0.0024 |
| Output |  |  |  |
| LiMn2O4, in slurry | kg | 8.366 | 10.196 |
| Brine effluent, for potassium extraction | kg | 292.264 | 397 |
| Wastewater | kg | 0 | 30348 |

Table 7 | Life cycle inventory data of Li2CO3 precipitation for 1 kg Li2CO3 production. The LiMn2O4, in slurry is the output from Table 5.

|  | Unit | SIMULATION | LAB |
| --- | --- | --- | --- |
| Input |  |  |  |
| LiMn2O4, in slurry | kg | 8.366 | 10.196 |
| Na2S2O8 | kg | 5.507 | 6.711 |
| NaOH | kg | 0.06 | 0.06 |
| Na2CO3 | kg | 1.434 | 1.434 |
| HCl | kg | 0.04 | 0.04 |
| water | kg | 20.914 | 20.914 |
| electricity, pumping | kWh | 0.0017 | 0.0017 |
| electricity, stirring | kWh | 0.0001 | 0.0001 |
| electricity, heating (90 °C) | kWh | 3.6461 | 3.6461 |
| Output |  |  |  |
| Li2CO3, battery grade | kg | 1 | 1 |
| waste Mn(OH)2 | kg | 0.082 | 2.006 |
| wastewater | kg | 20.914 | 20.914 |

Table 8 | List of the reference life cycle inventory. From ecoinvent 3.10 database for LCA.

|  | Activity name in ecoinvent 3.10 |
| --- | --- |
| Electricity | market for electricity, medium voltage ¦ electricity, medium voltage ¦ APOS, U - CL |
| Hydrochloric acid | market for hydrochloric acid, without water, in 30% solution state ¦ hydrochloric acid, without water, in 30% solution state ¦APOS, U - RoW |
| Manganese oxide | market for manganese dioxide ¦ manganese dioxide ¦ APOS, U - GLO |
| Sodium carbonate | market for soda ash, light ¦ soda ash, light ¦ APOS, U - RoW |
| Sodium hydroxide | market for sodium hydroxide, without water, in 50% solution state ¦ sodium hydroxide, without water, in 50% solution state ¦ APOS, U - RoW |
| Sodium persulfate | market for sodium persulfate ¦ sodium persulfate ¦ APOS, U - GLO |
| Solid waste treatment | treatment of waste zeolite, inert material landfill ¦ waste zeolite ¦ APOS, U - RoW |
| Soybean meal | market for soybean meal ¦ soybean meal ¦ APOS, U - BR |
| Wastewater treatment | treatment of wastewater, average, wastewater treatment ¦ wastewater, average ¦ APOS, U - RoW |

Table 9 | Result of water consumption for 1 kg Li2CO3 production. Unit in m3.

|  | In-situ water | Ex-situ water | Brine’s water |
| --- | --- | --- | --- |
| This study | 0.084 | 0.295 | 0.006 |
| Atacama | 0.041 | 0.045 | 0.215 |
| Olaroz | 0.217 | 0.032 | 0.450 |

Table 10 | Result of climate change impact for 1 kg Li2CO3 production. Unit in kg CO2-equivalent.

|  | Li intercalation/concentration | Li2CO3 precipitation |
| --- | --- | --- |
| This study | 3.71 | 13.09 |
| Atacama | 1.85 | 1.52 |
| Olaroz | 5.28 | 2.11 |

Table 11 | Additional results of water consumption in background system of this study, ex-situ water. Unit in m3/kg Li2CO3.

|  |  | SIMULATION | LAB |
| --- | --- | --- | --- |
| Li intercalation | Sodium lactate | 0.019 | 0.068 |
|  | Manganese oxide | 0.005 | 0.117 |
|  | Soybean meal | 0.001 | 0.001 |
|  | Electricity | 0.002 | 0.004 |
|  | Brine pumping | 0.000 | 0.000 |
|  | Groundwater pumping | 0.000 | 0.002 |
| Li2CO3 precipitation | Sodium persulfate | 0.239 | 0.291 |
|  | Sodium carbonate | 0.025 | 0.025 |
|  | Electricity | 0.004 | 0.004 |
|  | Sodium hydroxide | 0.001 | 0.001 |
|  | Hydrochloric acid | 0.000 | 0.000 |
|  | Wastewater treatment | 0.000 | 0.000 |
|  | Solid waste treatment | 0.000 | 0.000 |
| Total |  | 0.295 | 0.513 |

Table 12 | Additional results of climate change impact of this study. Unit in kg CO2-equivalent/kg Li2CO3.

|  |  | SIMULATION | LAB |
| --- | --- | --- | --- |
| Li intercalation | Sodium lactate | 2.086 | 7.629 |
|  | Manganese oxide | 0.274 | 6.726 |
|  | Soybean meal | 0.396 | 0.396 |
|  | Electricity | 0.890 | 2.331 |
|  | Brine pumping | 0.055 | 0.076 |
|  | Groundwater pumping | 0.004 | 1.391 |
| Li2CO3 precipitation | Sodium persulfate | 10.217 | 12.448 |
|  | Electricity | 0.660 | 0.660 |
|  | Sodium carbonate | 2.074 | 2.074 |
|  | Sodium hydroxide | 0.091 | 0.091 |
|  | Hydrochloric acid | 0.040 | 0.040 |
|  | Wastewater treatment | 0.011 | 0.011 |
|  | Solid waste treatment | 0.001 | 0.013 |
| Total |  | 16.799 | 33.887 |

Table 13 | All environmental Impacts of 1 kg Li2CO3 production. Based on ReCiPe 2016 methods.

|  |  | SIMULATION | LAB |
| --- | --- | --- | --- |
| Acidification: terrestrial | kg SO2-Eq | 0.0897 | 0.1586 |
| Climate change | kg CO2-Eq | 16.7991 | 33.8872 |
| Ecotoxicity: freshwater | kg 1,4-DCB-Eq | 2.0249 | 3.1993 |
| Ecotoxicity: marine | kg 1,4-DCB-Eq | 2.5554 | 4.1818 |
| Ecotoxicity: terrestrial | kg 1,4-DCB-Eq | 179.2851 | 324.5271 |
| Energy resources: non-renewable, fossil | kg oil-Eq | 4.5567 | 9.2149 |
| Eutrophication: freshwater | kg P-Eq | 0.0072 | 0.0136 |
| Eutrophication: marine | kg N-Eq | 0.0018 | 0.0030 |
| Human toxicity: carcinogenic | kg 1,4-DCB-Eq | 4.1352 | 7.1518 |
| Human toxicity: non-carcinogenic | kg 1,4-DCB-Eq | 38.5904 | 64.3499 |
| Ionising radiation | kBq Co-60-Eq | 0.8044 | 1.7145 |
| Land use | m2*a crop-Eq | 0.5918 | 0.9377 |
| Material resources: metals/minerals | kg Cu-Eq | 0.2196 | 0.5435 |
| Ozone depletion | kg CFC-11-Eq | 0.0000 | 0.0000 |
| Particulate matter formation | kg PM2.5-Eq | 0.0668 | 0.1249 |
| Photochemical oxidant formation: human health | kg NOx-Eq | 0.0417 | 0.0833 |
| Photochemical oxidant formation: terrestrial ecosystems | kg NOx-Eq | 0.0438 | 0.0878 |
| Water use | m3 | 0.2945 | 0.5130 |

Table 14 | List of the reference prices of raw material and electricity for the techno-economic assessment. Unit in USD/kg material or USD/kWh electricity.

|  | Base | Best case | Worst case | References |
| --- | --- | --- | --- | --- |
| Manganese oxide | 0.40 | 0.20 | 0.80 | https://xtmkcom.en.made-in-china.com/product/IyeJLhWdLoki/China-Batter-Materials-Electrolytic-Manganese-Dioxide-Emd-Powder.html |
| Sodium lactate | 3.15 | 2.80 | 3.50 | https://zm-biotech.en.made-in-china.com/product/MJSYWZPykqVe/China-Zhuangmei-Biotech-Produce-Sodium-Lactate-Powder-96-at-Competitive-Price.html |
| Soybean meal | 0.60 | 0.56 | 0.65 | https://humicchina.en.made-in-china.com/product/vOnGRTmdvPAi/China-75-Amino-Acid-Powder-Soybean-or-Soybean-Meal-Organic-Nitrogen-Inorganic-Nitrogen.html?pv_id=1i1ojqm22150&faw_id=1i1ojqvcfb41 |
| Sodium persulfate | 0.63 | 0.55 | 0.70 | https://hongbangjinhua.en.made-in-china.com/product/gnSpTbwvhtYX/China-Best-Price-99-Purity-Potassium-Sodium-Persulfate-for-Triggering-Agent.html |
| Sodium carbonate | 0.25 | 0.24 | 0.26 | https://wffondland.en.made-in-china.com/product/POxAvNpEbzhC/China-99-2-Industrial-Grade-Dense-Light-Soda-Ash-Sodium-Carbonate-for-Glass-Paper-Making.html?pv_id=1hrod1qnp269&faw_id=1hrod3bjb7cc |
| Sodium hydroxide | 0.48 | 0.47 | 0.48 | https://zf-sodiumhydroxide.en.made-in-china.com/product/EwmaMJtduHfU/China-Hot-Sale-Chemical-Sodium-Hydroxide-CAS-1310-73-2-From-Supplier.html?pv_id=1hrocp0ll10c&faw_id=1hrocubvs673 |
| Hydrochloric acid | 0.18 | 0.15 | 0.21 | https://sincerechemical01.en.made-in-china.com/product/vOcfVoKZGeRq/China-Hydrochloric-Acid-31-33-34-35-36-37-HCl-Muriatic-Acid.html?pv_id=1hrodehh551f&faw_id=1hrodf9p87b5 |
| Waste treatment | 0.08 | 0.08 | 0.08 | Huang et al. 2021 https://doi.org/10.1021/acssuschemeng.0c08733 |
| Electricity | 0.10 | 0.08 | 0.12 | https://www.statista.com/statistics/1029737/chile-electricity-average-market-price/ |

Table 15 | Details of production cost for 1 kg Li2CO3 production. The operational expenditure per year includes capital expenditure, represented under asset depreciation (20 years facility lifetime). The unit cost calculation is based on a 70,000-ton of annual production of Li2CO3 production.

|  | Unit | SIMULATION | LAB |
| --- | --- | --- | --- |
| Raw materials | USD/year | 378,450,555 | 853,905,824 |
| Utilities | USD/year | 36,951,359 | 76,305,611 |
| Operation and maintenance | USD/year | 1,545,000 | 1,854,000 |
| Overhead, tax and insurance, general expenses | USD/year | 466,667 | 560,000 |
| Asset depreciation | USD/year | 394,967 | 473,960 |
| Total annual production cost | USD/year | 417,808,548 | 933,099,395 |
| Unit cost per kg Li2CO3 | USD | 5.97 | 13.33 |

- References

[S1]	Momma, K., Izumi, F.: VESTA 3 for three-dimensional visualization of crystal, volumetric and morphology data. Journal of Applied Crystallography 44(6), 1272–1276 (2011)

[S2]	Izumi, F., Momma, K.: Three-dimensional visualization in powder diffraction. Solid State Phenomena 130, 15–20 (2007)

[S3]	Knight, J.C., Therese, S., Manthiram, A.: Delithiation mechanisms in acid of spinel LiMn2−xMxO4 (M = Cr, Fe, Co, and Ni) cathodes. Journal of The Electrochemical Society 162(3), 426 (2014)

[S4]	Hunter, J.C.: Preparation of a new crystal form of manganese dioxide: λ-MnO2. Journal of Solid State Chemistry 39(2), 142–147 (1981)

[S5]	Shimokawa, K., Matsubara, S., Okamoto, A., Ichitsubo, T.: Light-induced Li extraction from LiMn2O4/TiO2 in a water-in-salt electrolyte for photo-rechargeable batteries. Chemical Communications 58(69), 9634–9637 (2022)

[S6]	Liu, M., Rong, Z., Malik, R., Canepa, P., Jain, A., Ceder, G., Persson, K.A.: Spinel compounds as multivalent battery cathodes: a systematic evaluation based on ab initio calculations. Energy & Environmental Science 8(3), 964–974 (2015)

[S7]	Kanamura, K., Naito, H., Yao, T., Takehara, Z.: Structural change of the LiMn2O4 spinel structure induced by extraction of lithium. Journal of Materials Chemistry 6(1), 33–36 (1996)

[S8]	Kim, S., Kang, J.S., Joo, H., Sung, Y.-E., Yoon, J.: Understanding the behaviors of λ-MnO2 in electrochemical lithium recovery: key limiting factors and a route to the enhanced performance. Environmental Science & Technology 54(14), 9044–9051 (2020)

[S9]	Jin, K., Park, J., Lee, J., Yang, K.D., Pradhan, G.K., Sim, U., Jeong, D., Jang, H.L., Park, S., Kim, D., et al.: Hydrated manganese(II) phosphate (Mn3(PO4)2·3H2O) as a water oxidation catalyst. Journal of the American Chemical Society 136(20), 7435–7443 (2014)

[S10]	Kitchaev, D.A., Dacek, S.T., Sun, W., Ceder, G.: Thermodynamics of phase selection in MnO2 framework structures through alkali intercalation and hydration. Journal of the American Chemical Society 139(7), 2672–2681 (2017)

[S11]	Lee, S.-Y., Wu, L., Poyraz, A.S., Huang, J., Marschilok, A.C., Takeuchi, K.J., Takeuchi, E.S., Kim, M., Zhu, Y.: Lithiation mechanism of tunnel-structured MnO2 electrode investigated by in situ transmission electron microscopy. Advanced Materials 29(43), 1703186 (2017)

[S12]	Jiao, F., Bruce, P.G.: Mesoporous crystalline β-MnO2—a reversible positive electrode for rechargeable lithium batteries. Advanced Materials 19(5), 657–660 (2007)

[S13]	Sarciaux, S., La Salle, A.L.G., Verbaere, A., Piffard, Y., Guyomard, D.: γ-MnO2 for Li batteries: Part II. some aspects of the lithium insertion process into γ-MnO2 and electrochemically lithiated γ-LixMnO2 compounds. Journal of Power Sources 81, 661–665 (1999)

[S14]	Sun, W., Kitchaev, D.A., Kramer, D., Ceder, G.: Non-equilibrium crystallization pathways of manganese oxides in aqueous solution. Nature Communications 10(1), 1–9 (2019)

[S15]	Zhou, Z., Liu, Y., Tang, Z., Xia, J., Jin, H., Zhang, J., Chen, Y., Wang, C.: Facile and efficient recycling of cathode materials of spent lithium manganate batteries. Chemical Communications 59(26), 3906–3909 (2023)