Supplementary Information for

A radical polymer for highly efficient solar evaporation and gas separation

Wei Liu1,2,+, Ming Yang3,+, Jing Liu,4,+ Meijia Yang,5 Jing Li,6 Yanqiu Lu,1 Susilo Japip,1 Zhongxin Chen,6 Ji Wu,1 Feng Li,1 Sui Zhang1,*

1 Department of Chemical and Biomolecular Engineering, National University of Singapore, 4 Engineering Drive 4, Singapore 117585, Singapore

2School of Physics, Southeast University, Nanjing, 211189, China

3Department of Applied Physics, The Hong Kong Polytechnic University, Hung Hom, Hong Kong SAR, China

4School of Materials Science and Engineering, Guilin University of Electronic Technology, Guang Xi, China

5Key Laboratory for Polymeric Composite and Functional Materials of Ministry of Education, School of Chemistry, Sun Yat–sen University, Guangzhou 510275, China

6Department of Chemistry, National University of Singapore, 3 Science Drive 3, Singapore 117543, Singapore

+: These authors contributed equally to this work.

Correspondence should be addressed to: chezhangsui@nus.edu.sg;

Methods and instruments

Scanning electronic microscopy (SEM) images were obtained using a Jeol JSM-6701F instrument. For X-ray photoelectron spectroscopy (XPS) investigations, samples were dispersed on Au-coated Si wafers. The XPS spectra were collected with the Phobios 100 electron analyzer equipped with 5 channeltrons, using an unmonochromated Al Ka X-ray source (1486.6 eV). Fourier-transform infrared spectroscopy (FTIR) measurements were performed at room temperature in a continuous vacuum environment. The FTIR samples were prepared by compressing samples with KBr into a disc. Solid 13C NMR spectra were recorded with Bruker 400 MHz NMR. UV-VIS-NIR adsorption spectra were collected with Shimadzu UV-3600. Thermal gravimetric analysis (TGA) was performed at a heating rate of 10 ºC /min in nitrogen atmosphere. The free volume size, fraction and distribution of RP as a function of temperature were characterized by positron annihilation lifetime spectroscopy (PALS) using a conventional fast-fast coincidence spectroscope. Two Kapton® films were used to sandwich a radioactive source of 22Na as the source of positrons. The samples were vacuumed for at least 12 h prior to testing and five million counts were collected for each spectrum. The data were resolved into three lifetimes using the PATFIT program, which assumes a Gaussian distribution of the logarithm of the lifetime for each component. The free volume distribution was analysed based on the MELT program.

Supplementary figure 1｜X-ray photoelectron spectroscopy spectrum of RP-CN.

Supplementary figure 2｜Thermal gravimetric analysis curve of RP-CN.

Supplementary figure 3｜XRD profile of RP-CN. No obvious peak observed, indicating the amorphous of the cross-linked radical polymer.

Supplementary figure 4｜Solid state 13C NMR spectra of RP-CN and RP-COOH

Supplementary figure 5｜Optical images of RP-water/GF composite membrane.

Supplementary figure 6｜Differential scanning calorimetric (DSC) curve of RP-water. The calculated vaporization enthalpy of water is 1972 J g-1. Samples were placed in open Al crucibles and heated in the temperature range from 30 to 200 oC at a heating rate of 5 oC/min under a nitrogen flow flux f 20 ml/min. Before measuring the RP-water sample, sapphire is used as the reference to calibrate the DCS. The effective heat capacity of RP-water can be calculated by comparing the measured heat flow with that of the standard sapphire sample.

Supplementary figure 7｜Optical images showing the morphologies of RP-water/GF hydrogel membrane before (a) and after (b) 1-sun irradiation.

Supplementary figure 8｜X-ray photoelectron spectroscopy (XPS) spectra and FTIR spectra of RP-CN and RP-COOH. a, N1s spectra of RP-CN and RP-COOH. RP-CN has two distinct peaks at ~398.7 eV and ~401.4 eV, while the second peak disappeared in RP-COOH. The first peak can be assigned to the –C=N-C- of formed triazine rings. The second peak is associated with unreacted nitrile group, which accounts for 20.5% of whole N content. b, FTIR spectra of RP-CN and RP-COOH. RP-COOH shows an additional peak at ~1722 cm-1 associated with –COO- group.

Supplementary figure 9｜EPR spectra of RP-CN and RP-COOH

Supplementary figure 10｜a, Robeson plot for H2/ N2 gas pairs with the 1991 upper bounds indicated by a pink line and 2008 upper bounds by a green line. The single-gas permeation data of RP-CN membrane (red star) were compared with accumulated literature data for state-of-the-art ultrapermeable PIMs (black squares), microporous solids (zeolites, MOFs, POPs and inorganic 2D materials, blue triangles) and commercial polymer membranes (purple triangles). b, Robeson plot for CO2/N2 gas pairs with the 2008 upper bounds by a green line. The single-gas permeation data of RP-COOH membrane (red star) was compared with accumulated literature data of PIM-PIs (green diamond) and ladder PIMs (purple triangles).

Supplementary figure 11｜The calculated DOSs of f-RP with one radical state, in which the top figure is the DOS without spin-polarization, and the bottom figure is the DOS with spin-polarization. The SOMO state in the DOS is denoted by the black arrow. The f-RP with one radical state is energetically more favourable with spin-polarization.