Selective Aerobic Oxidation of C−H Bond over C−C Bond by Single-Atom Catalysts

Tianbo Li,1, 2, ‡ Qian Zhang,2, ‡ Yalin Guo,3 Mingyang Qin,4 Hai Wang4, Xiang-Ting Min,2, * Yi-Tao Cui,5 Shijian Lu,6 Liang Wang,4 Lin Li,2 Botao Qiao,2, * Tao Zhang2

- School of Chemical Engineering and Technology, China University of Mining and Technology, Xuzhou 221116, China.

- CAS Key Laboratory of Science and Technology on Applied Catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China.

- State Key Laboratory of Coal Mine Disaster Dynamics and Control, Institute of Advanced Interdisciplinary Studies, School of Chemistry and Chemical Engineering, Chongqing University, Chongqing 401331, China.

- Key Lab of Biomass Chemical Engineering of Ministry of Education, College of Chemical and Biological Engineering, Zhejiang University, Hangzhou 310027, China.

- Shenzhen Innovation Light-source Facility (SILF), Institute of Advanced Science Facilities (IASF), Shenzhen 518103, China.

- Carbon Neutrality Institute, Jiangsu Key Laboratory of Coal-based Greenhouse Gas Control and Utilization, China University of Mining and Technology, Xuzhou 221116, China.

Table of Contents

1.	Catalyst preparation	2

2.	Catalyst characterization	5

3.	Catalytic activity testing and product analysis.	6

4.	Control experiments and mechanism investigations.	7

5.	Supplementary figures and tables	9

6.	References	29

- Catalyst preparation

Materials

PdCl2 (99.99%), RuCl3•3H2O (99.99%), HAuCl4•4H2O (99.99%) were purchased from Tianjin Fengchuan. 36% Hydrochloric acid was purchased from Tianjin Kemel. Polyethylene glycol (97%, molecular mass 1750 ± 50), ethanol (98%), ethylbenzene (99.8%), acetophenone (99%), MnO2 (98.0%), MgSO4 (98.0%), NaBH4 (98%) were purchased from Sigma-Aldrich. Deionized water was obtained from a Millipore Autopure system. All reagents were used without further purification. Helium (99.999%), hydrogen (99.999%), oxygen (99.999%) and nitrogen (99.999%) were purchased from Dalian Special Gases Company. 18O2 (96%) was purchased from Linde Gas NA (Shanghai).

Mn2O3 support

Mn2O3 support was prepared by a calcination and decomposing method. MnO2 power was calcined at 500 oC for 3 h in air. The XRD figures showed that after calcination α-MnO2 would decompose to Mn2O3, same case with Pd1/Mn2O3 catalyst (Figure S1).

Pd1/Mn2O3 catalyst

Mn2O3 supported Pd single-atom catalysts (SACs) was prepared by impregnation on MnO2 and a subsequent calcination in which MnO2 decomposed to Mn2O3. Typically, 1 g MnO2 powder was dispersed in 2 mL deionized water with rigorous stirring. Appropriate amount of PdCl2·HCl solution (prepared by mixing 100 mg of PdCl2, 4 mL concentrated HCl, and a certain amount of H2O) was added into 3 mL deionized water. The diluted PdCl2·HCl solution was added into the MnO2 solution at one time for another 5 h under vigorous stirring. The solution was filtrated, and the obtained filter cake was washed for three times by deionized water followed by drying at 120 °C for 4 h and calcination at 500°C for 3 h in air, denoted as Pd1/Mn2O3.

In addition, for preparation of a higher loading Pd SACs, the preliminary preparation was consistent with the above, except the obtained solution was stirred by glass rod meanwhile dried at 95 oC water bath for 0.5 hours. After the stirring under water bath process, the solid power was calcined at 500 oC for 3 h in air, denoted as 0.7Pd1/Mn2O3.

The inductively coupled plasma optical emission spectrometry (ICP-OES) tests showed that the actual loading of the Pd1/Mn2O3 and 0.7Pd1/Mn2O3 were 0.09% and 0.69%, respectively.

Pd-NP/Mn2O3 catalysts

For comparison, a Pd-NP/Mn2O3 catalyst containing Pd nanoparticles (NPs) of 6-10 nm in size was prepared by deposing colloidal Pd NPs onto the Mn2O3 surface. The typical process used 1 g Mn2O3 powder (from 1. Mn2O3 support) dispersed in deionized water with rigorous stirring. Appropriate amount of colloidal Pd NPs solution were dropwise added into the Mn2O3 solution under stirring at 95 oC and continued stirring until the ethanol was evaporated. Then the Mn2O3 supported Pd NPs were calcined at 300 oC for 1 hours in air to remove the protection agent and the final catalyst was denoted as Pd-NP/Mn2O3. The actual loading of Pd NPs was 0.67% measured by ICP.

Colloidal Pd NPs were prepared according previous reported procedure.[1] All operations were carried out under inert atmosphere (Ar). H2PdCl4 solution (2.0 mmol/L) was prepared by mixing 0.6 mmol of PdCl2, 6.0 mL of 0.2 M HCl, and 294 mL of H2O. A mixture of 15 mL of a 2.0 mmol H2PdCl4 solution, 21 mL of H2O, 14 mL of ethanol (40 vol %), and 0.0333 g of PVP were refluxed for 3 h in air. The solution thus prepared had a dark brown color. The obtained Pd nanocluster solution was very stable and ready for deposition on Mn2O3 support.

Ru1/Mn2O3 catalysts

Mn2O3 supported Ru1 single-atom catalyst (SACs) was prepared by impregnation on MnO2 and a subsequent calcination in which MnO2 decomposed to Mn2O3. Typically, 1 g MnO2 powder was dispersed in 2 mL deionized water with rigorous stirring. Appropriate amount of RuCl3 solution (prepared by mixing 100 mg of RuCl3.3H2O, and a certain amount of H2O) was added into 3 mL deionized water. The diluted RuCl3 solution was added into the MnO2 solution at one time for another 5 h under vigorous stirring. The solution was filtrated, and the obtained filter cake was washed for three times by deionized water followed by drying at 120°C for 4 h and calcination at 500°C for 3 h in air, denoted as 0.1Ru1/Mn2O3.

Ru-NP/Mn2O3 catalysts

Ru-NP/Mn2O3 catalyst containing Ru NPs was prepared by deposing colloidal Ru NPs onto the Mn2O3 surface. The typical process used 1 g Mn2O3 powder (from 1. Mn2O3 support) dispersed in 2 mL deionized water with rigorous stirring. Appropriate amount of colloidal RuCl3 solution (prepared by mixing 100 mg of RuCl3.3H2O, and a certain amount of H2O) were dropwise added into the Mn2O3 solution under stirring at 95 oC. Then added 5 times stoichiometric NaBH4 solution (prepared by mixing 5 times stoichiometric NaBH4 with 2 mL deionized water) at one time, and continued stirring until the H2O was evaporated. The Mn2O3 supported Ru NPs were calcined at 300 oC for 1 hours in air and the final catalyst was denoted as 0.7Ru-NP/Mn2O3.

Au1/Mn2O3 catalysts

Mn2O3 supported Au1 single-atom catalyst (SACs) was prepared by impregnation on MnO2 and a subsequent calcination in which MnO2 decomposed to Mn2O3. Typically, 1 g MnO2 powder was dispersed in 2 mL deionized water with rigorous stirring. Appropriate amount of HAuCl4 solution (prepared by mixing 100 mg of HAuCl4•4H2O, and a certain amount of H2O) was added into 3 mL deionized water. The diluted HAuCl4 solution was added into the MnO2 solution at one time for another 5 h under vigorous stirring. The solution was filtrated, and the obtained filter cake was washed for three times by deionized water followed by drying at 120°C for 4 h and calcination at 500°C for 3 h in air, denoted as 0.1Au1/Mn2O3.

Au-NP/Mn2O3 catalysts

Au-NP/Mn2O3 catalyst containing Au NPs was prepared by deposing colloidal Au NPs onto the Mn2O3 surface. The typical process used 1 g Mn2O3 powder (from 1. Mn2O3 support) dispersed in 2 mL deionized water with rigorous stirring. Appropriate amount of colloidal HAuCl4 solution (prepared by mixing 100 mg of HAuCl4.4H2O, and a certain amount of H2O) were dropwise added into the Mn2O3 solution under stirring at 95 oC. Then added 5 times stoichiometric NaBH4 solution (prepared by mixing 5 times stoichiometric NaBH4 with 2 mL deionized water) at one time, and continued stirring until the H2O was evaporated. The Mn2O3 supported Au NPs were calcined at 300 oC for 1 hours in air and the final catalyst was denoted as 0.7Au-NP/Mn2O3.

In addition, catalysts 0.15Pd1/TiO2, 0.65Pd-NP/TiO2 were prepared following the procedures developed in the literature.[2]

Pd1/Mn2O3-PM and Pd-NP/Mn2O3-PM catalyst.

Physically grind Mn2O3 (200 mg) with Pd1/Mn2O3 (200 mg) to synthesis the Pd1/Mn2O3-PM.

Physically grind Mn2O3 (200 mg) with Pd-NP/Mn2O3 (200 mg) to synthesis the Pd-NP/Mn2O3-PM.

- Catalyst characterization

Metal loadings of the catalysts were measured by inductively coupled plasma spectrometry-atomic emission spectrometry (ICP-AES) on an IRIS Intrepid II XSP instrument (Thermo Electron Corporation). X-ray diffraction (XRD) patterns were collected on a PW3040/60 X’ Pert PRO (PANalytical) diffractometer equipped with a Cu Kα radiation source (λ = 0.15432 nm), operating at 40 kv and 40 mA. A continuous mode was used for collecting data in the 2θ range from 20o to 90o at a scanning speed of 5o/min. High-angel annual dark-field scan transmission electron microscopy (HAADF-STEM) analyses were performed with a JEM-2100F microscope operated at 200 kV. And the abreaction-corrected HAADF-STEM images were obtained on a JEOL JEM ARM microscope. For all microscopy analysis the samples were ultrasonically dispersed in ethanol and then a drop of the solution was put onto microgrid carbon polymer supported on copper grid.

X-ray photoelectron spectroscopy (XPS). XPS was measured on a Thermo ESCALAB 250Xi spectrometer equipped with an Al anode (Al Kα = 1846.6 eV), operated at 15 kV and 10.8 mA. The background pressure in the analysis chamber was lower than 1×10-8 Pa, and the operating pressure was around 7.1×10-5 Pa. The survey and spectra were acquired at a pass-energy of 20 eV. Energy calibration was carried out using the C1s peak of adventitious C at 284.6 eV.

In situ diffuse reflectance infrared Fourier transform spectra (DRIFTS). CO-DRIFTS were recorded with a Bruker Vertex 70 FT-IR spectrometer equipped with a mercury cadmium telluride (MCT) detector cooled by liquid nitrogen at a 4 cm-1 resolution over 32 scans. First, the samples were pretreated by 30 mL/min of 10 vol% H2 /He at 200 °C/0.5 h for Pd-NP sample and 80 °C/10 min for Pd SAC, then cooled to room temperature to collect a background spectrum. Subsequently, a 2 vol% CO/He flow was introduced until saturation coverage before purged with flowing helium to remove gas phase CO on the catalysts. Spectra were recorded in Kubelka Munk (KM) pattern throughout the entirety of experiments.

In situ Fourier transform infrared technique (FTIR). FTIR for acetophenone absorption was performed on a VERTEX 70V infrared spectrometer equipped with a mercury cadmium telluride (MCT) detector. Prior to the adsorption, the sample was pretreated under in O2/He for 0.5 h to remove water or trace impurities. The background spectrum was collected in ﬂowing O2 and automatically subtracted from the tested sample spectrum. The adsorption tests were conducted under 120 oC, in which the samples were exposed to mixed gases of acetophenone diluted in O2 until reached adsorption saturation.

The X-ray absorption spectroscopy (XAS). The X-ray absorption spectroscopy study was performed at the BL08B2* of SPring-8 (8 GeV, 100 mA), Japan, in which, the X-ray beam was monochromatized with water-cooled Si (111) double-crystal monochromator and focused with two Rh coated focusing mirrors with the beam size of 2.0 mm in the horizontal direction and 0.5 mm in the vertical direction around sample position, to obtain X-ray adsorption fine structure (XAFS) spectra both in near and extended edge.1 Pd foil and PdO samples were used as references. The catalysts and standard samples were measured with fluorescence and transmission mode, respectively. The spectra were analyzed and fitted using an analysis program Demeter.2 Before measurement, the Pd/TiO2 sample was reduced under 10 vol% H2/He at 200 and 600 °C for 0.5 h, followed by purging with pure He until cooled to room temperature.

Electron paramagnetic resonance (EPR). The measurements were carried out at 298 K using a Bruker A200 spectrometer.

- Catalytic activity testing and product analysis.

The ethylbenzene oxidation reactions were conducted in an autoclave equipped with a magnetic bar. In a typical procedure, a certain amount of catalyst, 2.2 mL substrate was subjected to the autoclave which was then flushed with 2 MPa O2 for five times and charged successively with 2 MPa O2. After the autoclave was sealed, it was heated to 120 oC for 20 h. After reaction, 2.0 mL dodecane was added in to the reactor as inner standard and diluted with ethyl acetate. The product was qualitatively analyzed by a gas chromatography-mass spectrometry (GC-MS), and quantitatively analyzed on an Agilent 7890B instrument equipped with an on-column injector (260 oC), an FID detector (325 oC) and an HP-5 capillary column (30 m × 0.32 mm × 0.25 mm). The conversion and selectivity were calculated by gas chromatography.

The conversion of ethylbenzene was calculated as following:

C=Nsa + Nap +  NbaNsa + Nap +  Nba +Neb×100%

where Nsa, Nap, Nba,  and Neb represent mole amount of α-phenethyl alcohol (styralyl alcohol), acetophenone, benzoic acid, and ethylbenzene, respectively.

The selectivity to acetophenone was calculated as following:

S=NapNsa + Nap + Nba ×100%

The conversion of acetophenone in acetophenone oxidation was calculated as following:

Cap= Nba Nap+ Nba ×100%

The conversion of acetophenone in acetophenone halogenation was calculated as following:

Cap'= NIa Nap +  NIa×100%

where NIa represent mole amount of iodoacetophenone. This calculation method is same with reported work[3].

The specific rate was calculated as following:

Specific Rate =Conversion of ethylbenzenetime ×Mole ratio of Pd/substrate ×100%

- Control experiments and mechanism investigations.

Ethylbenzene oxidation reactions by lattice oxygen on Pd1/Mn2O3 were conducted in a similar procedure except that the O2 was replaced with highly pure N2. Typically, 100 mg of Pd1/ Mn2O3 and 200 μL ethylbenzene were subjected into the autoclave. Then, the autoclave was flushed with 2 MPa N2 for five times and charged successively with 2 MPa N2. After the autoclave was sealed, it was heated to 180 oC for 20 h. After reaction, 2.0 mL dodecane was added in to the reactor as inner standard and diluted with ethyl acetate. The reaction was qualitatively analyzed by a GC-FID.

The ethylbenzene oxidation reactions by 18O2 were conducted in a similar procedure except that the 2 MPa O2 was replaced with 1 MPa 18O2. In a typical procedure, 50 mg catalyst, 2.2 mL substrate was subjected to the autoclave which was then flushed with 0.15 MPa N2 for five times and charged successively with 0.4 MPa 18O2. After the autoclave was sealed, it was heated to 120 oC for 12 h. After reaction, 2.0 mL dodecane was added in to the reactor as inner standard and diluted with ethyl acetate. The reaction was qualitatively analyzed by a GC-FID.

The acetophenone oxidation reactions by O2 were conducted in an autoclave equipped with a magnetic bar. In a typical procedure, 10 mg catalyst, 2 mL acetophenone and 1ml t-butylhydroperoxide were subjected to the autoclave which was then flushed with 2 MPa O2 for five times and charged successively with 2 MPa O2. After the autoclave was sealed, it was heated to 120 oC for 20 h. After reaction, 2.0 mL dodecane was added in to the reactor as inner standard and diluted with ethyl acetate. The reaction was qualitatively analyzed by a GC-FID.

The acetophenone halogenation reactions were conducted in an autoclave equipped with a magnetic bar. In a typical procedure, 150 mg catalyst, 2 g I2, 1 g CuO, 0.5 mL acetophenone and 5 mL dioxane were subjected to the autoclave. After the autoclave was sealed, it was heated to 120 oC for 8 h. 2.0 mL dodecane was added in to the reactor as inner standard and diluted with ethyl acetate. The reaction was qualitatively analyzed by a GC-MS and GC-FID.

The acetophenone deuterated reaction was conducted in a Sealed vessel equipped with a magnetic bar. In a typical procedure, 10 mg catalyst, 2.0 mmol AP and 2.0 mL CD3OD were subjected to the Sealed vessel. After the Sealed vessel was sealed, it was heated to 90 oC for 12 h. After reaction, the reaction mixture was subjected to centrifugation, the liquid was collected, and then subjected to rotary evaporation. The resulting products were analyzed using 1H NMR directly.

- Supplementary figures and tables

Figure S1. Powder XRD pattern of purchased uncalcined MnO2 (black line, approximate to akhtenskite MnO2, Jade card No.89-5171), calcined MnO2 (orang line, approximate to bixbyite Mn2O3, Jade card No. 89-4836), calcined Pd1/Mn2O3 (blue line) and Pd-NP/Mn2O3 (red line).

Figure S2. AC-HAADF-STEM images of Pd1/Mn2O3 with different magnifications (a-b), and HAADF-STEM images of Pd-NP/Mn2O3 with different magnifications (c-d).

Figure S3. Pd K-edge XANES spectra of Pd1/Mn2O3.

Figure S4. XPS of Pd1/Mn2O3 (red line) and Pd-NP/Mn2O3 (black line). The Pd single atoms in Pd1/Mn2O3 predominantly exists as Pd2+ (binding energy of 337.5 eV)

Figure S5. Catalyst recycling experiment for selective oxidation of EB on Pd1/Mn2O3 catalyst. Reaction conditions: EB (2.2 mL), catalyst, O2 (2 MPa), 120 oC, 20 h.

Figure S6. AC-HAADF-STEM images of 0.7Pd1/Mn2O3 catalysts.

Figure S7. (a) Pd K-edge XANES spectra of 0.7Pd1/Mn2O3, (b) The EXAFS spectra at the k2-weighted Fourier transform spectra of 0.7Pd1/Mn2O3 catalyst and reference samples.

Figure S8. AC-HAADF-STEM images of 0.1Au1/Mn2O3 (a-b), HR-STEM of 0.7AuNP/Mn2O3 (c-d), respectively.

Figure S9. AC-HAADF-STEM images of 0.1Ru1/Mn2O3 (a-b), and HR-STEM of 0.7Ru NP/Mn2O3(c-d), respectively.

Figure S10. AC-HAADF-STEM of 0.15Pd1/TiO2 (a-b), HR-STEM of 0.65Pd NP/TiO2 (c-d), respectively.

Figure S11. Proposed reaction mechanism of acetophenone to benzoic acid on Pd-NP/Mn2O3. Oxidation of enolate intermediate (Int 1) will produce ketoacid (Int 2), and decarboxylation on ketoacid (Int 2) is likely to react. Similar mechanism was reported in cyclohexane oxidation.[4]

Figure S12. 1H NMR for the AP deuterated reactions catalyzed by Pd1/Mn2O3 and Pd-NP/Mn2O3.

Figure S13. Electron Paramagnetic Resonance (EPR) of Pd1/Mn2O3 and Pd-NP/Mn2O3.

Table S1. EXAFS data fitting results of Pd1/Mn2O3.

| Samples | Shell | N | R (Å) | σ2x102 (Å2) | ΔE0 (eV) | r-factor (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Pd foil | Pd-Pd | 12.0 | 2.74 | 0.5 | 4.7 | 0.2 |
| PdO | Pd-O | 4.0 | 2.02 | 0.1 | -6.8 | 0.6 |
|  | Pd-Pd | 4.0 | 3.05 | 0.5 | -6.8 |  |
|  | Pd-Pd | 8.0 | 3.44 | 0.4 | -6.8 |  |
| Pd1/Mn2O3 | Pd-O | 3.5 | 2.02 | 0.1 | 1.5 | 0.8 |

N, the coordination number for the absorber-backscatterer pair. R, the average absorber-backscatterer distance. σ2, the Debye-Waller factor. ΔE0, the inner potential correction. The accuracies of the above parameters were estimated as N, ±20%; R, ±1%; σ2, ±20%.

Table S2. Performances of Pd/Mn2O3 catalyst compared with the active heterogenous catalysts reported for EB solvent-free oxidation by O2.

| Entry | Catalyst | Conv.(%) | Sel. of ketone (%) | Sel. of acid (%) | Specific rate (mol·molmetal-1·h-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Pd1/Mn2O3 | 15.6 | 66.2 | 0 | 6632[a] | This work |
| 2 | Pd-NP/Mn2O3 | 24.3 | 63.8 | 0 | 3469[a] | This work |
| 3[b] | HMS-Co (III) complex | 76 | 94 | 6 | 208 | Ref [5] |
| 4 | MnO4-1 exchanged Mg-Al hydrotalcite | 22.6 | 98.4 | --[c] | 9 | Ref [6] |
| 5 | NiAl hydrotalcite | 47 | 99.3 | -- | 0.4 | Ref [7] |
| 6 | 0.5%Pd@C-GluA | 14.2 | 94 | -- | 245 | Ref [8] |
| 7[d] | Au/LDH hybrid | 32.5 | 91.9 | -- | 1446 | Ref [9] |
| 8 | Mn-MgAl-hydrotalcite | 50.3 | 96.7 | -- | 25 | Ref [10] |
| 9 | Co-N-C/CeO2 | 33.1 | 74.8 | -- | 193 | Ref [11] |

[a] Specific rate was measured under 2 h reaction time with a lower conversion, 15.6% for Pd1/Mn2O3 and 24.3% for Pd-NP/Mn2O3, other reaction conditions are same with Table 1, Reaction conditions: EB (2.2 mL), catalyst, O2 (2 MPa)); [b] catalysts cannot be reused; [c] Not noted; [d] t-butyl hydroperoxide (TBHP, 3 mol% based on substrate) was added as initiator, only 5.3% conversion observed without TBHP.[9]

Table S3. EXAFS data fitting results of different 0.7Pd1/Mn2O3 samples.

| Samples | Shell | N | R (Å) | σ2x102 (Å2) | ΔE0 (eV) | r-factor (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Pd foil | Pd-Pd | 12.0 | 2.74 | 0.5 | 0.7 | 0.04 |
| PdO | Pd-O | 4.0 | 2.02 | 0.4 | -4.1 | 0.03 |
|  | Pd-Pd | 8.0 | 3.07 | 0.8 | -4.9 |  |
|  | Pd-Pd | 4.0 | 3.44 | 0.3 | -4.9 |  |
| 0.7Pd1/Mn2O3 | Pd-O | 3.4 | 2.01 | 0.3 | -5.6 | 0.7 |
|  | Pd-Pd | 1.2 | 3.10 | 0.4 | 11.7 |  |
|  | Pd-Mn | 3.0 | 3.38 | 0.4 | 11.7 |  |

N, the coordination number for the absorber-backscatterer pair. R, the average absorber-backscatterer distance. σ2, the Debye-Waller factor. ΔE0, the inner potential correction. The accuracies of the above parameters were estimated as N, ±20%; R, ±1%; σ2, ±20%.

Table S4. Low conversion rates experiment of EB and styralyl alcohol using O18 as the oxygen source.

| Entry | Catalyst | Substrate | Sel. of styralyl alcohol (%) | Sel. of AP (%) | Conv. (%) | 18O AP product | H216O |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 [a] | Pd1/Mn2O3 |  | 100 | N.D. | <1 | 96 [c] | -- |
| 2 [a] | Pd-NP/Mn2O3 |  | 100 | N.D. | <1 | 96 [c] | -- |
| 3 [b] | Pd1/Mn2O3 |  | - | 100 | <1 | N.D. [c] | 40% [d] |

[a] Reaction conditions: ethylbenzene, 2.2 mL; catalyst, 50 mg; P18O2 = 0.4 MPa; temperature, 120 °C; reaction time, 12 h. [b] Styralyl alcohol, 2.2 mL; P18O2 = 0.25 MPa. N.D.= not detected. [c] For organic products. [d] For H2O. In entry 1 and 2, styralyl alcohol marked by 18O were detected as the main production, while trace amount 16O styralyl alcohol were detected which might be ascribe to the impurity of 18O2 (96%). As a comparison, styralyl alcohol oxidation in entry 3, which has been generally regarded to follow Mars-van-Krevelen mechanism,[12] was detected unnegligible amount of H216O (about two-fifths of H2O). All substrates were treated with Magnesium sulfate anhydrous to remove H216O before reaction.

Table S5. Direct oxidation experiments of acetophenone with or without TBHP.

| Entry | Catalyst | Catalyst (mg) | TBHP (mL) | AP (mL) | Benzoic Acid (%) |
| --- | --- | --- | --- | --- | --- |
| 1a | Pd1/Mn2O3 | 50 | 0 | 0.5 | 0 |
| 2a | Pd-NP/Mn2O3 | 50 | 0 | 0.5 | 0 |
| 3a | Pd1/Mn2O3 | 10 | 1.0 | 1.0 | 2.1 |
| 4b | Pd-NP/Mn2O3 | 10 | 1.0 | 1.0 | 85.4 |
| 5b | Pd1/Mn2O3 | 10 | 2.0 | 0.1 | 0 |
| 6b | Pd-NP/Mn2O3 | 10 | 2.0 | 0.1 | 0 |

aReaction conditions: PO2=2 MPa; temperature, 120 °C; reaction time, 12 h. b1 atm air.

Table S6. Performance of various SACs in ethylbenzene oxidation.

| Entry | Catalyst | Conv. (%) | Sel. Of PA (%) | Sel. Of AP (%) | Sel. Of BA (%) |
| --- | --- | --- | --- | --- | --- |
| 1a | 0.1Au1/Mn2O3 | 46 | 7 | 93 | 0 |
| 2a | 0.7AuNPs/Mn2O3 | 48 | 5 | 86 | 8 |
| 3a | 0.1Ru1/Mn2O3 | 50 | 5 | 95 | 0 |
| 4a | 0.7RuNPs/Mn2O3 | 45 | 4 | 85 | 11 |
| 5b | 0.15Pd1/TiO2 | 16% | 18 | 82 | 0 |
| 6b | 0.65PdNPs/TiO2 | 45% | 2 | 32 | 63 |
| aReaction conditions: aEB (2.2 mL), catalyst (10 mg), O2 (2 MPa), 120 oC, 20 h. b EB (2.0 mmol), catalyst (20 mg), O2 (1.0 MPa), MeCN (5.0 mL), 120 oC, 20 h. |  |  |  |  |  |

Table S7. Performance of Pd1/Mn2O3-PM and Pd-NP/Mn2O3-PM in ethylbenzene oxidation.

| Entry | Catalyst (Pd/EB) | Conv. | Sel. of PA | Sel. of AP | Sel. of BA |
| --- | --- | --- | --- | --- | --- |
| 1a | Pd1/Mn2O3-PM (12 ppm) | 43% | 11% | 89% | 0% |
| 2b | Pd-NP/Mn2O3-PM (35 ppm) | 69% | 3% | 9% | 88% |
| Reaction conditions: aEB (2.2 mL), Pd1/Mn2O3-PM (60 mg), Mn2O3 (20 mg), O2 (2.0 MPa), 120 oC, 20 h. bEB (2.2 mL), catalyst, O2 (2.0 MPa), 120 oC, 20 h. bPd-NP/Mn2O3-PM (20 mg). |  |  |  |  |  |

- References

[1]	a) Y. Wang, J. W. Ren, K. Deng, L. L. Gui, Y. Q. Tang, Chemistry of Materials 2000, 12, 1622-1627; b) L. Yin, M. A. El-Sayed, J.phys.chem.b 2001, 105.

[2]	Y. Guo, Y. Huang, B. Zeng, B. Han, M. Akri, M. Shi, Y. Zhao, Q. Li, Y. Su, L. Li, Q. Jiang, Y.-T. Cui, L. Li, R. Li, B. Qiao, T. Zhang, Nature Communications 2022, 13, 2648.

[3]	M. M. Peng, M. Ganesh, R. Vinodh, M. Palanichamy, H. T. Jang, Arab. J. Chem. 2019, 12, 1358-1364.

[4]	D. Pan, G. Li, Y. Su, H. Wei, Z. Luo, Chinese Journal of Chemical Engineering 2021, 29, 183-189.

[5]	B. K. Das, J. H. Clark, Chemical Communications 2000, 605-606.

[6]	V. Choudhary, J. Indurkar, V. Narkhede, R. Jha, Journal of Catalysis 2004, 227, 257-261.

[7]	S. K. Jana, P. Wu, T. Tatsumi, Journal of Catalysis 2006, 240, 268-274.

[8]	P. Zhang, Y. Gong, H. Li, Z. Chen, Y. Wang, Nature Communications 2013, 4, 1593.

[9]	L. Wang, Y. Zhu, J. Q. Wang, F. Liu, J. Huang, X. Meng, J. M. Basset, Y. Han, F. S. Xiao, Nat Commun 2015, 6, 6957.

[10]	S. K. Jana, Y. Kubota, T. Tatsumi, Journal of Catalysis 2007, 247, 214-222.

[11]	Y. Chen, S. Zhao, Z. Liu, Physical Chemistry Chemical Physics 2015, 17.

[12]	T. Li, F. Liu, Y. Tang, L. Li, S. Miao, Y. Su, J. Zhang, J. Huang, H. Sun, M. Haruta, Angewandte Chemie International Edition 2018.