Table 1 Catalytic performance of Mn2O3-supported Pd catalysts in selective oxidation of EBa.

| Entry | Catal. | Pd/EB (ppm) | Conv. of EB | Sel. of PA | Sel. of AP | Sel. of BA |
| --- | --- | --- | --- | --- | --- | --- |
| 1b | Mn2O3 | 0 | 13% | 27% | 73% | 0% |
| 2 | Pd-NP/Mn2O3 | 35 | 71% | 4% | 8% | 88% |
| 3c | Pd-NP/Mn2O3 | 35 | 55% | 10% | 68% | 22% |
| 4 | Pd1/Mn2O3 | 12 | 41% | 13% | 87% | 0% |
| 5d | Pd1/Mn2O3 | 12 | 63% | 6% | 94% | 0% |
| aReaction conditions: EB (2.2 mL), catalyst, O2 (2 MPa), 120 oC, 20 h. b10 mg Mn2O3. c8 h. d40 h. |  |  |  |  |  |  |

Table 2. Selective C−H bond oxidation on Pd1/Mn2O3 catalysts for diverse hydrocarbon substrates.

| Entrya | Substrate | Products | Conv. (%) | Sel. (%) |
| --- | --- | --- | --- | --- |
| 1 |  |  | 41 | 89 |
| 2 |  |  | 82 | 92 |
| 3 |  |  | 49 | 93 |
| 4 |  |  | 42 | 93 |
| 5 |  |  | 99 | 99 |
| 6 |  |  | 68 | 100 |
| 7b |  |  | 90 | 100 |
| 8c |  |  |  |  |
| 9c |  |  |  |  |
| aReaction conditions: substrate (2.2 mL), Pd1/Mn2O3 (10 mg), O2 (2.0 MPa), 120 °C; 20 h. bPd-NP/Mn2O3 as the catalyst. c5 mmol of cyclohexane, 1 mol% of N-hydroxyphthalimide, 30 mg of the catalyst, 15 mL of acetonitrile as the solvent, 1.0 MPa of O2, 120 °C; 12 h. |  |  |  |  |