Supporting Information

Aramid Nanofibers at Ultralow Loadings: Driving Significant Multifunctionality in Epoxy Composite Dielectrics

Haowen Yuan1,2, Zi Wang1, Zicheng Zang1, Qingzhou Wu3, Guoqing Jiang1, Huachao Wei1, Yiyi Zhang2, Jiajia Zheng4, Junwen Ren1,*, Guanglei Wu5,*, Shenli Jia1

1College of Electrical Engineering, Sichuan University, Chengdu 610065, P.R. China

2Guangxi Power Transmission and Distribution Network Lightning Protection Engineering Technology Research Center, Guangxi University, Nanning 530000, P.R. China

3Key Laboratory of Pulsed power, Institute of Fluid Physics, CAEP, Mianyang 621900, P.R. China

4Key Laboratory of Standardization and Measurement for Nanotechnology, National Center for Nanoscience and Technology, Beijing 100190, P.R. China

5Institute of Materials for Energy and Environment, State Key Laboratory of Bio-fibers and Eco-textiles, College of Materials Science and Engineering, Qingdao University, Qingdao 266071, P.R. China;

* Corresponding author.

E-mail: myboyryl@scu.edu.cn/jwren_scu@163.com (J. Ren); wuguanglei@qdu.edu.cn (G. Wu)

Fig S1. AFM images of ANFs exfoliated for (a)1 day, (b)3 days, (c)5 days and (d)7 days.

Fig S2. Volume electrical resistivity of neat epoxy film and ANF/Epoxy composite dielectrics films

Table S1. Values of the scales parameter estimators E and of the shape estimator parameter β.

| Samples | E (kV/mm) | β |
| --- | --- | --- |
| Neat Epoxy | 47.71 | 17.1 |
| ANFs/Epoxy-0.025wt% | 87.22 | 2.3 |
| ANFs/Epoxy-0.05wt% | 105.93 | 4.5 |
| ANFs/Epoxy-0.075wt% | 160.94 | 3.9 |
| ANFs/Epoxy-0.1wt% | 196.85 | 3.2 |

Table S2. Toughness and its corresponding growth rate of the ANF/EP composites.

| Samples | Toughness (MJ/m3) | Enhancement (%) |  |
| --- | --- | --- | --- |
| Neat Epoxy | 71.44 |  | / |
| ANFs/Epoxy-0.025wt% | 84.93 |  | 18.87 |
| ANFs/Epoxy-0.05wt% | 94.22 |  | 31.88 |
| ANFs/Epoxy-0.075wt% | 146.27 |  | 104.73 |
| ANFs/Epoxy-0.1wt% | 188.41 |  | 163.71 |

Table S3. TGA characteristic temperatures of neat epoxy and ANF/EP composites.

| Samples | T5% (℃) | T30% (℃) | THRI (℃) |
| --- | --- | --- | --- |
| Neat Epoxy | 368.67 | 411.17 | 193.14 |
| ANFs/Epoxy-0.025wt% | 364.33 | 410.33 | 192.05 |
| ANFs/Epoxy-0.05wt% | 369.00 | 409.17 | 192.62 |
| ANFs/Epoxy-0.075wt% | 365.33 | 410.50 | 192.29 |
| ANFs/Epoxy-0.1wt% | 375.33 | 414.17 | 195.33 |

The THRI of the composites can be calculated and measured by thefollowing formula

where THRI is the heat resistance index temperature, which characterizes the heat resistance performance of the material; T5% is the initial thermal decomposition temperature corresponding to 5% weight loss of the sample; and T30% is the temperature corresponding to 30% weight loss of the sample.

Table S4. Values of the scales parameter estimators E and of the shape estimator parameter β.

| Samples | E (kV/mm) | β |
| --- | --- | --- |
| Neat Epoxy | 47.7 | 17.1 |
| ANF1d/Epoxy | 28.2 | 7.2 |
| ANF3d/Epoxy | 71.62 | 10.5 |
| ANF5d/Epoxy | 176.9 | 4.9 |
| ANF7d/Epoxy | 196.2 | 3.2 |