Supplementary Information

Minimized Optical/Electrical Energy Loss for 25.1% Monolithic Perovskite/Organic Tandem Solar Cells

Zhangwei He1, Runnan Yu1,*, Yiman Dong1, Ruyue Wang1, Yuling Zhang1, Zhan’ao Tan1,*

1Beijing Advanced Innovation Center for Soft Matter Science and Engineering, Beijing University of Chemical Technology, Beijing, 100029, China.

*Corresponding author: yurunnan@mail.buct.edu.cn, tanzhanao@mail.buct.edu.cn

Supplementary Fig. 1. The high-resolution XPS spectra of Cs 3d for the pristine and PBP-treated perovskite films.

Supplementary Fig. 2. Histogram of PL peak intensity distribution (extracted from PL mapping data).

Supplementary Fig. 3. SCLC curves of electron-only devices with the structure of ITO/SnO2/perovskite/C60/BCP/Ag and hole-only devices with the structure of ITO/PEDOT:PSS/perovskite/Spiro-MeOTAD/MoO3/Ag.

Supplementary Fig. 4. J–V characteristics of the electron-only and hole-only devices with and without PBP treatment.

Supplementary Fig. 5. TRPL spectra of perovskite films with or without PBP treatment.

Supplementary Fig. 6. Nyquist plots of PerSCs with and without PBP treatment measured in the dark condition. The inset shows the equivalent circuit.

Supplementary Fig. 7. Dark J−V characteristics of PerSCs with and without PBP treatment.

Supplementary Fig. 8. VOC and JSC dependence on the light intensity of the PerSCs with and without PBP treatment.

Supplementary Fig. 9. J–V curves of the PerSCs with different concentrations of PBP treatment.

Supplementary Fig. 10. Calculations of the bandgap of PerSCs with PBP treatment by the derivative of the EQE spectra.

Supplementary Fig. 11. Photovoltaic performance of PerSCs with and without PBP treatment, including VOC, FF, JSC, and PCE.

Supplementary Fig. 12. Operational stability of encapsulated PerSCs with and without PBP treatment under LED illumination.

Supplementary Fig. 13. Thermal stability of unencapsulated PerSCs with and without PBP treatment at 65 °C fixed temperature in N2 atmosphere.

Supplementary Fig. 14. UPS spectra of the V2O5 film.

Supplementary Fig. 15. Tauc plots of V2O5 films.

Supplementary Fig. 16. Energy level alignment of the materials involved in the TSCs.

Supplementary Fig. 17. The chemical structures of the donor and acceptor materials in the OSCs.

Supplementary Fig. 18. Absorption and transmittance spectra of the MoO3 and V2O5 films.

Supplementary Fig. 19. Normalized TPC decay curves and TPV decay curves of MoO3-based and V2O5-based OSCs.

Supplementary Fig. 20. Photocurrent density versus effective voltage curves for OSCs.

Supplementary Fig. 21. AFM images of the MoO3, V2O5, MoO3/BHJ and V2O5/BHJ layers.

Supplementary Fig. 22. Contact angle images of water and diiodomethane on MoO3/PM6, MoO3/BTP-eC9, MoO3/BHJ, V2O5/PM6, V2O5/BTP-eC9 and V2O5/BHJ layers.

Supplementary Fig. 23. J–V curves of the MoO3-based and V2O5-based OSCs with different thicknesses.

Supplementary Fig. 24. Photovoltaic performance of MoO3-based and V2O5-based OSCs, including FF, VOC, JSC, and PCE.

Supplementary Fig. 25. J–V curves of the perovskite/organic TSCs with different thicknesses of MoO3-based and V2O5-based ICL.

Supplementary Fig. 26. Statistics of FF, VOC and JSC for 30 perovskite/organic TSCs with MoO3-based and V2O5-based ICLs over different batches.

Supplementary Table 1. Decay lifetime of the perovskite films with and without PBP treatment.

| Sample | A1 | τ1 (ns) | A1 | τ2 (ns) | τavg (ns) |
| --- | --- | --- | --- | --- | --- |
| W/O PBP | 659.6 | 50.0 | 1305.7 | 204.3 | 187.3 |
| With PBP | 246.8 | 102.3 | 1572.4 | 563.0 | 550.2 |

Supplementary Table 2. EIS fitting parameters of PerSCs with and without PBP treatment measured under dark conditions.

| Sample | Rs (Ω) | Rct (Ω) | Rrec (Ω) | Cct (F) | Crec (F) |
| --- | --- | --- | --- | --- | --- |
| W/O VM | 213.8 | 9.60 × 104 | 7.64 × 105 | 1.20 × 10−9 | 3.64 × 10−9 |
| With VM | 43.36 | 6.32 × 104 | 1.12 × 106 | 1.35 × 10−9 | 4.33 × 10−9 |

Supplementary Table 3. Photovoltaic parameters of PerSCs with different concentrations of PBP treatment.

| Sample | Scan direction | VOC (V) | FF (%) | JSC (mA cm−2) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| 0.3 mg/mL PBP | forward | 1.30 | 78.1 | 17.56 | 18.19 |
| 0.3 mg/mL PBP | reverse | 1.31 | 80.6 | 17.21 | 17.88 |
| 0.5 mg/mL PBP | forward | 1.32 | 78.9 | 17.66 | 18.42 |
| 0.5 mg/mL PBP | reverse | 1.32 | 80.3 | 17.70 | 18.76 |
| 0.7 mg/mL PBP | forward | 1.30 | 77.0 | 17.66 | 17.71 |
| 0.7 mg/mL PBP | reverse | 1.30 | 78.2 | 17.68 | 18.01 |

Supplementary Table 4. The best photovoltaic parameters of PerSCs with and without PBP treatment.

| Sample | Scan direction | VOC (V) | FF (%) | JSC (mA cm−2) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| W/O PBP | Forward | 1.29 | 76.3 | 17.53 | 17.28 |
|  | Reverse | 1.29 | 77.6 | 17.59 | 17.73 |
| With PBP | Forward | 1.32 | 79.4 | 17.60 | 18.39 |
|  | Reverse | 1.33 | 81.2 | 17.72 | 19.08 |

Supplementary Table 5. Parameters of water and diiodomethane contact angles for donor, acceptor, and blend films on MoO3 and V2O5.

| Surface | θWater (°) | θDiiodomethane (°) | γ (mN m−1) | χD−A (%) |
| --- | --- | --- | --- | --- |
| MoO3/PM6 | 101.1 | 50.3 | 35.4 | 0.2 |
| MoO3/BTP-eC9 | 98.1 | 40.6 | 40.9 |  |
| V2O5/PM6 | 105.5 | 53.4 | 34.4 | 0.3 |
| V2O5/BTP-eC9 | 71.5 | 42.5 | 41.3 |  |
| MoO3/Blend | 101.0 | 49.5 | 35.9 |  |
| V2O5/Blend | 106.1 | 46.5 | 39.5 |  |

Supplementary Table 6. Photovoltaic parameters of OSCs with different thicknesses of MoO3 and V2O5 HTL.

| Sample | VOC (V) | FF (%) | JSC (mA cm−2) | PCE (%) |
| --- | --- | --- | --- | --- |
| 15 nm MoO3 | 0.837 | 72.0 | 26.90 | 16.21 |
| 20 nm MoO3 | 0.840 | 72.1 | 26.75 | 16.20 |
| 25 nm MoO3 | 0.838 | 72.4 | 26.43 | 16.02 |
| 10 nm V2O5 | 0.838 | 74.7 | 27.50 | 17.21 |
| 15 nm V2O5 | 0.840 | 75.4 | 27.29 | 17.28 |
| 20 nm V2O5 | 0.842 | 74.7 | 26.93 | 16.94 |

Supplementary Table 7. The photovoltaic parameters of TSCs with different thicknesses of MoO3-based and V2O5-based ICLs.

| Sample | Scan direction | VOC (V) | FF (%) | JSC (mA cm−2) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| 15 nm MoO3 | forward | 2.08 | 70.7 | 14.54 | 21.32 |
| 15 nm MoO3 | reverse | 2.09 | 75.2 | 14.33 | 22.50 |
| 20 nm MoO3 | forward | 2.06 | 74.1 | 14.42 | 22.05 |
| 20 nm MoO3 | reverse | 2.07 | 77.7 | 14.41 | 23.20 |
| 25 nm MoO3 | forward | 2.08 | 70.9 | 14.21 | 20.95 |
| 25 nm MoO3 | reverse | 2.09 | 73.7 | 14.21 | 21.90 |
| 10 nm V2O5 | forward | 2.08 | 76.4 | 14.63 | 23.27 |
| 10 nm V2O5 | reverse | 2.10 | 79.7 | 14.82 | 24.83 |
| 15 nm V2O5 | forward | 2.08 | 75.6 | 14.65 | 23.02 |
| 15 nm V2O5 | reverse | 2.10 | 81.1 | 14.68 | 25.07 |
| 20 nm V2O5 | forward | 2.08 | 74.9 | 14.39 | 22.39 |
| 20 nm V2O5 | reverse | 2.10 | 79.7 | 14.35 | 24.04 |