Supplementary Material

Supporting Information for

Adsorption of strontium ions on bentonite and phyllite - effect of environmental conditions

Kyziol-Komosińska J. 1) , Janeczek J.2) , Dzieniszewska A. 1), Fabiańska M. 2), Czupiol J. 1), Krzątała A.2), Pająk M. 1)

1) Institute of Environmental Engineering Polish Academy of Sciences, 34 M. Skłodowska-Curie St., 41-819 Zabrze, Poland;

2) Faculty of Natural Sciences, University of Silesia, 60 Będzińska St., 41-200 Sosnowiec, Poland

Table 1S. Isotherms equations

| Isotherm model | Equation | Parameters | Eq. |
| --- | --- | --- | --- |
| Freundlich |  | KF – Freundlich isotherm constant ((mg/g)·(L/mg)1/n) and it is an approximate indicator of sorption capacity. 1/n – a function of the strength of sorption in the sorption process | 1S. |
| Langmuir |  | qL – maximum monolayer coverage capacity (mg/g). KL – Langmuir isotherm constant related to the affinity of binding sited (L/mg). | 2S. |
| Dubinin-Radushkevich | q=qD.exp(-βε2) | qD – the sorption capacity of studied minerals for Eu(III) (mol/g). β – the constant (mol2/J2). ε – the Polanyi potential (J/mol) which is equal to . R – the gas constant (8.314 J/mol K). T – absolute temperature (K). E= – free energy (E) of the adsorption (kJ/mol) | 3S. 4S. |
| Sips | q=qsKsCeqms1+KsCeqms | qs – Sips maximum sorption capacity (mg/g). KS – the Sips equilibrium constant (L/mg)m. mS – the Sips model exponent | 5S. |

Table 2S. List of error function

| Error function | Abbreviation | Expression | Eq. |
| --- | --- | --- | --- |
| Sum squares error | SSE |  | 6S. |
| Nonlinear chi-square test | χ2 |  | 7S. |

‘‘meas’’ and ‘‘calc’’ show the measured and calculated values. n is the number of observations in the experimental data.

SEM/EDS analysis

BENTONITE

Before Sr adsorption

Ca (atomic %) 0.65 – 1.08, mean 0.927±0.131

Sr (atomic %)  0.11 – 0.29, mean 0.209±0.043

Sr/Ca 0.274±0.075

After Sr adsorption

Ca (atomic %) 0.27 – 0.77, mean 0.68±0.157

Sr (atomic %)  0.73 – 1.00, mean 0.835±0.066

Sr/Ca 1.895±0.324

Fig. 1S. SEM/EDS analysis of Ca and Sr on the bentonite surface (A - before and B - after Sr adsorption)

PHYLLITE

Before Sr adsorption

Ca (atomic %) 0.03 – 0.14, mean 0.0712±0.03

Sr (atomic %)  0.01 – 0.22, mean 0.134±0.067

Sr/Ca 1.952±1.952±1.341

After Sr adsorption

Ca 0.01 – 0.14, mean 0.0625±0.0364

Sr  0.06 – 0.31, mean 0.183±0.083

Sr/Ca 4.121±0.289

Fig. 2S. SEM/EDS analysis of Ca and Sr on the phyllite surface (A - before and B - after Sr adsorption)

Table 3S. The isotherm constants for the adsorption of Sr(II) ions onto bentonite and phyllite

|  | B |  |  |  |  |  | Phy |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | IS 0 M, L:S 100:1 |  | IS 0.1 M, L:S 100:1 |  | IS 0 M, L:S 500:1 | IS 0.1 M, L:S 500:1 | IS 0 M, L:S 100:1 | IS 0.1 M, L:S 100:1 | IS 0 M, L:S 500:1 | IS 0.1 M, L:S 500:1 |
| Freundlich isotherm |  |  |  |  |  |  |  |  |  |  |
| 1/n | 0.4406 |  | 0.8596 |  | 0.3279 | 0.6318 | 0.4482 | 0.8397 | 0.4505 | 0.6215 |
| KF | 2.463 |  | 0.2062 |  | 6.110 | 1.088 | 0.3139 | 0.0275 | 1.006 | 0.2856 |
| R2 | 0.9843 |  | 0.9856 |  | 0.9705 | 0.9480 | 0.9931 | 0.9981 | 0.9666 | 0.9641 |
| SSE | 4.154 |  | 1.397 |  | 9.391 | 4.131 | 0.089 | 0.0068 | 5.321 | 2.651 |
| χ2 | 1.696 |  | 0.477 |  | 3.374 | 1.361 | 0.211 | 0.043 | 1.475 | 1.639 |
| Langmuir isotherm |  |  |  |  |  |  |  |  |  |  |
| q | 14.25 |  | 10.19 |  | 28.20 | 23.21 | 3.00 | 2.10 | 9.41 | 6.69 |
| qL | 17.21 |  | 34.32 |  | 30.13 | 38.33 | 3.641 | 7.52 | 12.02 | 10.81 |
| KL | 0.0759 |  | 0.0044 |  | 0.0875 | 0.0118 | 0.0242 | 0.0022 | 0.0238 | 0.0097 |
| R2 | 0.9952 |  | 0.9922 |  | 0.9931 | 0.9807 | 0.9898 | 0.9994 | 0.9953 | 0.9887 |
| SSE | 1.263 |  | 0.774 |  | 3.246 | 5.63 | 0.132 | 0.0236 | 0.836 | 0.830 |
| χ2 | 2.037 |  | 0.225 |  | 2.472 | 1.561 | 0.489 | 0.0531 | 1.228 | 0.592 |
| Dubinin-Raduskevich isotherm |  |  |  |  |  |  |  |  |  |  |
| qD (mmol/g) | 0.629 |  | 1.62 |  | 0.761 | 1.489 | 0.123 | 0.305 | 0.367 | 0.421 |
| β | 0.00411 |  | 0.00626 |  | 0.00317 | 0.00667 | 0.00561 | 0.00607 | 0.00493 | 0.00708 |
| E | 11.09 |  | 8.94 |  | 12.56 | 8.66 | 9.44 | 9.07 | 10.07 | 8.41 |
| R2 | 0.9929 |  | 0.9925 |  | 0.9885 | 0.9706 | 0.9913 | 0.9988 | 0.9801 | 0.9771 |
| SSE | 1.882 |  | 1.011 |  | 2.262 | 2.196 | 0.321 | 0.0071 | 3.261 | 1.706 |
| χ2 | 0.451 |  | 0.750 |  | 1.571 | 1.317 | 0.315 | 0.1249 | 0.667 | 0.973 |
| Sips isotherm |  |  |  |  |  |  |  |  |  |  |
| qs |  | 20.48 |  | 14.27 | 34.86 | 25.18 | 5.908 | 6.168 | 11.32 | 7.381 |
| Ks |  | 0.0889 |  | 0.0020 | 0.1296 | 0.0025 | 0.0376 | 0.0022 | 0.0182 | 0.00127 |
| ms |  | 0.7959 |  | 1.550 | 0.7221 | 1.894 | 0.649 | 1.0512 | 1.112 | 1.701 |
| R2 |  | 0.9971 |  | 0.9995 | 0.9981 | 0.9995 | 0.9983 | 0.9995 | 0.9958 | 0.9993 |
| SSE |  | 0.769 |  | 0.2731 | 0.604 | 0.059 | 0.0227 | 0.0236 | 0.533 | 0.0501 |
| χ2 |  | 0.345 |  | 0.333 | 0.449 | 0.288 | 0.0307 | 0.0534 | 1.673 | 1.103 |

Table 4S. Sr distribution coefficient values (L/g)

| L:S | C0 | IS 0.01 M NaCl, pH 3 – 8 | IS 0.1 M NaCl, pH 3 – 8 |  |  | IS 0.5 M NaCl, pH 3 – 8 |
| --- | --- | --- | --- | --- | --- | --- |
| Bentonite |  |  |  |  |  |  |
| 100:1 | 1 mg/L | 0.534 – 10.39 | 0.105 – 0.221 |  |  | 0.022- 0.128 |
| 500:1 | 1 mg/L | 0.972 – 12.88 | 0.245 – 0.901 |  |  | 0.116 – 0.244 |
| 100:1 | 10 mg/L | 0.514 – 1.02 | 0.065 – 0.134 |  |  | 0.011 – 0.0354 |
| 500:1 | 10 mg/L | 0.826 – 2.55 | 0.159 – 0.355 |  |  | 0.092 – 0.283 |
| 100:1 | 100 mg/L | 0.226 – 0.329 | 0.042 – 0.115 |  |  | 0.009 – 0.0271 |
| 500:1 | 100 mg/L | 0.227 – 0.363 | 0.101 - 0.227 |  |  | 0.0026 – 0.0532 |
| Phyllite |  |  |  |  |  |  |
| 100:1 | 1 mg/L | 0.101 – 0.218 | 0.007 – 0.0232 |  |  | 0.0008 – 0.00225 |
| 500:1 | 1 mg/L | 0.132 – 0.374 | 0.016 – 0.0641 |  |  | 0.0026 – 0.0069 |
| 100:1 | 10 mg/L | 0.0186 – 0.0623 | 0.0033 – 0.0172 |  |  | 0.0007 – 0.0016 |
| 500:1 | 10 mg/L | 0.074 – 0.241 | 0.0093 – 0.0531 |  |  | 0.0023 – 0.0047 |
| 100:1 | 100 mg/L | 0.0041 – 0.0161 | 0.0014 – 0.0104 |  |  | 0.00099 – 0.0014 |
| 500:1 | 100 mg/L | 0.0018 – 0.0987 | 0.0051 – 0.0376 |  |  | 0.0018 – 0.00237 |
| L:S | C0 | IS 0 M, pH 8.0 |  | IS 0.1 M, pH 8.0 |  |  |
| Bentonite |  |  |  |  |  |  |
| 100:1 | 0.01-200 mg/L | 7.153 – 0.0554 |  | 0.0812 – 0.1575 – 0.0462 |  |  |
| 500:1 | 0.01-200 mg/L | 42.168 – 0.04585 |  | 0.1036 – 0.3905 - 0.0597 |  |  |
| Phyllite |  |  |  |  |  |  |
| 100:1 | 0.01-200 mg/L | 0.9992 – 0.00555 |  |  | 0.01264 – 0.01539 – 0.00813 |  |
| 500:1 | 0.01-200 mg/L | 1.2313 – 0.0382 |  |  | 0.0292 – 0.0895 – 0.0591 |  |