2D single-faceted IrO2(101) monolayer enabling high-performing proton exchange membrane water electrolysis beyond 8,000 h stability at 1.5 A cm-2

Deren Yang1*, Chunyang Zhang1, Yufeng Qin1, Xiaoyun Shi1, Kang Hua1, Xuemin An1, Yubo Liu1, Yang Yue1, Louyu Jin1, Yipeng Zhang1, Shouwei Zuo2*, Aidong Tan1* and Jianguo Liu1*

1Institute of Energy Power Innovation, North China Electric Power University, 2 Beinong Road, Beijing 102206, P. R. China. 2Beijing Synchrotron Radiation Facility, Institute of High Energy Physics, Chinese Academy of Sciences, Beijing 100049, P. R. China.

Deren Yang and Chunyang Zhang contributed equally to this work.

*E-mail: jianguoliu@ncepu.edu.cn; yangderen@ncepu.edu.cn

Supplementary Fig. 1 The PDOS plots of the exposed Ir atoms in the (110), (200) and (101) facets, respectively.

50 nm

200 nm

100 nm

100 nm

Supplementary Fig. 2 TEM images of 2D IrO2(101) monolayer

N

O

Ir

a

b

Supplementary Fig. 3 (a) STEM image of IrO2(101) monolayer, (b) distribution of Ir, O and N along the blue line in (a).

Supplementary Fig. 4 EDX spectrum of IrO2(101) monolayer.

Supplementary Fig. 5 AFM image in 3D form of IrO2(101) monolayer.

IrO2(101) monolayer

IrO2 NP

C-IrO2 (Alfa Aesar)

C-IrO2 (Umicore)

Supplementary Fig. 6 Photos taken by IrO2(101) monolayer, IrO2 NP, C-IrO2 (Alfa Aesar) and C-IrO2 (Umicore) on weighing paper.

b

a

Supplementary Fig. 7 (a) Ir 4f, (b) O 1s XPS spectra of IrO2 NP.

Supplementary Fig. 8 Pore diameter distribution of IrO2(101) monolayer, IrO2 NP and C-IrO2. Inset shows the pore diameter distribution from 2 to 8 nanometers.

Supplementary Fig. 9 XRD patterns of IrO2 synthesized with 0 g, 3.2 g, 6.4 g and 12.8 g ammonia, respectively.

b

a

200 nm

c

d

500 nm

200 nm

200 nm

Supplementary Fig. 10 TEM images of IrO2 synthesized with (a) 0 g, (b) 3.2 g, (c) 6.4 g and (d) 12.8 g ammonia, respectively.

Supplementary Fig. 11 XRD patterns of IrO2 synthesized at different calcination temperatures.

Supplementary Fig. 12 TEM images of IrO2 synthesized at (a) 350 ℃ and (b) 550 ℃.

b

a

Supplementary Fig. 13 Calibration of the saturated calomel electrode (SCE) electrode with respect to reversible hydrogen electrode (RHE) in a) 0.1 M HClO4 and b) 0.5 M H2SO4 aqueous electrolytes bubbled with pure hydrogen gas at room temperature. Scan rate: 1 mV s-1.

a

b

Supplementary Fig. 14 Comparison of overpotential at (a) 10 mA cm-2 and (b) 50 mA cm-2 for IrO2(101) monolayer, IrO2 NP, C-IrO2, and C-Ir black.

Supplementary Fig. 15 EIS curves of IrO2(101) monolayer, IrO2 NP, C-IrO2, and C-Ir black in O2-saturated 0.1 M HClO4 electrolyte.

b

a

Supplementary Fig. 16 Adhesion test of membrane electrodes to bubbles with (a) IrO2(101) monolayer, (b) IrO2 NP and C-IrO2, bubbles contact membrane electrode at position 1, are compressed to maximum extent at position 2, and are detached from membrane electrode at position 3.

b

a

Supplementary Fig. 17 Comparison of (a) geometric activities, (b) ECSA-based activities at 1.50 V vs. RHE for IrO2(101) monolayer, IrO2 NP, C-IrO2, and C-Ir black.

a

b

c

d

Supplementary Fig. 18 CV curves at different sweep speeds of (a) IrO2(101) monolayer and (c) Clean GC, CDL fitting curves of (b) IrO2(101) monolayer and (d) Clean GC in O2-saturated 0.5 M H2SO4 electrolyte.

f

e

d

c

b

a

Supplementary Fig. 19 CV curves at different sweep speeds of (a) IrO2 NP, (c) C-IrO2 and (e) C-Ir black, CDL fitting curves of (b) IrO2 NP, (d) C-IrO2 and (f) C-Ir black in O2-saturated 0.5 M H2SO4 electrolyte.

c

d

a

b

Supplementary Fig. 20 (a) Polarization curves, (b) Tafel plots, (c) Mass activisities at 1.5 V vs RHE and (d) EIS curves of IrO2(101) monolayer, IrO2 NP, C-IrO2, and C-Ir black in O2-saturated 0.5 M H2SO4 electrolyte.

a

d

Supplementary Fig. 21 (a) Polarization curves, (b) Tafel plots of IrO2 synthesized with 0 g 3.2 g, 6.4 g and 12.8 g ammonia in O2-saturated 0.1 M HClO4 electrolyte with iR-correction.

b

a

Supplementary Fig. 22 (a) Polarization curves, (b) Tafel plots of IrO2 synthesized at 350 ℃, 450 ℃ and 550 ℃ in O2-saturated 0.1 M HClO4 electrolyte with iR-correction.

Supplementary Fig. 23 Durability test of IrO2(101) monolayer at 200 mA cm-2 in O2-saturated 0.1 M HClO4 electrolyte.

Supplementary Fig. 24 Cyclic voltammetry of IrO2(101) monolayer. CV curves of the first and 10000th CV cycles in O2-saturated 0.1 M HClO4 electrolyte.

b

a

Supplementary Fig. 25 (a) Polarization curves before the first, after the 2,000th and 10,000th CV cycle. (b) Overpotential at 10 and 50 mA cm-2 before the first, after the 2,000th and 10,000th CV cycle in O2-saturated 0.1 M HClO4 electrolyte.

200 nm

Supplementary Fig. 26 TEM image of IrO2(101) monolayer after durability test at 50 mA cm-2 in O2-saturated 0.1 M HClO4 electrolyte.

Supplementary Fig. 27 Comparison of XRD before and after durability test at 50 mA cm-2 in O2-saturated 0.1 M HClO4 electrolyte for IrO2(101) monolayer.

Supplementary Fig. 28 Comparison of XPS spectra before and after durability test at 50 mA cm-2 in O2-saturated 0.1 M HClO4 electrolyte for IrO2(101) monolayer.

Supplementary Fig. 29 Photo of the PEM electrolyzer.

Supplementary Table 1 EDX result of IrO2(101) monolayer.

| Element | (keV) | Mass% | Counts | Sigma | Atom% | K |
| --- | --- | --- | --- | --- | --- | --- |
| N K | 0.392 | 2.58 | 322.21 | 0.16 | 12.15 | 0.6898 |
| O K | 0.525 | 14.38 | 2493.78 | 0.36 | 59.33 | 0.4971 |
| Ir M | 1.977 | 83.05 | 7161.16 | 1.48 | 28.52 | 1.0000 |
| Total |  | 100.00 |  |  | 100.00 |  |

Supplementary Table 2 Binding energy of signal peak in XPS spectra.

| Catalyst | Ir(IV)-O 4f5/2 | Ir(IV)-O 4f7/2 | Ir-O | Ovancy | Oabsorbed |
| --- | --- | --- | --- | --- | --- |
| IrO2(101) monolayer | 64.92 | 61.87 | 530.08 | 531.6 | 533.42 |
| IrO2 NP | 64.67 | 61.67 | 530.03 | 531.26 | 532.65 |
| C-IrO2 | 64.87 | 61.95 | 530.08 | 531.41 | 533.05 |

Supplementary Table 3 Frequency of signal peaks in Raman spectra.

| Catalyst | Eg | A1g |
| --- | --- | --- |
| IrO2(101) monolayer | 540.09 | —— |
| IrO2 NP | 543.55 | 714.50 |
| C-IrO2 | 547.71 | 712.47 |

Supplementary Table 4 Average pore diameter of IrO2(101) monolayer, IrO2 NP and C-IrO2.

| Catalyst | Average pore diameter (nm) |
| --- | --- |
| IrO2(101) monolayer | 3.29 |
| IrO2 NP | 4.90 |
| C-IrO2 | 9.19 |

Supplementary Table 5 EXAFS parameters

| Catalyst | Shell | N | σ2 | R | R factor (%) |
| --- | --- | --- | --- | --- | --- |
| IrO2(101) monolayer | Ir-O | 5.9 | 0.003 | 2.00 | 0.14 |
| C-IrO2 | Ir-O | 6.0 | 0.002 | 2.00 | 0.07 |
| Ir foil | Ir- Ir | 12.0 | 0.003 | 2.71 | 0.63 |

Supplementary Table 6 Charge transfer resistance (RCT) calculated by fitting EIS of IrO2(101) monolayer, IrO2 NP, C-IrO2 and C-Ir black.

| Catalyst | RCT (ohm) |
| --- | --- |
| IrO2(101) monolayer | 10.32 |
| IrO2 NP | 109.60 |
| C-IrO2 | 88.49 |
| C-Ir black | 18.06 |

Supplementary Table 7 Inductively coupled plasma test of iridium dissolved in HClO4 electrolyte after durability test at 50 mA cm-2.

| Catalyst | Label | 193 (KED) [ppb] |
| --- | --- | --- |
| IrO2(101) monolayer | 1 | 387.492 |
|  | 2 | 398.953 |
|  | 3 | 398.459 |
|  | Mean: | 394.968 |
|  | RSD [%]: | 1.6 |
|  | SD: | 6.5 |
| IrO2 NP | 1 | 446.569 |
|  | 2 | 391.611 |
|  | 3 | 452.126 |
|  | Mean: | 430.102 |
|  | RSD [%]: | 7.8 |
|  | SD: | 33.5 |
| C- IrO2 | 1 | 1244.936 |
|  | 2 | 1248.965 |
|  | 3 | 1123.690 |
|  | Mean: | 1205.846 |
|  | RSD [%]: | 5.9 |
|  | SD: | 71.2 |

Supplementary Table 8 S-number of IrO2(101) monolayer, IrO2 NP and and C- IrO2

| Catalyst | nO2(mol) | nIr(mol) | S-number |
| --- | --- | --- | --- |
| IrO2(101) monolayer | 0.41976 | 9.05+e-8 | 4.64+e6 |
| IrO2 NP | 0.04741 | 9.86+e-8 | 4.18+ e5 |
| C- IrO2 | 0.03158 | 2.76+e-7 | 1.14+ e5 |