Supplementary Material

Effect of the composition of block copolypeptides on their biocompatibility and anti-bacterial activities

Ying-Jung Chenga#, Yi-Sheng Jianga#, Cheng-Rung Huang b, Chang-Shi Chen b and Jeng-Shiung Jana,c*

a Department of Chemical Engineering, National Cheng Kung University, No. 1, University Rd., East Dist., Tainan 70101, Taiwan; yinglongcheng@gmail.com (Y.-J.C.); js3794490@gmail.com (Y.-S.J.)

b Department of Biochemistry and Molecular Biology, College of Medicine, National Cheng Kung University, Tainan, Taiwan; jackie31428@gmail.com (C.-R H); cschen@mail.ncku.edu.tw (C.-S. C.)

c Program on Smart and Sustainable Manufacturing, Academy of Innovative Semiconductor and Sustainable Manufacturing, National Cheng Kung University, Tainan, 70101, Taiwan

# These authors contributed equally to this work.

*Correspondence: Jeng-Shiung Jan, Department of Chemical Engineering, National Cheng Kung University, No. 1 University Road, Tainan City 701, Taiwan, E-mail: jsjan@mail.ncku.edu.tw, Phone: 886-6-275-7575 ext. 62660, Fax: 886-6-234-4496.

Table S1. Degrees of polymerization, initiator to monomer ratios, and calculated molecular weights of all the block copolypeptides derived from 1H NMR spectra.

| Sample code | Feed ratio | Peptide composition |  |  |
| --- | --- | --- | --- | --- |
|  |  | DP | Initiator : ZLL : L-group | Mn |
| Lys20-Ala10 | 1 : 20 : 10 | 27 | 1 : 17 : 10 | 4346 |
| Lys20-Leu10 | 1 : 20: 10 | 26 | 1 : 17 : 9 | 4683 |
| Lys20-Phe10 | 1 : 20 : 10 | 27 | 1 : 19 : 8 | 4812 |
| 3s-Lys10-Ala5 | 1 : 30 : 15 | 18 | 1 : 12 : 6 | 8909 |
| 3s-Lys10-Leu5 | 1 : 30 : 15 | 19 | 1 : 12 : 6 | 9665 |
| 3s-Lys10-Phe5 | 1 : 30 : 15 | 17 | 1 : 11 : 6 | 9836 |

Figure S1. 1H-NMR spectra of ZLys20-Ala10, ZLys20-Leu10 and ZLys20-Phe10 block copolypeptides.

Figure S2. 1H-NMR spectra of 3s-ZLys10-Ala5, 3s-ZLys10-Leu5 and 3s-ZLys10-Phe5 block copolypeptides.

Figure S3. 1H-NMR spectra of Lys20-Ala10, Lys20-Leu10, and Lys20-Phe10 block copolypeptides.

Figure S4. 1H-NMR spectra of 3s-Lys20-Ala10, 3s-Lys20-Leu10, and 3s-Lys20-Phe10 block copolypeptides.

Figure S5. The cell viability of BEAS-2B cell organoids after treatment with polypeptides (n = 3).