Supplementary Materials

The photographs of (a) GdCaAl3O7: x% Eu3+  (x=10, 20, 30, 40, 50, 60, 70), (b) GdCaAl3O7: y% Tb3+ (y=10, 20, 30, 40, 50, 60, 70, 80 ) and (c) GdCaAl3O7: 50% Tb3+@x% Eu3+ (x=0, 1, 3, 5, 7, 9, 11) phosphors under the irradiation NUV light are presented in the Figure. S1. It can be observed from Figure. S1(a) that the red emission color of the GdCaAl3O7: x% Eu3+ phosphors changed gradually, and the red light became deeper with increasing Eu3+ contents. Subsequently, the red emission intensity decreased due to the well-known concentration quenching effects caused by non-radiative (NR) energy transfer among the neighboring Eu3+. The optimal red color could be obtained when the doping content of Eu3+ reached 40%. It can be seen from Figure. S1(b) that the green emission color of the GdCaAl3O7: y% Tb3+ phosphors changed gradually, and the green light became deeper with increasing Tb3+ contents. The GdCaAl3O7: y% Tb3+ phosphors emitted the brightest green light under NUV light source when the doping concentration of Tb3+ was up to 50%. When the doping concentration was more than this percent, the emission intensity decreased owing to the influence of concentration quenching. It can be observed from the Figure. S1(c)  images that the GdCaAl3O7: 50% Tb3+@x% Eu3+ could turn from greenish yellow, yellow, yellowish orange to near-red emission with increasing Eu3+ contents under NUV light, indicating that the emission color of the phosphors could changed significantly. The result indicates that the as-obtained GdCaAl3O7: 50% Tb3+@x% Eu3+ phosphors are color-tunable, which possess advantages of polychromatic light emissions under a single wavelength light and have potential applications as multicolor phosphors for white LEDs devices.

FIGURE S1 The photographs of the (a) GdCaAl3O7: x% Eu3+  (x=10, 20, 30, 40, 50, 60, 70), (b) GdCaAl3O7: y% Tb3+ (y=10, 20, 30, 40, 50, 60, 70, 80 ) and (c) GdCaAl3O7: 50% Tb3+@x% Eu3+ (x=0, 1, 3, 5, 7, 9, 11) phosphors under the irradiation NUV light.