On Relative importance of C-H‧‧‧O, C-H‧‧‧π and S‧‧‧π interactions in the crystal of  2H-1-benzopyran-2-one phenyl sulfoxide - A coumarin derivative

Provash Joarddar1, Goutam Biswas2,*, Atish Dipankar Jana1,6*, Sasthi Charan Halder1,3, Sandip Kundu4 and Subrata Dasgupta5

1Centre for research in nano science and crystal engineering, Sibani Mandal Mahavidyalaya, Namkhana,West Bengal, India, 743357

2Acharya Prafulla Chandra College, Department of Physics, New-Barrackpore, Kolkata-700131.

3Department of Physics, Behala College, Parnasree, Kolkata, India, 700060

4Indian Institute of Chemical Biology (IICB), Central Instrumentation facility XRD Laboratory, Jadavpur, Kolkata -700032.

5Department of Chemistry, National Institute of Technology (NIT), Durgapur 713209.

6Institue of Astronomy, Space and Earth Sciences, P 177, CIT Road, Scheme 7m, Kolkata 700054

E-mail: atishdipankarjana@yahoo.in, gbiswas.08@gmail.com

Supplementary file:

- CIF file corresponding to the reported crystal:

data_shelx

_audit_creation_method            'SHELXL-2018/3'

_shelx_SHELXL_version_number      '2018/3'

_chemical_name_systematic         ?

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          'C15 H10 O3 S'

_chemical_formula_sum             'C15 H10 O3 S'

_chemical_formula_weight          270.29

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'C'  'C'   0.0181   0.0091

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0492   0.0322

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'S'  'S'   0.3331   0.5567

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_space_group_crystal_system       monoclinic

_space_group_IT_number            14

_space_group_name_H-M_alt         'P 21/c'

_space_group_name_Hall            '-P 2ybc'

_shelx_space_group_comment

;

The symmetry employed for this shelxl refinement is uniquely defined

by the following loop, which should always be used as a source of

symmetry information in preference to the above space-group names.

They are only intended as comments.

;

loop_

_space_group_symop_operation_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a                    4.6038(4)

_cell_length_b                    11.5300(12)

_cell_length_c                    23.073(2)

_cell_angle_alpha                 90

_cell_angle_beta                  92.407(5)

_cell_angle_gamma                 90

_cell_volume                      1223.7(2)

_cell_formula_units_Z             4

_cell_measurement_temperature     114(2)

_cell_measurement_reflns_used     1845

_cell_measurement_theta_min       6.58

_cell_measurement_theta_max       66.279

_exptl_crystal_description        'LIQUID'

_exptl_crystal_colour             ?

_exptl_crystal_density_meas       ?

_exptl_crystal_density_method     ?

_exptl_crystal_density_diffrn     1.467

_exptl_crystal_F_000              560

_exptl_transmission_factor_min    ?

_exptl_transmission_factor_max    ?

_exptl_crystal_size_max           0.200

_exptl_crystal_size_mid           0.020

_exptl_crystal_size_min           0.010

_exptl_absorpt_coefficient_mu     2.366

_shelx_estimated_absorpt_T_min    0.649

_shelx_estimated_absorpt_T_max    0.977

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   ?

_exptl_absorpt_correction_T_max   ?

_exptl_absorpt_process_details    ?

_exptl_absorpt_special_details    ?

_diffrn_ambient_temperature       114(2)

_diffrn_radiation_wavelength      1.54178

_diffrn_radiation_type            CuK\a

_diffrn_source                    ?

_diffrn_measurement_device_type   'Bruker Kappa Apex -II '

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_reflns_number             19499

_diffrn_reflns_av_unetI/netI      0.0451

_diffrn_reflns_av_R_equivalents   0.0893

_diffrn_reflns_limit_h_min        -5

_diffrn_reflns_limit_h_max        5

_diffrn_reflns_limit_k_min        -13

_diffrn_reflns_limit_k_max        13

_diffrn_reflns_limit_l_min        -27

_diffrn_reflns_limit_l_max        24

_diffrn_reflns_theta_min          3.835

_diffrn_reflns_theta_max          66.279

_diffrn_reflns_theta_full         66.279

_diffrn_measured_fraction_theta_max   0.973

_diffrn_measured_fraction_theta_full  0.973

_diffrn_reflns_Laue_measured_fraction_max    0.973

_diffrn_reflns_Laue_measured_fraction_full   0.973

_diffrn_reflns_point_group_measured_fraction_max   0.973

_diffrn_reflns_point_group_measured_fraction_full  0.973

_reflns_number_total              2157

_reflns_number_gt                 1845

_reflns_threshold_expression      'I > 2\s(I)'

_reflns_Friedel_coverage          0.000

_reflns_Friedel_fraction_max      .

_reflns_Friedel_fraction_full     .

_reflns_special_details

;

Reflections were merged by SHELXL according to the crystal

class for the calculation of statistics and refinement.

_reflns_Friedel_fraction is defined as the number of unique

Friedel pairs measured divided by the number that would be

possible theoretically, ignoring centric projections and

systematic absences.

;

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     ?

_computing_structure_refinement 'SHELXL-2018/3 (Sheldrick, 2018)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details           ?

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'w=1/[\s^2^(Fo^2^)+(0.0717P)^2^+0.7156P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      ?

_atom_sites_solution_secondary    ?

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     constr

_refine_ls_extinction_method      'SHELXL-2018/3 (Sheldrick 2018)'

_refine_ls_extinction_coef        0.0085(11)

_refine_ls_extinction_expression

'Fc^*^=kFc[1+0.001xFc^2^\l^3^/sin(2\q)]^-1/4^'

_refine_ls_number_reflns          2157

_refine_ls_number_parameters      173

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0566

_refine_ls_R_factor_gt            0.0498

_refine_ls_wR_factor_ref          0.1340

_refine_ls_wR_factor_gt           0.1276

_refine_ls_goodness_of_fit_ref    1.080

_refine_ls_restrained_S_all       1.080

_refine_ls_shift/su_max           0.013

_refine_ls_shift/su_mean          0.003

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_site_symmetry_order

_atom_site_calc_flag

_atom_site_refinement_flags_posn

_atom_site_refinement_flags_adp

_atom_site_refinement_flags_occupancy

_atom_site_disorder_assembly

_atom_site_disorder_group

S1 S 0.23046(13) 0.64040(6) 0.39566(3) 0.0294(3) Uani 1 1 d . . . . .

O1 O 0.7294(4) 0.46591(16) 0.28586(7) 0.0323(5) Uani 1 1 d . . . . .

O3 O 0.1956(4) 0.60554(16) 0.45702(8) 0.0328(5) Uani 1 1 d . . . . .

O2 O 0.4068(4) 0.60760(17) 0.27325(8) 0.0376(5) Uani 1 1 d . . . . .

C5 C 0.8501(5) 0.3900(2) 0.38200(11) 0.0274(6) Uani 1 1 d . . . . .

C6 C 0.8849(5) 0.3907(2) 0.32214(12) 0.0303(6) Uani 1 1 d . . . . .

C4 C 0.6456(5) 0.4692(2) 0.40537(11) 0.0277(6) Uani 1 1 d . . . . .

H4 H 0.613027 0.469341 0.445750 0.033 Uiso 1 1 calc R U . . .

C2 C 0.5355(5) 0.5443(2) 0.30732(12) 0.0310(6) Uani 1 1 d . . . . .

C11 C 0.4503(5) 0.7698(2) 0.39807(11) 0.0286(6) Uani 1 1 d . . . . .

C3 C 0.5000(5) 0.5434(2) 0.36966(11) 0.0290(6) Uani 1 1 d . . . . .

C10 C 1.0155(5) 0.3116(2) 0.41589(12) 0.0299(6) Uani 1 1 d . . . . .

H10 H 0.996129 0.309513 0.456707 0.036 Uiso 1 1 calc R U . . .

C9 C 1.2066(6) 0.2373(2) 0.39023(12) 0.0336(7) Uani 1 1 d . . . . .

H9 H 1.319795 0.184911 0.413542 0.040 Uiso 1 1 calc R U . . .

C16 C 0.4718(6) 0.8395(2) 0.34929(13) 0.0361(7) Uani 1 1 d . . . . .

H16 H 0.375466 0.818625 0.313577 0.043 Uiso 1 1 calc R U . . .

C8 C 1.2346(6) 0.2385(2) 0.33050(12) 0.0344(7) Uani 1 1 d . . . . .

H8 H 1.364180 0.185940 0.313219 0.041 Uiso 1 1 calc R U . . .

C7 C 1.0749(6) 0.3160(2) 0.29588(12) 0.0349(7) Uani 1 1 d . . . . .

H7 H 1.095447 0.317676 0.255092 0.042 Uiso 1 1 calc R U . . .

C15 C 0.6362(6) 0.9398(3) 0.35377(13) 0.0400(7) Uani 1 1 d . . . . .

H15 H 0.654079 0.988334 0.320851 0.048 Uiso 1 1 calc R U . . .

C12 C 0.5841(7) 0.7992(3) 0.45021(13) 0.0415(7) Uani 1 1 d . . . . .

H12 H 0.565133 0.751195 0.483287 0.050 Uiso 1 1 calc R U . . .

C14 C 0.7740(7) 0.9694(3) 0.40574(14) 0.0475(8) Uani 1 1 d . . . . .

H14 H 0.888057 1.038017 0.408439 0.057 Uiso 1 1 calc R U . . .

C13 C 0.7473(8) 0.9002(3) 0.45393(15) 0.0574(10) Uani 1 1 d . . . . .

H13 H 0.841137 0.921656 0.489787 0.069 Uiso 1 1 calc R U . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

S1 0.0250(4) 0.0335(4) 0.0301(4) -0.0007(3) 0.0065(3) -0.0023(3)

O1 0.0308(10) 0.0392(11) 0.0275(10) -0.0014(8) 0.0099(8) -0.0005(8)

O3 0.0320(10) 0.0355(10) 0.0317(11) -0.0002(8) 0.0108(8) -0.0025(8)

O2 0.0419(11) 0.0416(11) 0.0294(11) 0.0022(9) 0.0033(9) 0.0018(9)

C5 0.0237(12) 0.0285(13) 0.0305(14) -0.0024(11) 0.0061(11) -0.0074(10)

C6 0.0247(13) 0.0360(15) 0.0305(14) -0.0019(12) 0.0039(11) -0.0056(11)

C4 0.0237(12) 0.0324(14) 0.0275(13) -0.0016(11) 0.0073(10) -0.0066(11)

C2 0.0276(13) 0.0323(14) 0.0333(15) -0.0029(12) 0.0045(11) -0.0046(11)

C11 0.0232(12) 0.0295(13) 0.0337(15) -0.0004(11) 0.0069(11) 0.0008(11)

C3 0.0242(13) 0.0343(14) 0.0290(14) -0.0013(11) 0.0079(11) -0.0058(11)

C10 0.0274(13) 0.0323(14) 0.0307(14) 0.0001(11) 0.0075(11) -0.0062(11)

C9 0.0281(14) 0.0336(15) 0.0395(16) -0.0001(12) 0.0058(12) -0.0045(11)

C16 0.0378(15) 0.0358(15) 0.0351(16) 0.0009(12) 0.0050(12) 0.0013(12)

C8 0.0281(13) 0.0364(15) 0.0395(16) -0.0073(12) 0.0112(12) -0.0040(12)

C7 0.0311(14) 0.0415(16) 0.0330(15) -0.0066(13) 0.0103(12) -0.0053(12)

C15 0.0433(16) 0.0352(16) 0.0425(17) 0.0063(13) 0.0125(14) -0.0023(13)

C12 0.0466(17) 0.0397(17) 0.0380(17) 0.0055(13) -0.0003(13) -0.0115(13)

C14 0.0533(19) 0.0400(17) 0.0491(19) 0.0017(15) 0.0030(15) -0.0172(15)

C13 0.074(2) 0.051(2) 0.045(2) 0.0049(16) -0.0146(17) -0.0275(18)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

S1 O3 1.4868(19) . ?

S1 C3 1.792(3) . ?

S1 C11 1.802(3) . ?

O1 C2 1.377(3) . ?

O1 C6 1.384(3) . ?

O2 C2 1.209(3) . ?

C5 C6 1.397(4) . ?

C5 C10 1.400(4) . ?

C5 C4 1.433(4) . ?

C6 C7 1.385(4) . ?

C4 C3 1.347(4) . ?

C4 H4 0.9500 . ?

C2 C3 1.454(4) . ?

C11 C12 1.371(4) . ?

C11 C16 1.390(4) . ?

C10 C9 1.379(4) . ?

C10 H10 0.9500 . ?

C9 C8 1.390(4) . ?

C9 H9 0.9500 . ?

C16 C15 1.384(4) . ?

C16 H16 0.9500 . ?

C8 C7 1.388(4) . ?

C8 H8 0.9500 . ?

C7 H7 0.9500 . ?

C15 C14 1.376(4) . ?

C15 H15 0.9500 . ?

C12 C13 1.386(4) . ?

C12 H12 0.9500 . ?

C14 C13 1.379(4) . ?

C14 H14 0.9500 . ?

C13 H13 0.9500 . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O3 S1 C3 104.72(12) . . ?

O3 S1 C11 106.09(12) . . ?

C3 S1 C11 97.53(11) . . ?

C2 O1 C6 121.4(2) . . ?

C6 C5 C10 118.3(2) . . ?

C6 C5 C4 118.2(2) . . ?

C10 C5 C4 123.5(2) . . ?

O1 C6 C7 116.5(2) . . ?

O1 C6 C5 121.6(2) . . ?

C7 C6 C5 122.0(3) . . ?

C3 C4 C5 119.5(2) . . ?

C3 C4 H4 120.2 . . ?

C5 C4 H4 120.2 . . ?

O2 C2 O1 118.0(2) . . ?

O2 C2 C3 125.1(2) . . ?

O1 C2 C3 116.9(2) . . ?

C12 C11 C16 121.5(3) . . ?

C12 C11 S1 117.6(2) . . ?

C16 C11 S1 120.8(2) . . ?

C4 C3 C2 122.4(2) . . ?

C4 C3 S1 121.7(2) . . ?

C2 C3 S1 115.8(2) . . ?

C9 C10 C5 120.2(3) . . ?

C9 C10 H10 119.9 . . ?

C5 C10 H10 119.9 . . ?

C10 C9 C8 120.5(3) . . ?

C10 C9 H9 119.8 . . ?

C8 C9 H9 119.8 . . ?

C15 C16 C11 118.7(3) . . ?

C15 C16 H16 120.7 . . ?

C11 C16 H16 120.7 . . ?

C7 C8 C9 120.6(2) . . ?

C7 C8 H8 119.7 . . ?

C9 C8 H8 119.7 . . ?

C8 C7 C6 118.5(3) . . ?

C8 C7 H7 120.7 . . ?

C6 C7 H7 120.7 . . ?

C14 C15 C16 120.2(3) . . ?

C14 C15 H15 119.9 . . ?

C16 C15 H15 119.9 . . ?

C11 C12 C13 119.0(3) . . ?

C11 C12 H12 120.5 . . ?

C13 C12 H12 120.5 . . ?

C15 C14 C13 120.4(3) . . ?

C15 C14 H14 119.8 . . ?

C13 C14 H14 119.8 . . ?

C14 C13 C12 120.2(3) . . ?

C14 C13 H13 119.9 . . ?

C12 C13 H13 119.9 . . ?

loop_

_geom_torsion_atom_site_label_1

_geom_torsion_atom_site_label_2

_geom_torsion_atom_site_label_3

_geom_torsion_atom_site_label_4

_geom_torsion

_geom_torsion_site_symmetry_1

_geom_torsion_site_symmetry_2

_geom_torsion_site_symmetry_3

_geom_torsion_site_symmetry_4

_geom_torsion_publ_flag

C2 O1 C6 C7 -179.7(2) . . . . ?

C2 O1 C6 C5 0.7(4) . . . . ?

C10 C5 C6 O1 -179.9(2) . . . . ?

C4 C5 C6 O1 0.5(4) . . . . ?

C10 C5 C6 C7 0.5(4) . . . . ?

C4 C5 C6 C7 -179.1(2) . . . . ?

C6 C5 C4 C3 -1.8(4) . . . . ?

C10 C5 C4 C3 178.6(2) . . . . ?

C6 O1 C2 O2 179.9(2) . . . . ?

C6 O1 C2 C3 -0.6(3) . . . . ?

O3 S1 C11 C12 11.5(2) . . . . ?

C3 S1 C11 C12 -96.2(2) . . . . ?

O3 S1 C11 C16 -165.7(2) . . . . ?

C3 S1 C11 C16 86.5(2) . . . . ?

C5 C4 C3 C2 1.9(4) . . . . ?

C5 C4 C3 S1 177.34(18) . . . . ?

O2 C2 C3 C4 178.7(3) . . . . ?

O1 C2 C3 C4 -0.7(4) . . . . ?

O2 C2 C3 S1 3.0(4) . . . . ?

O1 C2 C3 S1 -176.41(17) . . . . ?

O3 S1 C3 C4 -7.0(2) . . . . ?

C11 S1 C3 C4 101.9(2) . . . . ?

O3 S1 C3 C2 168.72(18) . . . . ?

C11 S1 C3 C2 -82.4(2) . . . . ?

C6 C5 C10 C9 -0.1(4) . . . . ?

C4 C5 C10 C9 179.5(2) . . . . ?

C5 C10 C9 C8 -0.7(4) . . . . ?

C12 C11 C16 C15 1.0(4) . . . . ?

S1 C11 C16 C15 178.1(2) . . . . ?

C10 C9 C8 C7 1.2(4) . . . . ?

C9 C8 C7 C6 -0.8(4) . . . . ?

O1 C6 C7 C8 -179.7(2) . . . . ?

C5 C6 C7 C8 -0.1(4) . . . . ?

C11 C16 C15 C14 -0.2(4) . . . . ?

C16 C11 C12 C13 -0.8(5) . . . . ?

S1 C11 C12 C13 -178.0(3) . . . . ?

C16 C15 C14 C13 -0.6(5) . . . . ?

C15 C14 C13 C12 0.8(6) . . . . ?

C11 C12 C13 C14 0.0(5) . . . . ?

_refine_diff_density_max    0.563

_refine_diff_density_min   -0.464

_refine_diff_density_rms    0.075

2.  CheckCIF report: