Fe/N/C Catalysts with Hierarchical Porous Structure Derived from Fe-doped ZIF-8 for Accelerated ORR Activity

Kaixiang Lia, Jinyu Zhaob, Ruipeng Yuanb, Jiajun Chenb, Huijun Lib, Xiaomin Wangb, *

a GAC AION NEW ENERGY AUTOMOBILE Co. Ltd. 36 Longyin Road Guangzhou Guangdong, China, 511436

b College of Materials Science and Engineering, Taiyuan University of Technology, Taiyuan 030024, China

Corresponding author: Xiaomin Wangb, *

E-mail address: wangxiaomin@tyut.edu.cn（X Wang）

Figure S1 SEM image and EDS images of Fe-N-C 1000

Figure S2 XPS spectra of N 1s and Fe 2p

Figure S3 (a-d) N2 adsorption/desorption isotherms of Fe-N-C 700, Fe-N-C 800, Fe-N-C 900, Fe-N-C 1100 and corresponding aperture distribution

Figure S4 The morphology and structure after stability test of Fe-N-C 1000

Figure S5 LSV curves of FeNC-1000 and Pt/C catalysts in 0.1 M HClO4.

Table S1 Pore size analysis of Fe-N-C derived from Fe-ZIF-8 by a series of high temperature annealing treatments

| Samples | SBET (m2 g-1) | Vt (cm3 g-1) | Pore Volume (cm3 g-1) |  |  | Pore Volume (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Vmicro | Vmeso | Vmacro | Vmicro | Vmeso | Vmacro |
| Fe-N-C 700 | 44.49 | 0.557 | 0.00582 | 0.164 | 0.349 | 1.1% | 32% | 66.9% |
| Fe-N-C 800 | 128.9152 | 0.617 | 0.036 | 0.254 | 0.308 | 6.0 % | 42.5% | 51.5% |
| Fe-N-C 900 | 271.0849 | 0.837 | 0.087 | 0.478 | 0.802 | 10.7% | 48.9% | 40.4% |
| Fe-N-C 1000 | 572.1957 | 1.106 | 0.205 | 0.882 | 1.055 | 19.4% | 64.1% | 16.2% |
| Fe-N-C 1100 | 1162.2 | 1.749 | 0.46 | 0.586 | 0.252 | 35.4% | 45% | 19.4% |

a The specific surface area (SSA) was calculated by BET method.

b The total pore volume (TPV) was obtained at relative pressure p/p0=0.99.

c The pore volume based on different pore size range was calculated by DFT model.

Table S2 Summary of obtained and other repored catalysts for ORR in acidic

Electrolytes

| Catalyst | E1/2（V） | JK （mA cm-2） | Tafel slopes （mv dec-1） | References |
| --- | --- | --- | --- | --- |
| Fe-N-C 1000 | 0.791 | 10.1 | 52 | This work |
| Fe2-N-C | 0.78 | 16.4 | 83 | 1 |
| HP-FeN4 | 0.80 | - | 72 | 2 |
| Fe-Zn-SA/NC | 0.78 | - | 54.3 | 3 |
| Mn-Fe@ NCNTs | 0.76 | - | 78.5 | 4 |
| FeCu-SAC | 0.779 | 16.33 | 53.6 | 5 |
| FeSA/AC@NC | 0.80 | - | 52 | 6 |
| Fe(Cd)-N-C | 0.837 | - | 56 | 7 |
| Fe/ZnS-SNC | 0.81 | 21.8 | 41.3 | 8 |
| FeSNC-TA | 0.76 | 6.9 | 61.2 | 9 |
| Fe@Fe-N-C | 0.829 | 11.1 | 76.3 | 10 |

References

1.	Ye, W.;  Chen, S.;  Lin, Y.;  Yang, L.;  Chen, S.;  Zheng, X.;  Qi, Z.;  Wang, C.;  Long, R.;  Chen, M.;  Zhu, J.;  Gao, P.;  Song, L.;  Jiang, J.; Xiong, Y., Precisely Tuning the Number of Fe Atoms in Clusters on N-Doped Carbon toward Acidic Oxygen Reduction Reaction. Chem 2019, 5 (11), 2865-2878.

2.	Zhang, N.;  Zhou, T.;  Chen, M.;  Feng, H.;  Yuan, R.;  Zhong, C. a.;  Yan, W.;  Tian, Y.;  Wu, X.;  Chu, W.;  Wu, C.; Xie, Y., High-purity pyrrole-type FeN4 sites as a superior oxygen reduction electrocatalyst. Energy & Environmental Science 2020, 13 (1), 111-118.

3.	Xu, J.;  Lai, S.;  Qi, D.;  Hu, M.;  Peng, X.;  Liu, Y.;  Liu, W.;  Hu, G.;  Xu, H.;  Li, F.;  Li, C.;  He, J.;  Zhuo, L.;  Sun, J.;  Qiu, Y.;  Zhang, S.;  Luo, J.; Liu, X., Atomic Fe-Zn dual-metal sites for high-efficiency pH-universal oxygen reduction catalysis. Nano Research 2021, 14 (5), 1374-1381.

4.	Guo, X.;  Xue, S.;  Zhang, X.;  Qin, J.;  Hong, M.;  Chen, Q.;  Liu, W.;  Du, C.; Chen, J., Mn atomic clusters and Fe nanoparticles in-situ conﬁned nitrogen carbon nanotubes for efficient and durable ORR electrocatalysts in both alkaline and acidic media. Journal of Alloys and Compounds 2023, 953, 169992.

5.	Yang, H.;  Huang, H.;  Wang, Q.;  Shang, L.;  Zhang, T.; Wang, S., Fe, Cu dual-metal single atom catalyst on commercial carbon black for efficient oxygen reduction reaction. Journal of Materials Chemistry A 2023, 11 (12), 6191-6197.

6.	Chen, C.;  Wu, Y.;  Li, X.;  Ye, Y.;  Li, Z.;  Zhou, Y.;  Chen, J.;  Yang, M.;  Xie, F.;  Jin, Y.;  Jones, C.;  Wang, N.;  Meng, H.; Chen, S., Modulating Fe spin state in FeNC catalysts by adjacent Fe atomic clusters to facilitate oxygen reduction reaction in proton exchange membrane fuel cell. Applied Catalysis B: Environmental 2024, 342, 123407.

7.	Luo, Z.;  Zhou, T.;  Guan, Y.;  Zhang, L.;  Zhang, Q.;  He, C.;  Sun, X.; Ren, X., Building Atomic Scale and Dense Fe─N4 Edge Sites of Highly Efficient Fe─N─C Oxygen Reduction Catalysts Using a Sacrificial Bimetallic Pyrolysis Strategy. Small 2023, n/a (n/a), 2304750.

8.	Pei, F.;  Li, M.;  Huang, Y.;  Guo, Q.;  Song, K.;  Kong, F.; Cui, X. Constructing FeS and ZnS Heterojunction on N,S-Codoped Carbon as Robust Electrocatalyst toward Oxygen Reduction Reaction Nanomaterials [Online], 2023.

9.	Liu, H.;  Jiang, L.;  Sun, Y.;  Khan, J.;  Feng, B.;  Xiao, J.;  Zhang, H.;  Xie, H.;  Li, L.;  Wang, S.; Han, L., Revisiting the Role of Sulfur Functionality in Regulating the Electron Distribution of Single-Atomic Fe Sites Toward Enhanced Oxygen Reduction. Advanced Functional Materials 2023, 33 (35), 2304074.

10.	Li, L.;  Wen, Y.;  Han, G.;  Kong, F.;  Du, L.;  Ma, Y.;  Zuo, P.;  Du, C.; Yin, G., Architecting FeNx on High Graphitization Carbon for High-Performance Oxygen Reduction by Regulating d-Band Center. Small 2023, 19 (22), 2300758.