Electronic Supporting Material on the publication entitled

Determination of size and particle number concentration of metallic nanoparticles using isotope dilution analysis combined with single particle ICP-MS to overcome            matrix effect

Marta Hernández-Postigo, Armando Sánchez-Cachero,                          María Jiménez-Moreno and Rosa Carmen Rodríguez Martín-Doimeadios

Department of Analytical Chemistry and Food Technology,                         Environmental Sciences Institute (ICAM), University of Castilla-La Mancha,                                      Avda. Carlos III s/n, 45071 Toledo, Spain.

Table S1. Isotope abundance (%) of ionic Pt and 194Pt enriched standard solution.

| Standard solution | Isotope abundance (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 190Pt | 192Pt | 194Pt | 195Pt | 196Pt | 198Pt |
| Pt | 0.01236 ± 0.00033 | 0.771 ± 0.026 | 32.81 ± 0.13 | 33.793 ± 0.064 | 25.358 ± 0.026 | 7.26 ± 0.19 |
| 194Pt enriched | 0.00028 ± 0.00018 | 0.02298 ± 0.00044 | 96.705 ± 0.066 | 2.289 ± 0.042 | 0.824 ± 0.020 | 0.1580 ± 0.0039 |

Table S2. Characterization of biological and environmental samples. Mean and standard deviation (n=3).

| Sample | pH | Conductivity (mS cm-1) | Cl- (mg L-1) |
| --- | --- | --- | --- |
| Human urine | 6.787 ± 0.015 | 6.607 ± 0.015 | 1858 ± 44 |
| DMEM | 8.0633 ± 0.0058 | 13.9233 ± 0.0058 | 8463 ± 197 |
| Synthetic seawater* | 6.417 ± 0.032 | 34.367 ± 0.058 | 16087 ± 380 |
| Atlantic Ocean seawater | 7.640 ± 0.010 | 43. 83 ± 0.21 | 19978 ± 465 |

*Synthetic seawater sample prepared following EPA-821-R-02-12 protocol [Ref. 32].

Table S3. Event loss (%), background signal change (%), calculated against UPW, and transport efficiency values (%, n = 3) in the studied matrices for 30 nm PtNPs in SP-ICP-MS

| Matrix | Event loss (%) | Background signal change (%) | Transport Efficiency (%) |
| --- | --- | --- | --- |
| UPW | - | - | 9.49 ± 0.78 |
| Humar urine | 32.0 | 4.0 | 8.33 ± 0.39 |
| Human urine + 1 % TMAH | 71.1 | 486.3 | 9.380 ± 0.073 |
| DMEM | 37.0 | 11.8 | 8.35 ± 0.68 |
| Synthetic seawater | 28.7 | 51.6 | 7.77 ± 0.43 |
| Atlantic Ocean seawater | 19.3 | 66.1 | 8.44 ± 0.25 |