Supplementary data

Sub-ambient radiative cooling realized using CaCO3 microparticle-based single layer without metal reflector for entire

Hangyu Lim, Dongwoo Chae, Soomin Son, Sucheol Ju, Jisung Ha and Heon Lee *

Department of Material Science and Engineering, Korea University, Seoul, South Korea

The Supporting Information contains:

Number of Pages: 6

Number of Figures: 3

Number of Tables: 1

References

Figure. S1 XRD 2Ɵ scan data of CaCO3 powders

Figure. S2. Optical properties of CaCO3 on glass in accordance with thickness. (a) Absorption and (b) transmittance.

Table S1. Average absorption (0.3-2.5 µm), emissivity (8-13 µm) and net cooling power at 300 K in accordance with thickness of CaCO3 composite.

| Sample | Solar power absorption ratio (0.3-2.5 µm) | Average emissivity (8-13 µm) | Net cooling power at 300 K (W/m2) |
| --- | --- | --- | --- |
| 130 µm | 0.027 | 0.883 | 105.5 |
| 240 µm | 0.042 | 0.902 | 95.0 |
| 350 µm | 0.041 | 0.896 | 93.1 |
| 500 µm | 0.079 | 0.886 | 59.7 |

Figure. S3. (a) Solar power density of AM1.5 direct + circumsolar and (b) ideal and (c) mid-latitude atmospheric transmittance window in range of 0.3–15 μm.1,2 (d) Transmittance of
LDPE film using wind shield when measuring outside.

References

1. Berk, A. et al. MODTRAN® 6: A major upgrade of the MODTRAN® radiative transfer code. in Workshop on Hyperspectral Image and Signal Processing, Evolution in Remote Sensing vols 2014-June (IEEE Computer Society, 2014).

2. S. D. Lord, A New Software Tool for Computing Earth's Atmospheric Transmission of Near- and Far-Infrared Radiation, Vol. 103957, Ames Research Center, Moffett Field, CA, USA 1992