Supplementary file

Anticorrosion properties of ionic liquid functionalized graphene oxide epoxy composite coating on the carbon steel for CCUS environment

Nikhil Rahul Dhongde a, Sayani Adhikari a, Prasanna Venkatesh Rajaraman a*

a Department of Chemical Engineering, Indian Institute of Technology, Guwahati – 781039, Assam, India

*Corresponding Author; Email: rprasanna@iitg.ac.in

S1: Properties of epoxy and hardener

Bisphenol A diglycidyl ether (epoxy) Properties

| Chemical formula | C21H24O4 |
| --- | --- |
| Molar mass | 340.419 (g/mol) |
| density | 1.16 (g/mL at 25 °C (lit.)) |
| Epoxide equivalent weight (EEW) | 172-176 |
| Solid content | 73-77 % |

4-4’-diaminodiphenyl sulfone (hardener) Properties

| Chemical formula | [4-(NH2)C6H4]2SO2 |
| --- | --- |
| Molar mass | 248.30 (g/mol) |
| Bulk density | 250‑350 (kg/m3) |
| Amine value | 230-250 (KOH mg /g) |
| Solid content | 48-52 % |

S2: FESEM image of 1 wt% GO/epoxy coating after treatment with CO2-NaCl medium

Fig. S1: FESEM image of 1 wt% GO/epoxy coating after treatment with CO2-NaCl medium