Ultrathin Ni-fumarate MOFs decorated with PVP-Au NPs for simultaneous dopamine and paracetamol sensor and DFT investigations

Feng Zhou1, Limei Gai2*, Hua Liu1, Danfeng Qin3, Tushagu Abudouwufu4, Yi Liu5*

1School of Engineering, Guangzhou College of Technology and Business, Guangzhou 510880, Guangdong, P.R. China

2National-Local Joint Engineering Laboratory of Harbour Oil & Gas Storage and Transportation Technology/Zhejiang Key Laboratory of Petrochemical Environmental Pollution Control, School of Petrochemical Engineering & Environment, Zhejiang Ocean University, Zhoushan 316022, P.R. China

3School of Medicine Guangxi University of Science and Technology, Liuzhou 545006, Guangxi, P.R. China

4School of Pharmacy and Food Science, Zhuhai College of Science and Technology, No. 8 Anji East Road, Jinwan District, Zhuhai 519041, P.R. China

5State Key Laboratory of Functional Materials and Devices for Special Environments Conditions, Xinjiang Technical Institute of Physics & Chemistry of CAS, 40-1 South Beijing Road, Urumqi, 830011, China

*Email address: liu_yi@ms.xjb.ac.cn, gailimei@zjou.edu.cn

Table S1- Parameters of the porous structures determined from the N adsorption values.

| Samples | Ni-MOF (Ni(CH3CO2)2) | Au@Ni-MOF (Ni(CH3CO2)2) |
| --- | --- | --- |
| SBET (m2g-1) | 12.7379 | 10.0816 |
| VBJH (cm3g-1) | 0.0301 | 0.0188 |
| Pore size | 9.4555 | 7.4406 |

Fig. S1 (A) CVs obtained for (a) bare SPCE, (b) Ni-MOF (Ni(CH3CO2)2)/SPCE, and (c) Au@Ni-MOF (Ni(CH3CO2)2)/SPCE in 5.0 mmol L-1 K3[Fe(CN)6] as redox probe in 0.1 mol L-1 KCl at a scan rate of 50 mV s-1 and (B) EIS got for (a) bare SPCE, (b) Ni-MOF (Ni(CH3CO2)2)/SPCE, and (c) Au@Ni-MOF (Ni(CH3CO2)2)/SPCE in 5.0 mmol L-1 [Fe(CN)6]3-/4- as redox probe in 0.1 mol L-1 KCl at a scan rate of 50 mV s-1.

Fig. S2 The possible reaction mechanism for the reaction of the nickel acetate with H3BTC.

Fig. S3 (A) CV and (B) DPV of (a) Ni-MOF (Ni(CH3CO2)2)/SPCE, (b) Au@Ni-MOF (Ni(CH3CO2)2) (0.02 mM of AuNPs)/SPCE, (c) Au@Ni-MOF (Ni(CH3CO2)2) (0.12 mM of AuNPs)/SPCE, and (d) Au@Ni-MOF (Ni(CH3CO2)2) (0.36 mM of AuNPs)/SPCE in PBS (pH=6) electrolyte at scan rate of 50 mV s-1. (50μM of DAand UA were added).

Fig. S4 (A) The plots of the conjugate orbital along with the HOMO and LUMO distributions for DA (A, B) and UA (C, D), respectively; The plots of the electron density for DA (E) and UA (F).

Table S2 Energy gap (Eg) analysis for DA and UA.

| Analyte | HOMO (eV) | LUMO (eV) | Eg (eV) | Eg (kJ/mol) | η (kJ/mol) | σ (kJ/mol) | χ (kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DA | -0.175964 | -0.025313 | 0.150651 | 14.54 | 7.27 | 0.138 | 9.71 |
| UA | -0.194448 | -0.068916 | 0.125532 | 12.11 | 6.06 | 0.165 | 12.71 |

Fig. S5 The adsorption formation of 2DA (A), 2UA (B), and DA/UA (C) on the surface of Ni-MOF (Ni(CH3CO2)2), the adsorption formation of 2DA (D), 2UA (E), and DA/UA (F) on the surface of Au@Ni-MOF (Ni(CH3CO2)2). Carbon, oxygen, nitrogen, hydrogen, and gold atoms are depicted in gray, red, blue, white, and yellow, respectively.

Table S3 Adsorption energy (Eads) analysis for DA and UA on the surface of Ni-MOF (Ni(CH3CO2)2) and Au@Ni-MOF (Ni(CH3CO2)2).

| Energy | ESubstrate (eV) |  | EAdsorbate (eV) | EComplex (eV) | Eads (eV) | Eads (kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- |
| Ni-MOF (Ni(CH3CO2)2)-2DA | -5186.17764 |  | -8224.64425 | -13411.8712 | -1.0493 | -101.24 |
| Ni-MOF (Ni(CH3CO2)2)-2UA | -6553.79262 |  | -8224.64425 | -14779.5172 | -1.0803 | -104.24 |
| Ni-MOF (Ni(CH3CO2)2)-DA/UA | -5869.98513 |  | -8224.64425 | -14096.4742 | -1.8448 | -178.00 |
| Au@Ni-MOF (Ni(CH3CO2)2)-2DA | -5186.17764 |  | -22348.4175 | -27540.1569 | -5.5618 | -536.63 |
| Au@Ni-MOF (Ni(CH3CO2)2)-2UA | -6553.79262 |  | -22348.4175 | -28906.4071 | -4.1970 | -404.95 |
| Au@Ni-MOF (Ni(CH3CO2)2)-DA/UA | -5869.98513 | -22348.4175 |  | -28222.9084 | -4.5058 | -434.74 |