Table 1 grouping in animal model

|  | Groups |
| --- | --- |
| 1 | Scaffold 2/5% SPC+ co-culture |
| 2 | Scaffold 0% spc + co-culture |
| 3 | Scaffold 2/5% SPC+ keratinocyte |
| 4 | Scaffold 0% spc + keratinocyte |
| 5 | Scaffold 2/5% SPC+ mesenchyme cell |
| 6 | Scaffold 0% spc + mesenchyme cell |
| 7 | Control ( vaselin) |

Table 2  Wound-healing process, pathological parameters and ranking criteria

Table 3. Wound healing rate in different groups studied n=3

| Groups | Day | wound area | % wound closure | Std. Deviation |
| --- | --- | --- | --- | --- |
| All Group | 0 | 50 | - |  |
| Scaffold 2/5% SPC+ co-culture | 3 | 35.63 | 28.74 | 0/03536 |
| Scaffold 2/5% SPC+ keratinocyte |  | 37.019 | 25.962 | 0/09899 |
| Scaffold 2/5% SPC+ mesenchyme cell |  | 41.324 | 17.352 | 0/00707 |
| Scaffold 0% spc + co-culture |  | 42.82 | 14.36 | 0/03536 |
| Scaffold 0% spc + keratinocyte |  | 44.375 | 11.25 | 0/007071 |
| Scaffold 0% spc + mesenchyme cell |  | 45.539 | 8.922 | 0/001414 |
| Control ( vaselin) |  | 45.629 | 8.742 | 0/006364 |
| Scaffold 2/5% SPC+ co-culture | 7 | 25.954 | 48.092 | 0/002124 |
| Scaffold 2/5% SPC+ keratinocyte |  | 35.445 | 29.11 | 0/02121 |
| Scaffold 2/5% SPC+ mesenchyme cell |  | 37.722 | 24.556 | 0/03182 |
| Scaffold 0% spc + co-culture |  | 38.297 | 23.406 | 0/07071 |
| Scaffold 0% spc + keratinocyte |  | 41.324 | 17.352 | 0/01500 |
| Scaffold 0% spc + mesenchyme cell |  | 42.12 | 15.76 | 0/07071 |
| Control ( vaselin) |  | 44.043 | 11.914 | 0/0042 |
| Scaffold 2/5% SPC+ co-culture | 10 | 3.414 | 93.172 | 0/056 |
| Scaffold 2/5% SPC+ keratinocyte |  | 10.735 | 78.53 | 0/014 |
| Scaffold 2/5% SPC+ mesenchyme cell |  | 12.763 | 74.474 | 0/0007 |
| Scaffold 0% spc + co-culture |  | 17.595 | 64.81 | 0/014 |
| Scaffold 0% spc + keratinocyte |  | 33.168 | 33.664 | 0/042 |
| Scaffold 0% spc + mesenchyme cell |  | 35.803 | 28.394 | 0/001414 |
| Control ( vaselin) |  | 35.962 | 28.076 | 0/0015 |
| Scaffold 2/5% SPC+ co-culture | 14 | 0.005 | 99.98 | 0/0495 |
| Scaffold 2/5% SPC+ keratinocyte |  | 5.538 | 88.924 | 0/0127 |
| Scaffold 2/5% SPC+ mesenchyme cell |  | 8.41 | 83.18 | 0/07071 |
| Scaffold 0% spc + co-culture |  | 12.081 | 75.838 | 0/03536 |
| Scaffold 0% spc + keratinocyte |  | 13.38 | 73.24 | 0/027 |
| Scaffold 0% spc + mesenchyme cell |  | 14.441 | 71.118 | 0 |
| Control ( vaselin) |  | 18.617 | 62.766 | 0/091 |

Table 4 The average pathology rate for each of the epidermal and dermal criteria