Electronic Supplementary Information (ESI)

Synthesis of CHA from MFI by three interzeolite transformation strategies and

its Application in NH3-SCR reaction

Table S1. Synthesis conditions and characteristics of products obtained from various combinations of starting silica/alumina source

| Synthesis conditions |  |  |  | Product information |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sample | Starting materials | MFI (SiO2/Al2O3) | Crystallization time[h] | Phase | Solid yield [%] | Relative crystallinity [%] |
| 1 | HSZ+Al | 120 | 1.5 | MFI | — | — |
| 2 |  |  | 2 | CHA(few) + MFI | — | — |
| 3 |  |  | 2.5 | CHA + MFI | — | 33.3 |
| 4 |  |  | 3 | CHA + MFI(few) | 81.8 | 98.5 |
| 5 |  |  | 4 | CHA | 85.0 | 102.6 |
| 6 |  |  | 4.5 | CHA | 85.4 | 103.3 |
| 7 |  |  | 6 | CHA | 83.4 | 100.7 |
| 8 |  |  | 12 | CHA | 82.7 | 103.1 |
| 9 |  |  | 24 | CHA | 84.8 | 102.1 |
| 10 |  |  | 48 | CHA + quartz（few） | 86.7 | 98.0 |
| 11 | CZTZ | 38 | 1.5 | MFI | — | — |
| 12 |  |  | 3 | CHA + MFI | — | 26.7 |
| 13 |  |  | 4.5 | CHA+MOR(few) | 61.4 | 89.5 |
| 14 |  |  | 6 | CHA | 68.7 | 96.2 |
| 15 |  |  | 9 | CHA | 70.2 | 103.4 |
| 16 |  |  | 12 | CHA | 68.4 | 102.5 |
| 17 |  |  | 24 | CHA | 69.5 | 102.9 |
| 18 |  |  | 48 | CHA | 71.8 | 103.1 |
| 19 | LSZ+Si | 24 | 1.5 | MFI | — | — |
| 20 |  |  | 2 | CHA(few) + MFI | — | 33.1 |
| 21 |  |  | 2.5 | CHA + MFI(few) | 60.7 | 79.6 |
| 22 |  |  | 3 | CHA | 64.5 | 100.1 |
| 23 |  |  | 4 | CHA | 65.0 | 101.2 |
| 24 |  |  | 4.5 | CHA | 63.2 | 96.4 |
| 25 |  |  | 6 | CHA | 64.3 | 97.2 |
| 26 |  |  | 12 | CHA | 64.5 | 96.3 |
| 27 |  |  | 24 | CHA + quartz(few) | 64.9 | 96.6 |
| 28 |  |  | 48 | CHA + quartz | 69.6 | 98.1 |

Table S2. Quantification of NH3 desorption amount based on NH3-TPD results

| Samples | Peak A (mmol·g-1) | Peak B (mmol·g-1) | Total amount (mmol·g-1) |
| --- | --- | --- | --- |
| HSZ-4.5 h | 0.37 | 0.50 | 0.87 |
| CZTZ-6 h | 0.37 | 0.57 | 0.94 |
| LSZ-4.5 h | 0.25 | 0.46 | 0.71 |

Fig. S1 (A) H2-TPR profiles and the (B) deconvolution of H2-TPR profiles of

Cu-HSZ-4.5 h, Cu-CZTZ-6 h and Cu-LSZ-4.5 h samples