Supplementary Information for

# Machine learning-enabled inverse design of bioinspired layered composite structures with maximum auxetic performances

This Supplementary Information includes:

Supplementary Discussion S1 to S3

Supplementary Figures S1 to S2

Supplementary Tables S1 to S3

Supplementary References 1 to 4

# Supplementary Discussion

## S1 Poisson's ratio for layered composite structures calculation based on classical laminate theory

In this paper, the IM7/977-3 was selected as the prepreg for layered composite structures (LCSs). The specific material parameters used for both theoretical and numerical analysis are shown in Table S1.

The findings concerning the minimum negative Poisson's ratios (NPR) and the lamination angles of low-dimensional layered composite structures (comprising up to 10 layers) determined through the multi-start resampling algorithm are presented in Table S2.

We concentrate on Poisson's ratio (PR) ν13, which is significantly affected by stiffness. According to the classical laminate theory (CLT), the out-of-plane PR can be calculated by the following equation [1]

ν13=-J31J11,#(S1)

where Jij are elements in the (i,j) entry of matrix J. The exact process will be derived and written in brief below.

For an LCS with arbitrary layup, the relation between load and deformation are written as

NM=ABBDεκ.#(S2)

From Eq. S2, we get

εκ=A*-BD*-1H*BD*-1-D*-1H*D*-1NM.#(S3)

Without the exerted moment, the expression for the strain vector ε can be obtained as

ε=A*-B*D*-1H*N=A-1+A-1BD-BA-1B-1BA-1N=JN,#(S4)

where

J=A-1+A-1BD-BA-1BBA-1.#(S5)

The elements of the aforementioned stiffness matrices A,B, and D can be defined as

Aij,Bij,Dij=k=1N  hk-1hk  Cijk1,Z,Z2dZ.#(S6)

In Eq. S6, Cijk represents the stiffness matrix of kth layer after angle transformation, which can be determined by the stiffness coefficients and the lamination angle θ.

The matrix C [1] is symmetric, with all elements given by the following formula:

C11=C11cos4θ+2C12+4C66cos2θsin2θ+C22sin4θ,C22=C22cos4θ+2C12+4C66cos2θsin2θ+C11sin4θ,C33=C33,C66=C11+C22-2C12-2C66cos2θsin2θ+C66sin4θ+cos4θ,C13=C31=C13cos2θ+C23sin2θ,C23=C32=C23cos2θ+C13sin2θ,C16=C61=C11-C12-2C66cos3θsinθ+C12-C22+2C66cosθsin3θ,C26=C62=C11-C12-2C66cosθsin3θ+C12-C22+2C66cos3θsinθ,C36=C63=C13-C23cosθsinθ.(S7)

## S2 Convergence Proof for the Multi-start Resampling Algorithm

### S2.1 Multi-Start Resampling Algorithm

1. Sampling step.

(a) Set np as the number of population size, ns as the number of sample size.

(b) In the space of [-90,90]N, np as N-dimensional vectors are uniformly generated, denote as Ω.

(c) Choose an initial point x1 at random from Ω.

(d) Choose the next point xi with probability (Pxi=Dxix∈Ω  D(x), where D(xi) is the minimal distance from xi to all sampled points).

(e) Repeat (d) until ns points have been chosen in total.

2. Evaluation step.

(a) For i = 1 ... ns, Do,

(b) Let xi be the starting point,

(c) xi=LS(xi), where LS() is a local search procedure.

(e) End For.

### S2.2 Hierarchical clustering algorithm

The clustering module utilizes the hierarchical clustering algorithm and includes the following steps.

Step 1: For layers N=3 to 20, calculate three indicator variables and two numerical variables to characterize the angular distribution and the minimum NPR at its lowest point for each layer.

Step 2: Calculate the similarity between each layer based on features.

Step 3: Construct a clustering tree based on the distance matrix using the ward linkage criterion. The resulting hierarchy of clusters can be visualized as a dendrogram.

Step 4: Determination of the final clustering results by cutting the dendrogram at a certain height or distance threshold. The cutting height is chosen using the maximum breakpoint of all breakpoints selected by the silhouette coefficient.

### S2.3 Convergence Proof for the Multi-start Resampling Algorithm

The proof involves introducing two key concepts:

1. Convergence Probability p : This is a constant representing the probability that a randomly chosen initial point will eventually converge to the global minimum after iterations.

2. Successful Convergence Number Kc : This is a random variable representing the number of initial points that will eventually converge to the global optimal point.

Here we assume p is a constant and is strictly greater than zero, basing on the assumption that the function f(x) is well-defined and has a global minimum.

When sampling ns random initial points, the successful convergence number Kc follows a binomial distribution with parameters ns and p, i.e., Kc∼Binns,p. Then the probability of no successful convergence point is

PKc=0=(1-p)ns.#(S8)

Therefore, the probability of at least one initial point that converges to global minimum is

PKc>0=1-(1-p)ns.#(S9)

As ns increases to infinity, (1-p)ns approaches 0. That is

limns→∞ PKc>0=1.#(S10)

This shows that with a large enough ns, the probability that at least one initial point will converge to the global minimum approaches 1.

The proportion of successful convergences Kcns has a standard deviation (SD) given by

SDKcns=p(1-p)ns.#(S11)

This indicates that as ns increases, the standard deviation of the proportion of successful convergences approaches zero, reflecting diminishing variability.

## S3 Analytical evidence for 4K LCSs

Highly regular results are typically achieved through numerical solutions; however, the accuracy of these results remains unvalidated, and the mechanisms underlying such regularity have not been fully elucidated. To tackle these critical issues, this section presents a detailed theoretical derivation of the minimum out-of-plane NPR for LCSs. The approach simplifies the task of locating the global minimum point to a polynomial root-finding problem. Remarkably, the optimal lamination angles deduced align precisely with those derived from the previously discussed numerical algorithm, providing indirect validation of the numerical algorithm's accuracy.

For the category N=4K, there are four assumptions as follow:

1. LCS is symmetrically layered.

2. The thickness of each layer is consistent.

3. The absolute value of the angle of each layer is equal.

4. The number of layers with a positive angle equals the number of layers with a negative angle.

The symmetry in Assumption 1 leads to B=0, thereby simplifying the matrix J in the inverse matrix of A. Then, the derivation of this numerical problem proceeds in two main steps. The first step is to use the assumptions to simplify the formula for calculating ν13 to a fraction that only relates to Cij. The second step is to utilize the properties of Cij in terms of sine and cosine functions and apply the substitution method to transform the problem of finding the extremum of ν13 into a polynomial root-finding problem. The process is as follows:

The expression for each element of the matrix A is:

Aij=k=1N  hCijk.#(S12)

From Eq. S14, we can express it in matrix form as follows:

A=hk=1N  Ck,#(S13)

where A and Ck are in matrix form which has been mentioned in Section 1 of SI. There exists an odd power term of sin⁡(θ), which lead C16,C26 and C36 to odd functions in matrix C. Therefore, the nature of the odd function of sin⁡(θ) can be utilized to transform A16,A26 and A36 to 0 under special conditions, which is a result of assumptions 3 and 4. This yields the A matrix as follows:

A=4KhC11C12C130C21C22C230C31C32C330000C66.#(S14)

With the above conditions satisfied, the values of A16,A26 and A36 are all 0 and the elements of the A matrix are simplified. At the same time, A is symmetric matrix. Following, ν13 has the expression:

ν13=-J31J11=-A-131A-111.#(S15)

According to the calculation method of matrix inverse, A-1 can be written as

A-1=1AadjA,#(S16)

where |A| is the determinant of A,  adj(A) is the adjoint matrix of A. Thus,

J11=C66×C22C33-C23C32×(4Kh)3|A|#(S17)J31=C66×C12C23-C22C13×(4Kh)3|A|#(S18)

Since Cij=Cji, the expression for ν13 can be simplified and written as:

ν13=-C12C23-C22C13C22C33-C232.#(S19)

In summary, we have finally simplified ν13 to an expression involving only C12,C13,C22,C23 and C33. Next, we will simplify Cij as a function of θ.

In the expression of C, all Cij has only two forms.

Form 1: C11,C12,C22,C66 can be transformed into a functional relation of the same form. i.e.,

f1θ=acos4θ+bcos2θsin2θ+csin4θ,#(S20)

where a,b, and c are constants.

Form 2: C13,C23 can be transformed into another functional equation of the same form, i.e.,

f2θ=pcos2θ+qsin2θ,#(S21)

where pand q are constants.

The first order derivatives of forms 1 and 2 can be expressed as:

f1'θ=2a-b+csin2θ+b-2asin2θ,#(S22)f2'θ=q-psin2θ.#(S23)

Denoting sin2⁡(θ)=x, we can transform f1,f2, and their derivatives into:

f1=a-b+cx2+b-2ax+a,#(S24)f1'=2a-b+cx+b-2asin2θ,#(S25)f2=q-px+p,#(S26)f2'=q-psin2θ.#(S27)

Next, we can transform the issue of solving the minimum value of ν13 into a matter of calculating the extreme value of ν13. Using the quotient rule for differentiation, the derivation of ν13 can be written as

ν13'=-C12C23-C22C13'C22C33-C232-C12C23-C22C13C22C33-C232'C22C33-C2322.#(S28)

Let

hθ=C12C23-C22C13,#(S29)gθ=C22C33-C232.#(S30)

When ν13'=0,  ν13 has critical points that may be extrema. Therefore, the points where derivatives are zero can be solved to find the corresponding θ values. Consequently, we denote the numerator of ν13' as F(θ), then

Fθ=h'θgθ-hθg'θ,#(S31)

where both terms of h'(θ) and g'(θ) contain sin⁡(2θ). Thus F(θ) can be extracted as a common factor in the expression for sin⁡(2θ), transforming the problem entirely into a problem of solving the zeros of a fourth-degree polynomial in x, where x=sin2⁡(θ). Following, it is sufficient to solve for the value of θ at ν13'=0.

After solving this polynomial equation, which has a pair of conjugate complex roots, a negative root, and only one valid solution, 0.1687, falls in the interval [0,1]. Solving again for sin2⁡(θ)=0.1687, the final result solves with θ=24.5∘ and -24.5∘.

# Supplementary Figures

Fig. S1 Boundary conditions of FEA with mesh convergence and theoretical comparison for 4K-layer LCSs. (a) Boundary conditions and load of the finite element model. (b) Mesh convergence results of FEA (red horizontal and vertical axes) and the comparison between the theoretical results of 4K-layer LCSs and the FEA results (blue horizontal and vertical axes).

Fig. S2 Ultrasonic testing setup and wave speed measurements. (a) Experimental apparatus for performing non-destructive ultrasonic testing. (b) Schematic diagrams of longitudinal and transverse wave measurements of the speed of sound.

# Supplementary Tables

Table S1. Material properties of IM7/977-3 unidirectional lamina [2-4]

| Thickness | E1 | E2 | E3 | ν12 | ν13 | ν23 | G12 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.14mm | 159 GPa | 9.2 GPa | 9.2 GPa | 0.253 | 0.253 | 0.45 | 4.37GPa |

Table S2. Minimum NPRs and corresponding layups for LCSs with 3 layers to 10 layers

| Number of layer | PR value | Layup |
| --- | --- | --- |
| 3(2K+1, K=1) | -0.3128 | [19.3/-30.7/19.3] |
| 4(4K, K=1) | -0.3367 | [24.5/-24.5/-24.5/24.5] |
| 5(2K+1, K=2) | -0.3285 | [21.3/-28.1/21.3/-28.1/21.3] |
| 6(4K+2, K=1) | -0.3347 | [22.3/-25.9/-25/25/25.9/-22.3] |
| 7(2K+1, K=3) | -0.3326 | [22.2/-27/22.2/-27/22.2/-27/22.2] |
| 8(4K, K=2) | -0.3367 | [24.5/24.5/-24.5/-24.5/-24.5/-24.5/24.5/24.5] |
| 9(2K+11, K=4) | -0.3342 | [22.7/-26.5/22.7/-26.5/22.7/-26.5/22.7/-26.5/22.7] |
| 10(4K+2, K=2) | -0.3365 | [25.4/-23.8/-24/24.8/-24.4/24.4/-24.8/24/23.8/-25.4] |
| … | … | … |

Table S3. 7 groups of LCSs ultrasonic calibration PR results

| Sample No. | LCS family & Layup (°) | Long. Sound Vel. (m/s) | Trans. Sound Vel. (m/s) | ν13 Meas. | ν13 Avg. | CLT Theor. ν13 |
| --- | --- | --- | --- | --- | --- | --- |
| 1-A | 3 layers (2K+1) [20/-30/20] | 2754.97 | 2166.67 | -0.310673 | -0.3166 | -0.3124 |
| 1-B |  | 2526.32 | 1990.78 | -0.319167 |  |  |
| 1-C |  | 2628.57 | 2073.24 | -0.323097 |  |  |
| 1-D |  | 2672.94 | 2103.70 | -0.313809 |  |  |
| 2-A | 4 layers (4K) [25/-25]S | 2815.50 | 2228.22 | -0.338084 | -0.3368 | -0.3362 |
| 2-B |  | 2764.10 | 2175.28 | -0.342201 |  |  |
| 2-C |  | 2714.55 | 2145.45 | -0.328872 |  |  |
| 2-D |  | 2713.51 | 2147.59 | -0.338270 |  |  |
| 3-A | 5 layers (2K+1) [20/-30/20/ -30/20] | 2540.00 | 2001.97 | -0.320040 | -0.3267 | -0.3266 |
| 3-B |  | 2710.20 | 2141.97 | -0.331947 |  |  |
| 3-C |  | 2839.74 | 2245.03 | -0.333370 |  |  |
| 3-D |  | 2546.34 | 2007.69 | -0.321603 |  |  |
| 4-A | 6 layers (4K+2) [20/-252/252/ -20] | 2692.22 | 2130.81 | -0.338414 | -0.3335 | -0.3309 |
| 4-B |  | 2788.30 | 2207.41 | -0.339535 |  |  |
| 4-C |  | 2814.46 | 2224.76 | -0.332809 |  |  |
| 4-D |  | 2684.15 | 2117.24 | -0.323433 |  |  |
| 5-A | 9 layers (2K+1) [20/-25/-25/ 20/20/20/ -25/-25/20] | 2695.89 | 2127.57 | -0.325626 | -0.3249 | -0.3234 |
| 5-B |  | 2690.45 | 2122.61 | -0.324271 |  |  |
| 5-C |  | 2535.06 | 2002.05 | -0.328709 |  |  |
| 5-D |  | 2759.73 | 2175.66 | -0.321043 |  |  |
| 6-A | 12 layers (4K) [25/-25]3S | 2807.55 | 2220.90 | -0.336012 | -0.3352 | -0.3362 |
| 6-B |  | 2737.11 | 2220.41 | -0.335998 |  |  |
| 6-C |  | 2730.00 | 2162.38 | -0.341884 |  |  |
| 6-D |  | 2598.79 | 2051.67 | -0.327206 |  |  |
| 7-A | 14 layers (4K+2) [-25/252/-25/25/ -252/252/-25/25/ -252/25] | 2652.85 | 2098.36 | -0.335667 | -0.3347 | -0.3361 |
| 7-B |  | 2714.89 | 2144.54 | -0.329671 |  |  |
| 7-C |  | 2588.24 | 2046.51 | -0.334055 |  |  |
| 7-D |  | 2480.38 | 1963.64 | -0.339535 |  |  |

Note: Subscript "s" denotes the symmetry.

# Supplementary references

[1] Fan, Y., Wang, Y.: The effect of negative poisson's ratio on the low-velocity impact response of an auxetic nanocomposite laminate beam. International Journal of Mechanics and Materials in Design 17, 153-169 (2021)

[2] Li, X., Ma, D., Liu, H., Tan, W., Gong, X., Zhang, C., Li, Y.: Assessment of failure criteria and damage evolution methods for composite laminates under low-velocity impact. Composite Structures 207, 727-739 (2019)

[3] Mohammadi, B., Rohanifar, M., Salimi-Majd, D., Farrokhabadi, A.: Micromechanical prediction of damage due to transverse ply cracking under fatigue loading in composite laminates. Journal of Reinforced Plastics and Composites 36(5), 377-395(2017)

[4] Zhang, J., Zhang, X.: An efficient approach for predicting low-velocity impact force and damage in composite laminates. Composite Structures 130, 85-94 (2015)