Supplementary material

- Supplementary-Method

Field Investigation

(1) Assessment of Pathogenic Distribution:

By visually inspecting or utilizing magnifying glasses and microscopes, observe the morphology of the biota on the surface of the cultural relics and determine the type of deterioration. Next, take photos to record the observed biota, and statistically record the area occupied, with the recording format as shown in Table S1.

(2) Evaluation of Cultural Relic Deterioration:

Based on Table S1, determine the impact of biota on the grotto cultural relics, and then complete the assessment of the degree of cultural relic deterioration caused by biotic factors.

Assessment Criteria for Microbial/Moss Damage Degree on Cultural Relics

| Deteriorative Level /Threat Level | Classification Description of Microbial/Moss Damage on Grotto Cultural Relics | Typical Organisms |
| --- | --- | --- |
| None | No microbial/moss colonization on the surface of Grotto cultural relics, and no obvious damage to areas with inscriptions or patterns. | None |
| Slight | Microbial/moss colonization area on the surface of Grotto cultural relics is less than 10%, and there is slight aesthetic damage to areas with inscriptions or patterns. | Bacteria, fungi, algae |
| Moderate | Microbial/moss colonization area on the surface of Grotto cultural relics is greater than or equal to 10%, but less than 50%, and there is significant aesthetic damage to areas with inscriptions or patterns, without obvious structural damage | Algae, fungi, lichens |
| Severe | Microbial/moss colonization area on the surface of Grotto cultural relics is greater than or equal to 50%, and there is significant aesthetic and structural damage to areas with inscriptions or patterns. | Lichens, moss, other higher plants |

(3) Information on preservation microenvironment

Environmental information, such as average annual temperature and precipitation, were gathered from National Meteorological Data Center of China (http://data.cma.cn).

The investigation present the environmental parameters for the Leshan Giant Buddha area based on data collected between 1950 and 2022 as follow. The annual average temperature is recorded at 17.7°C, with an annual average precipitation of 1332.15 mm. During the summer months (June to August), the average precipitation is 120.79 mm, while the average temperature rises to 29.02°C, and the average relative humidity reaches 79.1%. In contrast, during the winter months (December to February), the average precipitation drops to 69.02 mm, with an average temperature of 8.49°C and an average relative humidity of 74.4%. This seasonal and annual climatic information is crucial for assessing the environmental conditions impacting the conservation of the Leshan Giant Buddha, particularly in relation to moisture levels and temperature variations that may influence the weathering of the stone.

Preparation of Rock Samples:

(1) Use a sieve to obtain rock gravel and clay of different particle sizes from the ISO Standard Sand Co. Ltd (Xiamen, China) and clay gathered from LGB, Sichuan Province, China.

(2) Weigh the gravel and clay according to the particle size distribution of LGB standard sandstone measured by Xie et al. (2021), and mix them together.

(3) Prepare a mixture of Ca(OH)2 and water with a certain amount of water, in a ratio of H2O:Ca(OH)2:sand and clay=1:0.74:10. The higher the concentration of Ca(OH)2, the stronger the compressive strength of the final standard sandstone sample, which serves as the binding material between the sandstone particles.

(4) Pour the mixed clay and gravel into the Ca(OH)2 mixture and stir thoroughly, then fill it into a mold (see Figure 1). Allow the hammer to freely fall from the maximum height and strike the mixture 25 times continuously before removing it and placing it in a carbon dioxide incubator for 10 days.

Carbonic Anhydrase Enzyme Activity Measurement

Sample preparation：1) Tissues were homogenized in extraction buffer at a ratio based on tissue weight (g) to buffer volume (mL) ranging from 1:5 to 1:10. The homogenization was conducted in an ice bath; 2) the homogenate was then subjected to centrifugation at 8000g for 10 minutes at a temperature of 4°C; 3) the supernatant was collected and stored on ice for subsequent analysis. Spectrophotometric Assay: 1) the spectrophotometer was pre-warmed for 30 minutes, and the wavelength was set to 405 nm. Baseline calibration was performed using distilled water; 2) Reagents 1 and 2 were pre-warmed at 25°C for 10 minutes before the assay; 3) in a 1 mL glass cuvette, 100 μL of sample supernatant was added, followed by 700 μL of Reagent 1, and lastly, 200 μL of Reagent 2; 4) the reagents were immediately mixed, and absorbance readings were taken at 405 nm after 3 minutes (A1) and 6 minutes (A2). The change in absorbance (ΔA) was calculated as A2 - A1 and W represents samples fresh weight

(formula 2).

CA activity nmol*min-1*g-1=159.8*(△A-0.001)W

| Statistical Table of Different Types of Defects at All Survey Points of the Leshan Giant Buddha |  |  |  |
| --- | --- | --- | --- |
| Various types of deterioration | Total area of this type of deterioration in all sampling points （cm2） | Percentage of this type of deterioration relative to all deterioration(%) | Percentage of this type of deterioration relative to biological deterioration（%） |
| Bryophyta | 230231 | 50 | 61.8 |
| Lichen | 94601 | 20 | 25.4 |
| Biofilms | 20300 | 4 | 5.4 |
| Plants | 27666 | 6 | 7.4 |
| Powdering | 30479 | 7 | non_biocolonization |
| Discoloration | 62000 | 13 | non_biocolonization |