Supplementary Material for

Optical coherent perfect absorption and amplification in a time-varying medium

Emanuele Galiffi1*⸸, Anthony Harwood2*, Stefano Vezzoli2, Romain Tirole1,2, Andrea Alù1,3‡ & Riccardo Sapienza2†

1Photonics Initiative, Advanced Science Research Center, City University of New York, 85 St. Nicholas Terrace, 10031, New York, USA

2 The Blackett Laboratory, Imperial College London, South Kensington Campus, SW72AZ, London, United Kingdom

3Physics Program, Graduate Center, City University of New York, 365 5th Avenue, 10016, New York, USA

* These authors contributed equally.

⸸ egaliffi@gc.cuny.edu

‡ aalu@gc.cuny.edu

† r.sapienza@imperial.ac.uk

Fig. S1:  Linear characterisation of ITO thin film.

Fig. S2:  Experimental setup

- Theory for temporal coherent control in ITO film

Fig. S3: Illustration of scattering problem

- Eigenvalue problem for bulk subspaces

The scattering problem is shown in Fig. S3. We start from an ansatz for the electric field in the respective subspaces:

Where ,  denotes the respective subspaces (air, ITO, glass), and  refers to causally defined forward and backward sets of waves, namely incoming (-), reflected (+), internal transmitted (-), internal reflected (+) and transmitted (-). Note that in the unmodulated media the out-of-plane wavevector  is trivially related to the frequency according to , but this is not the case inside the ITO, where the dispersion relation is modified by the modulation. Therefore, inside the modulated ITO the superscript (n) labels the eigenstates, not simply the frequencies. Faraday’s Law reads:

Where the different terms are evaluated from the form of our Fourier expansion in Eq.  as:

This gives us the equation:

or, in vector notation:

.

where is a diagonal matrix with components , and the vectors run over all frequencies in the respective fields. For generality, we have removed the superscript on , which now refers to a specific eigenvalue in any subspace. Note that Faraday’s law yields no direct coupling between different frequencies as our time-modulated dielectric parameters do not enter the time-derivatives there.

Let us now consider Ampere-Maxwell’s Law:

We first include a temporal modulation in the background permittivity . The first term on the RHS of Eq.  reads:

which we can rewrite more compactly as:

Taking the inner product, we can write this as an amplitude vector , where  is a tridiagonal matrix with elements:

and  is the Kronecker delta. Note that all the elements of each column share the same pre-factor index n.

We then need to couple Maxwell’s Equations to the equation for the Drude current:

.

Substituting  with the total electron polarization  (neglecting for now the temporal dependence of the material parameters, as commonly assumed) we arrive at:

We will now introduce an ansatz for the polarization analogous to that of Eq. , and assume a temporal dependence of the plasma frequency as , so that Eq.  becomes:

Which we can rewrite using  as:

Taking the inner product, this becomes a linear system, each row of which reads:

Taking the time-derivative of the polarization field multiplies each row by , which results in the polarization contribution to the RHS of Eq.  being written as: , where  is a tridiagonal matrix whose elements read:

(note: all the elements of a row share the same prefactor index). From the x-component of Ampere-Maxwell’s law we obtain the linear set of equations:

This is the first equation that will form our eigenvalue problem for the bulk modes in ITO.

Similarly, the z-component of Ampere-Maxwell’s law gives:

,

allowing us to solve the z-component of the electric field as a function of the magnetic field. This can then be substituted into Eq.  to have the second part of the eigenvalue problem for bulk ITO:

We now have a complete set of equations for the eigenvectors  and eigenvalues :

which allows us to calculate the bulk modes in the three subspaces.

- Scattering problem

Consider a vector of incoming amplitudes  at the surface of ITO. Let us define matrices  whose columns contain the amplitudes of the forward (+) and backward (-) propagating eigenstates that we calculated in the previous section for air (j=1), ITO (j=2) and glass (j=3). For ITO, the distinction between forward and backward waves is non-trivial, and the entire matrix  needs to be used. The total fields at the air-ITO interface read:

in the Fourier basis, where  and  are incoming and reflected field amplitudes. Each entry of this vector corresponds to the in-plane electric (top  entries) or magnetic field (bottom  entries) amplitude for a different frequency. Applying continuity of the respective fields at the interface with the fields  inside ITO, where the vector  contains the amplitudes of the respective eigenstates within ITO, we have:

Each eigenstate of the modulated ITO propagates independently towards the far end (z=d) of the ITO thickness (i.e. the interface with glass). Hence, the amplitude of each eigenstate upon propagation through the ITO is given in the Fourier basis by , where the propagator  is a diagonal matrix whose amplitudes read , where d is the thickness of ITO and the label n refers to the corresponding eigenstate (each of which occupies a column of ). To match the solution at the ITO-glass interface, we set:

where  denotes the amplitudes transmitted into the glass, and “opposite” (i.e. incident from the glass, which will be set to zero later). We can now combine Eqs.  and  to solve for the reflected and transmitted amplitudes:

which is conveniently manipulated in matrix form as:

yielding the desired solution for the electric field amplitudes as:

where  is initialized with the incoming wave amplitude (generally to just 1 at the fundamental harmonic) while all amplitudes of  are set to zero (as there are no incoming waves coming from the glass side).

Fig. S4: Visibility of coherent modulation for 5 wavelengths around the ENZ region

- Coherent modulation for different wavelengths and fluctuation sources

Since there is no resonance at normal incidence in ITO, no surface mode is involved in the modulation process. However, because of the strong dispersion around the ENZ wavelength, shown in Fig. S3, the amount of reflected Signal/Ancilla changes significantly with wavelength, and so does the gain/efficiency of the amplification process. Nevertheless, it is always possible to balance the input powers of Signal and Ancilla and the intensity of the Pump, within reasonable boundaries, in such a way that the observed modulation contrast is optimized at least at one of the detectors. In Fig. S4 we show that consistently high visibility, around 80%, can be obtained for 5 wavelengths around the ENZ region. As in the main manuscript both pump and probe beams are all set at the same wavelength.

The error band is estimated by repeating the same measurements on different days and for slightly different alignment conditions: the Signal and Ancilla beam’s relative size, their spatial and angular overlap at the detector, their spatial and temporal overlap with the pump pulses and the amount of incoherent light impinging on the detector, all greatly affects the attainable minimum of the modulation, which in turns has a large effect on the visibility of the fringes.

- Pump power dependence

Fig. S5a shows the phase conjugate (PC) efficiency, defined as the fraction of the input ancilla power which gets time reversed, as a function of the delay between the ancilla and pump pulses. Similarly, Fig. S5b shows the modulation of the reflected signal versus delay. Unlike the sinusoidal modulation considered in this work which drives the amplification process at optical frequencies and can be considered instantaneous, the reflectivity modulation is associated with intraband electronic transitions induced by the absorption of pump energy and has a timescale of a few 100s fs (see e.g. Ref. [25] in the main text). Both the efficiency of time reversal and the amplitude of the reflectivity modulation increase with pump intensity (expressed in GW/cm2), as also illustrated in the colour maps in the bottom row. Moreover, the delays of maximum phase conjugate generation and minimum reflectivity modulation also slightly shift with the pump power. This is one of the factors affecting the modulation contrast.

Fig. S5:  Power dependence of phase conjugation (PC) and reflection signals as a function of pump-probe delay.

Fig. S6 illustrates the impact of the uneven broadening and red-shifting in the phase conjugation and the reflection spectra on the contrast of the coherent modulation, especially for large pump intensities. At low pump power (panel a), i.e. in the perturbative regime of parametric amplification, the two beams are spectrally very similar and the highest fringe visibility can be obtained. The colourmaps show the recorded spectra resulting from the interference of PC and R at detector 1, as a function of the relative phase Phi between signal and ancilla: the shape of the spectrum changes very little with delay and so almost perfect absorption is achievable around 2pi. At 147 GW/cm2 (panel b) one can start noticing a slant in the spectral map, as not all frequencies are cancelling out or they are not cancelling out for the same delay position, implying the contribution of a spectral phase. At the highest tested intensity (589 GW/cm2, panel c), the broadening is more evident. However, it is more evenly spread between the two beams and so it is possible to recover part of the modulation contrast, as shown in Fig. 4 in the main manuscript.

Fig S6: Effect of spectral broadening and shift at high power on the visibility of the coherent modulation.